This guide specification was issued January 2011 and may be superseded without notice at any time. Therefore, please confirm that this specification is still current and has not been superseded by checking at www.cetco.com or by calling CETCO at 1-847-392-5800.

CAST-IN-PLACE CONCRETE CONSTRUCTION SPECIFICATION

This guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute and is intended for use with cast-in-place concrete or metal decks. Contact CETCO regarding installation and application guidelines for CoreFlex Waterproofing System when used with shotcrete construction. CETCO, Building Materials Group – 1- 800-527-9948.

This master guide specification contains work sections in PART 3 – Execution – pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project.

STRATASEAL HR HOT RUBBERIZED ASPHALT WATERPROOFING GUIDE SPECIFICATION

Split-Slab Construction Assembly

COREFLEX® WATERPROOFING SYSTEM MASTER GUIDELINE SPECIFICATION FOR INTENSIVE GREENROOFS

Part I	General

  - Related Documents

- All of the contract documents, including General and Supplementary General Conditions and Division 1 General Requirements, apply to the work of this section.

  - Description of Work

- The work of this section includes, but is not limited to the furnishing and installing the following materials, per project specifications and drawings, or as directed by the waterproofing membrane manufacturer.

  - Related Sections

- Carefully examine all of the Contract Documents for requirements which affect the work of this section.

- Other specification Sections which directly relate to the work of this section include, but are not limited to, the following:

  - Section 03 50 00 Cast Decks and Underlayment

  - Section 05 30 00 Metal Decking

  - Section 06 10 00 Rough Carpentry

  - Section 07 10 00 Dampproofing and Waterproofing

  - Section 07 25 00 Weather Barriers

  - Section 07 60 00 Flashing and Sheet Metal

  - Section 07 70 00 Roof and Wall Specialties and Accessories

  - Section 07 90 00 Joint Protection

  - System Description

- Provide an intensive greenroof with Elvaloy KEE based thermoplastic reinforced membrane integrally bonded to an Active Polymer Core waterproofing membrane assembly with applicable detailing and accessory products as specified herein and indicated on project drawings.

  - Submittals

- Prior to commencement of the work, process submittals in accordance with the “Conditions of the Contract”.

- Submit manufactures product data complete with general and specific installation instructions, recommendations and limitations.

- Submit product samples representative of the waterproofing membrane, protection layer, insulation, filter fabric, and ballast.

- Submit material certification(s) signed by manufacturer certifying materials comply with specific performance characteristics and physical requirements. Certification must verify that all materials are supplied by a single source manufacturer.

- Submit manufactures written document that installer is certified as a current Approved Applicator with manufacturer.

- Submit sample copy of manufacturer’s waterproofing warranty identifying the terms and conditions.

  - Quality Assurance

- Installer must be a company with a minimum of at least three (3) years experience in work of the type required by this section, who can comply with the manufacturers warranty requirements, and who is an Approved Applicator as determined by manufacturer.

- Manufacturer must be a company with a minimum of forty (40) years in the direct production and sales of waterproofing materials. Manufacturer shall be capable of providing field service representation during construction, and recommending installation methods. Manufacturer shall have certified, approved applicators for membrane installation.

- Conduct a pre-installation conference at least two week prior to commencement of field installation to review conditions, establish procedures to maintain required working conditions and to coordinate this work with related and adjacent work. Representatives of the General Contractor, Architect, Installer, and Manufacturer shall be present at pre-installation conference.

- Construct mock-up of waterproofing membrane incorporating all of the components including: deck, waterproofing membrane, water management layer, filter fabric, growing media, and vegetation. Successful mock-up may remain as part of work.

- Maintain copy of manufacturer’s installation instructions and MSDS for all products on job-site as well as allow access to the job-site by Owner’s Independent Inspector, and Manufacturer Agent.

- Owner shall make arrangements and payments for cost associated with testing the integrity of the waterproofing membrane installation utilizing a proven low-voltage Electronic Leak Detection (ELD) method as approved by waterproofing manufacturer.  The ELD testing shall be selected and approved prior to waterproofing membrane installation, conducted after waterproofing membrane installation is completed and prior to subsequent assembly materials and/or overburden placement. ELD firm shall produce reports and digital photographs documenting the inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

- Owner shall make arrangements and payments for an independent inspection service to monitor installation compliance with the project documents and Manufacturer’s published literature, installation instructions, and site specific details. Independent inspection firm shall be a company participating with the Manufacturer’s Certified Inspection Program. Inspection service shall produce reports and digital photographs documenting each inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

- Documentation of Maintenance Contract: Owner shall provide proof of a 2 year min. maintenance contract with a qualified landscaper or horticulturalist in order to insure that every effort is made to provide professional care to the vegetation and the system supporting the vegetation.  This will insure the viability of the vegetation until it is established and matured.

  - Delivery, Storage and Handling

- Deliver materials in original unopened packaging, clearly labeled with manufacturer’s labels indicating name of manufacturer, product and all identifying numbers.

- Storage of materials must be in an appropriate location and manner as to protect from any construction damage, as well as damage from weather, prolonged sunlight, excessive temperature and sources of ignition. Remove of any damaged material from job-site and dispose of in accordance with applicable regulations. Do not double stack pallets during shipping or storage. Allow adequate ventilation.

- Handling of materials to be in accordance with manufacturers instructions.

  - Project Conditions

- All federal, state and local regulations, codes, and safety standards must be adhered to at all times.

- Do not apply waterproofing system on frost or wet covered surfaces.

- Horizontal deck or roof concrete surfaces should be sloped for proper drainage.

- The deck must be properly cleaned and prepared free of any and all contaminations.

- Form fins, ridges, ponding ridges and other protrusions should be level and smooth with monolithic concrete surface. Honeycombing, aggregate pockets, tie-rod holes and other voids should be completely filled with non-shrink cementitious grout and level with monolithic concrete surface.

- All expansion joints should receive applicable expansion joint sealant product manufactured by others prior to the installation of the CoreFlex Waterproofing System. Expansion joint material is the primary seal at the expansion joint and the expansion joint material manufacturer is responsible for water tightness of the joint.

- Protect adjoining surfaces not to be waterproofed against damage or soiling, including plants, vegetation and animals which may be affected by the waterproofing operations.

- Provide adequate protection for membrane after installation. Do not allow any foot or vehicular traffic on unprotected membrane. Do not allow any material or waste products to contaminate membrane. If contamination should occur contact Manufacturer.

  - Warranty

- Warranty must be validated by Manufacturer confirming acceptance of installation, including independent inspection reports, in accordance with all applicable instructions; as well as the final Electronic Leak Detection report per section 1.06 Quality Assurance.

- Manufacturer’s HydroShield Warranty.

  - HydroShield Warranty: Upon completion and acceptance of the work required by this section, the waterproofing materials manufacturer will provide a written fifteen (15) year warranty, covering both materials and labor to the project owner. Issuance of Manufacturer's HydroShield Warranty requires the following: (1) Waterproofing system products, drainage and insulation course products, and subsequent assembly products shall have been provided by a single manufacturer; (2) Installation of waterproofing products, drainage and insulation course products and subsequent products by Manufacturer's Approved Applicator; (3) Installation inspected by Independent Inspection Firm per Section 1.06G; (4) As applicable, installation of Waterstop-RX in all concrete pour joints. Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties.

Part II	Products

  - General – All components must be single source from membrane manufacturer to ensure system compatibility.

- Provide waterproofing and greenroof assembly materials manufactured or supplied by CETCO:

CETCO

2870 Forbs Avenue

Hoffman Estates, Illinois 60192 USA

800-527-9948 Toll free

847-851-1800 Phone

847-851-1899 Fax

www.cetco.com/BMG

2.011		DISTRIBUTOR

Bowman Construction Supply

10801 E. 54th Avenue

Denver, CO 80239

Phone: (303) 696-8960

  - Materials

- CoreFlex-60 MEMBRANE: 60 mil (1.5 mm) nominal thick Elvaloy KEE based thermoplastic membrane reinforced with a 5.0 oz. weft inserted knit polyester fabric integrally bonded to an Active Polymer Core (APC). Roll size: 54” x 50′ (1.4 m x 15 m). 54” wide thermoplastic membrane with APC layer offset 6” (150 mm) along the long roll edges.

| Physical Properties |  |  |
| --- | --- | --- |
| Property | Test Method | Typical Value |
|  |  | CoreFlex 60 |
| Membrane Composite Thickness | ASTM D751 | 150 mil (3.8 mm) |
| Hydrostatic Pressure Resistance (min 1 hour @ 100 psi) | ASTM D5385 | 231 ft (70 m) |
| Puncture Resistance | ASTM D4833 | 228 lbf (1014 N) |
| Breaking Yield Strength | ASTM D751 | 318 lbf/in (62.2 N/mm) |
| Low Temperature Flexibility (-30°F) | ASTM D2136 | Pass |
| Resistance to Wicking (max. 0.125” (3.2 mm)) | ASTM D751 | Pass |
| Tear Strength | ASTM D4533 | 95 lbf (423 N) |
| Hydrostatic Resistance | ASTM D751 | 756 psi (4.7 mPa) |
| Membrane Bursting Strength | ASTM D751 | 627 lbs (284 kg) |
| Water Vapor Retarder | ASTM E1745 | Class A |
| Water Vapor Transmission | ASTM E96 | 0.1 perms (0.036 gr/m/hr) |
| Tensile Strength | ASTM E154 | 387 lbf/in (68 kN/m) |
| Puncture Resistance | ASTM D1709 | 12 lbs (5500 grams) |

- CoreFlash-60: 60 mil (1.5 mm) nominal reinforced thermoplastic membrane used for non-exposed flashing applications including curbs, walls, field wraps and patches.  Membrane is yellow top coat and black bottom coat. Available in 54’ x 50’ (1.4 m x 15.2 m) rolls.

- CoreFlash-UV:  60 mil (1.5 mm) nominal reinforced UV stable thermoplastic membrane (white top coat) used for flashing applications exposed to direct UV and or weathering conditions. Including curbs, walls, field wraps and patches. Available in54” x 50’ (1.4 m x 15.2 m) rolls.

- CoreFlash-NR:  60 mil (1.5 mm) nominal UV stable non-reinforced extruded white thermoplastic membrane used for above or below grade flashing applications including curbs, walls, field wraps and patches.  Available in 4’ x 24’ (1.2 m x 7.3 m) rolls.

- CoreClad:  24 ga. (0.61 mm) stainless steel sheet laminated with a 20 mil (0.50 mm) nominal thick UV stable compatible thermoplastic coating on one side for above or below grade flashing and detail applications. Available in 4’ x 10’ (1.2 X 3 m) sheets.

- CoreDisc:  4” (100 mm) diameter thermoplastic discs.  Used for attaching CoreFlex membranes to vertical surfaces prior to concrete pour; and also for finishing T-Joints.

- Universal Corner:  Preformed injection molded thermoplastic flashings that will accommodate inside and outside corner details of any dimension. CoreFlex Universal Corners come as one piece and are trimmed to fit the appropriate condition.

- Adhesive SB-100:  Solvent-based adhesive for securing CoreFlash membranes to various substrates, including cured concrete, wood, metal and cementitious boards.

- AkwaSwell:  Hydrophilic polyurethane caulk used for detail work.

- Cortex:  A low permeable geotextile waterproofing material that utilizes Blended Polymer Alloy (BPA) technology.

- Termination Bar: 1/8” x 1” (3.2 mm x 25 mm) stainless steel termination bar punched 6” (150 mm) o. c. or approved equal.

- CETSEAL:  A multipurpose UV stable single component polyether moisture cure sealant / adhesive.  Primary applications are Grade termination Sealant, Membrane Lap Sealant and Waterstop Adhesive.

- Insulation shall be one of the following: (edit to project requirements) (optional)

  - XPS40 – 1.0” , 1.5” or 2” (25 mm, 38 mm or 51 mm) thick extruded polystyrene meeting ASTM C-578 Type VII with a minimum compressive value of 40PSI and a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu (0.88 m2 / kelvins / watt).

  - XPS60- 1.5” or 2.0” (38 mm or 51 mm) thick extruded polystyrene meeting ASTM C-578 Type VII with a minimum compressive value of 60PSI and a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu (0.88 m2 / kelvins / watt).

- Filter Fabric: BB-200 is a non-woven polypropylene geotextile filter fabric that protects the insulation layer by preventing stone and gravel as well as migration of particle fines from dropping between the joints of the insulation. It also can serve as a temporary confining layer for the insulation course when spot ballast is placed over it.

- Aeration Layer: Aquadrain G20 prefabricated 3-dimensional composites meeting the following physical properties: 40,000 PSF (1,915,212 n / m2) compressive strength per ASTM D1621 (mod); thickness of 0.25” (6.35 mm); 7 gpm/ft (87 lpm/m) width flow capacity per ASTM D4716. (edit to project requirements) (optional beneath insulation).

- Drainage / Retention: Aquadrain GS-310 – having a compressive strength per ASTM D1621 (mod) of 9,500 PSF (454 kPa) and a thickness of 1.0” (25 mm) with a flow capacity per ASTM D4716 of30 gpm/ft (376 lpm/m)of width.  GS-310 has 4 oz/sq.yd. (135.62 g/sq. m.) weight non-woven filter fabric on underside and a spun bond filter fabric on the topside.

- Drainage / Retention: Aquadrain GS-315 – having a compressive strength per ASTM D1621 (mod) of 864 PSF (4,218 kg/sq. m) when empty and a thickness of 1.5” (38 mm) with a flow capacity per ASTM D4716 of 23.5 gpm/ft (291.6 l/m width.  Filling the cups of GS-315 with lightweight aggregate greatly increases the compressive strength.

- Filter Fabric: GreenScapes GS-404 with a weight of 4-oz/sq-yd (135.62 g/m2). (for use over the GS-315, not for use over the Aquadrain GS-310).

- Growing Media:  GreenScapes GS-500 series that meets the following performance parameters per project specifications and design.. Growing media shall be capable of supporting the project’s specified vegetation.

| Property | GS-500 Extensive | GS-510 Intensive |
| --- | --- | --- |
| Grain Size Distribution |  |  |
| clay fraction | < 5 % | 0-10 % |
| passing #200 sieve | 1-10 % | 5-20 % |
| passing #60 sieve | 10-25 % | 20-35 % |
| passing #18 sieve | 20-50 % | 35-65 % |
| passing 1/8-inch sieve | 50-80 % | 65-90 % |
| passing 3/8-inch sieve | 80-100 % | 90-100 % |
| Density |  |  |
| Application Density | 0.6 - 1.1 g/cm3 (38 lbs – 69 lbs/cf) | 0.7 - 1.1 g/cm3 (44 lbs – 68 lbs/cf) |
| Saturated Density | 0.9 - 1.44 g/cm3 (56 lbs – 90 lbs/cf) | 1.0 - 1.57 g/cm3 (62 lbs - 98 lbs/cf) |
| Dry Density | 0.58 -1.07 g/cm3 (36 lbs – 67 lbs/cf) | 0.67 -1.15 g/cm3 (42 lbs - 72 lbs/cf) |
| Water & Air Management (% vol.) |  |  |
| saturated water capacity | >30 % | >40 % |
| saturated air content | >10 % | >8 % |
| Saturated Hydraulic Conductivity | .004-012 cm/s (5.4-.16.8 in/hr) | .002-..008 cm/s (2.88-11.3 in/hr) |
| pH, Lime, and Salt Content |  |  |
| pH (saturated paste) | 6.0 - 7.8 | 5.5 - 7.5 |
| carbonate content | <25 g/l | <25 g/l |
| salts content (water extract) | <2.5 g/l (<2.0 mmhos/cm) | <3.0 g/l (2.0 mmhos/cm) |
| Organics* |  |  |
| OM content | 3 – 6 mass % | 5 – 15 mass % |
| C/N ratio | <20 | <20 |
| Nutrients** (plant available) | in lb/1,000 ft3 | in lb/1,000 ft3 |
| nitrogen (NO3) | 3 – 15 | 3 – 15 |
| phosphorus | 1 – 7 | 1 – 7 |
| potassium | 6 – 15 | 6 – 15 |
| CEC Capacity | >5 cmol/kg | >10 cmol/kg |

- Values may be adjusted due to availability of local materials or special project conditions related to plant selection and/or environmental conditions.

- ** Nutrients shall be adjusted with appropriate slow-release fertilizer with micronutrient additions if below lower target range.

- Plants and vegetation shall be per project specifications.

Part III	Execution

  - Inspection

- The Installer, with the Owner’s Independent Inspector, shall examine all surfaces and other conditions under which this section of work is to be performed and notify the contractor in writing of circumstances detrimental to the proper completion of the work. Do not proceed with work until unsatisfactory conditions are corrected and are acceptable for compliance with Manufacturer’s warranty requirements. General conditions acceptable for the installation are list below. For conditions not covered in this Section contact CETCO for application guidance.

  - Preparation

- Cast-in-place concrete or composition decks must be monolithic, smooth, and free of voids, spalled areas, laitance, honeycombs, and protrusions. New concrete should be cured 28-days with a light brush or wood float finish texture. A steel float finish will provide too smooth of a surface for proper adhesion of the waterproofing materials, therefore concrete surfaces that have a steel float finish must be mechanically treated prior to the application of the waterproof material.

- Precast concrete decks shall be mechanically secured to minimize movement. All joints must be grouted.

- Metal decks must be a minimum of 22 gauge steel decking with adequate structural support according to all applicable codes and include gypsum board a minimum thickness of 5/8” (15.8mm) fire rated type “X” and mechanically fastened accordingly to all applicable codes.

- If the project is a re-roof or tear-off, then all existing roofing material must be removed down to the bare deck. The deck must be an acceptable deck type as stated below.

  - Concrete decks must be mechanically cleaned to ensure adequate adhesion of the waterproofing material.

  - Metal decks must be inspected for any signs of deterioration or rust. Remove and replace any sections that have any indication of deterioration or rust.

- Remove all dirt, debris, oil, grease, cement laitance or other foreign matter which will impair the performance of the waterproofing membrane.

- Protect adjacent work areas and finished surfaces from damage or contamination during installation operations.

- Expansion joints should be sealed with applicable expansion joint material by others. Detail waterproofing membrane to expansion joint per manufacturer’s standard details.

  - MEMBRANE WELDING PROCEDURES

    - Welding equipment shall be approved by CETCO. Contact CETCO for a list of suitable equipment.

    - All welding shall be performed only by qualified personnel trained by CETCO prior to field welding.  The technician performing the welding shall supply documentation of individual certification issued by CETCO.

    - Use of automated welding equipment is recommended for all CoreFlex and CoreFlash membrane overlap seams exceeding 10 feet (3 m) in length. Automated equipment can either be hot air welding machine or a wedge welding machine. All welds shall be continuous and without interruption or defect.

    - Prior to welding, start welding equipment and allow it to warm up to optimum welding temperature. Equipment warming period may vary depending on weather conditions and will need to be verified each day and after equipment has been cooled down and restarted and must be confirmed with a test weld.

    - Hot Air Welders: For all field seams use a 1-1/2” (40 mm) wide nozzle to create a nominal 1-1/2” (40 mm) wide homogeneous thermoplastic weld.  Use a minimum ¾ “ (20 mm) wide nozzle for corners, T-joints, patches and other field detailing, maintaining a nominal ¾” (20 mm) wide homogeneous thermoplastic weld. All welds shall be continuous and without interruption or defect.

    - All seams must be clean and dry prior to initiating any field welding procedures. Remove all foreign materials from the seams (dirt, oils, etc.) using CLEAN WHITE COTTON cloths. Do not use denim or synthetic, synthetic blend or paper rags for cleaning.  For detailed cleaning procedures consult CETCO.

    - Contamination occurring within a seam shall be patched to insure water-tight integrity of the weld.

    - Follow equipment manufacturer’s instructions and observe local codes and site requirements for electricity supply, grounding, GFI and other current protection. Dedicated circuit, house power or a dedicated portable generator is required. No other equipment (including but not limited to hand welders) shall be operated off the dedicated power source.

    - T-Joints (multiple overlaps)

- A 4” (100 mm) CoreDisc is required centered and hot air welded at the T-Joint intersection using the following steps.

- All membrane edges forming the T-Joint that will be covered by the CoreDisc, plus 1” (25 mm) beyond, must be feathered to provide a smooth transition for the CoreDisc. The feathering can be accomplished with a hot nozzle of hand welding tool.

- While hand welding the CoreDisc, use the edge of the hand roller to conform the CoreDisc completely to the thermoplastic membrane overlaps to prevent voids at the feathered membrane edges.

    - Hand Welding seams shall be competed per the following three steps.

- Step One:  Intermittently tack weld the overlap to hold the thermoplastic membrane overlap in place and maintain a uniform overlap width (minimum 4” (100 mm)).

- Step Two:  Insert the nozzle into the back of the overlap.  With a silicone roller pinch off the back edge to trap the hot air and make a thin pre-weld. The pre-weld will serve to concentrate heat along the exterior edge of the overlap during step three.

- Step Three:  Insert the nozzle of the hand welder into the lap at a 45° angle relative to the sheet edge. As the thermoplastic membrane surface begins to flow, apply light pressure with a hand roller oriented at a right angle to the tip of the hand welder.  As rolled, a small bead of molten material should bleed out of the seam edge.

    - Machine Welding

- Automated Hot-Air Welders

        - Use a 1-1/2” (40 mm) wide nozzle to create a nominal 1-1/2” (40 mm) wide homogeneous thermoplastic weld. Depending on the location of the bearing weight and design of the equipment, a sheet metal track may be required. Welds shall be continuous and without interruption or defect.

- .

    - Wedge Welders

- Use a minimum 2” (50 mm) wide wedge to create a nominal 2” (50 mm) wide homogeneous thermoplastic weld without interruption or defect.

- Membrane overlap assembly may need to be increased according to the requirements of the equipment.

- Prior to wedge welding, fold the APC geotextile selvage edge of the bottom sheet back under and out of the way in order for the thermoplastic membrane of the bottom sheet to make contact with the wedge.  Fold back the APC selvage edge for the entire length to be welded.

- After completing thermoplastic weld, lift up membrane and unfold the APC geotextile selvage edge to provide minimum 4” (100 mm) APC to APC overlap at the membrane overlap assembly.

    - Quality Control/Inspection of Welded Seams

- All welds shall be inspected by the waterproofing applicator’s job foreman and/or supervisor daily after cooling. Weld continuity inspection shall include, but not be limited to, the probing of all field welds with a rounded screwdriver or other dull pointed instrument.  Immediately mark and remediate any deficiencies per CETCO guidelines.

- Each days welding should begin with an evaluation of welded seams conducted on a test strip of membrane. Adjust equipment speed and or heat/power settings as necessary to achieve proper welds. Cut out and retain a 2” – 4” (50 mm – 100 mm) wide seam sample, date it and retain for the independent inspector/owners rep. from the test weld. Further testing may be required as conditions change during the day, as problems arise or at the independent inspector/owners rep. discretion. Taking samples of completed waterproofing should be avoided whenever possible. However, when necessary, each test cut shall be filled with Cortex and patched with CoreFlash extending 4” (100 mm) beyond the edges of the cut opening and completed with a homogeneous thermoplastic weld.  Each test cut shall be patched by the waterproofing applicator at no additional cost to the owner.

- Ensure that all aspects of the installation (sheet layout, attachment, welding, flashing details, etc.) are in strict accordance with the most current CETCO Specifications and Details. Excessive patching of field seams because of inexperienced or poor workmanship will not be accepted at time of FINAL INSPECTION FOR WARRANTY ACCEPTANCE. Deviations from this specification and/or details must be authorized in writing by CETCO, prior to execution.  Deviations from this procedure may result in forfeiture of warranty eligibility.

    - Perform Electronic Leak Detection (ELD) test over the entire waterproofing membrane installation per Quality Assurance Section 1.06F.  For areas to receive ELD testing provide the following:

- Prior to installation of the waterproofing membrane a complete installation and field testing procedure guideline, as provided by the ELD system manufacturer, shall be provided to the installer, General Contractor, Manufacturer, Architect and Owner.

- Thoroughly wet the waterproofing membrane in area of test.  Wetting can be accomplished by hand or mechanical spray devises.  Membrane must be wet during the testing procedures.  Ponded water is not necessary.

- Visually inspect and perform ELD testing to locate membrane breaches, if any. Document location of breaches found by the ELD test and visual inspections.

- Repair all breaches found per waterproofing manufacturer’s guidelines. Leave ELD conductor wire grid in place as secured to waterproofing membrane.

- Once membrane ELD testing is concluded and all repairs are complete, the membrane shall be immediately protected. General Contractor shall prohibit non-waterproofing construction traffic, activity and material storage on the tested membrane.

    - Insulation

- Install the insulation loose over the waterproofing membrane or Aeration Layer (if used), firmly butting each adjacent board. Do not leave gaps between adjacent boards.

- If multiple layers of insulation are required, then install the thicker layer on the bottom. Rotate the direction of each layer 90° and stager seams. All layers of insulation must be un-adhered to each other.

- Cut insulation to fit close to all cants, protrusions, and obstructions.

    - Insulation Filter Fabric

- Install BB-200 over the insulation overlapping the seams 6” (150mm) Cut to fit tightly at perimeters, corners and at all penetrations..

    - Drainage Layer (edit to requirements

- Install Aquadrain GS-315 or GS-310 course over the BB-200 in accordance with Manufacturers installation procedures.

- Cut drainage to fit close to all perimeter, protrusions and obstructions.

- Place subsequent ballast materials on as soon as possible.

    - Filter Fabric (for use in areas with Aquadrain GS-315)

- Place the filter fabric over the GS-315 drainage/retention layer.

- Overlap all edges 12” (100 mm) with a minimum of 6’ (150 mm) between all overlaps. Keep overlaps a minimum of 6’ from all perimeters. Secure filter fabric under any perimeter metal counter flashings.

- Cut filter fabric around any drainage openings so to not restrict water flow to the drain. Cut filter fabric around any penetrations in such a manner as to prevent any stone ballast from entering between penetration and insulation.

- Place subsequent ballast materials on as soon as possible.

    - Growing Media

- Install specified growing media in strict accordance with the project and design requirements. Avoid damage or displacement of other components including filter fabric, insulation, drainage composite, wall, hardscape and roofing.

    - Vegetation

- Install vegetation in strict accordance with the landscape architect / landscape designer’s instructions and plans following proper landscaping techniques.

- Follow all maintenance instructions as provided by architect or landscape designer.

    - Hardscape/Pavers

- Install hardscapes and/or pavers per project specifications and project layout drawings. Install in strict accordance with manufacturer’s installation guidelines.

  - Job Completion

    - Clean-Up

- In areas where adjacent finished surfaces are soiled by work of this Section, consult Manufacturer of surfaces for cleaning advice and conform to their recommendations and instructions.

- Remove all debris, tools, equipment and remaining product on-site. Dispose of debris and damaged product following all applicable regulations.

    - Inspection

      - The Installer with the Owner’s Independent Inspector shall examine all completed work.

END OF SECTION 071354