This guide specification was issued January 2011 and may be superseded without notice at any time. Therefore, please confirm that this specification is still current and has not been superseded by checking at www.cetco.com or by calling CETCO at 1-847-392-5800.

CAST-IN-PLACE CONCRETE CONSTRUCTION SPECIFICATION

This guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute and is intended for use with cast-in-place concrete or metal decks. Contact CETCO regarding installation and application guidelines for CoreFlex Waterproofing System when used with shotcrete construction. CETCO, Building Materials Group – 1- 800-527-9948.

This master guide specification contains work sections in PART 3 – Execution – pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project.

STRATASEAL HR HOT RUBBERIZED ASPHALT WATERPROOFING GUIDE SPECIFICATION

COREFLEX® WATERPROOFING SYSTEM MASTER GUIDELINE SPECIFICATION FOR EXTENSIVE GREENROOFS – HIGH SLOPE APPLICATIONS

- General

  - Related Documents

- All of the contract documents, including General and Supplementary General Conditions and Division 1 General Requirements, apply to the work of this section.

  - Description of Work

- The work of this section includes, but is not limited to the furnishing and installing the following materials, per project specifications and drawings, or as directed by the waterproofing membrane manufacturer.

  - Related Sections

- Carefully examine all of the Contract Documents for requirements which affect the work of this section.

- Other specification Sections which directly relate to the work of this section include, but are not limited to, the following:

  - Section 03 50 00 Cast Decks and Underlayment

  - Section 05 30 00 Metal Decking

  - Section 06 10 00 Rough Carpentry

  - Section 07 10 00 Dampproofing and Waterproofing

  - Section 07 25 00 Weather Barriers

  - Section 07 60 00 Flashing and Sheet Metal

  - Section 07 70 00 Roof and Wall Specialties and Accessories

  - Section 07 90 00 Joint Protection

  - System Description

- Provide an extensive greenroof with Elvaloy KEE based thermoplastic reinforced membrane integrally bonded to an Active Polymer Core waterproofing membrane assembly with applicable detailing and accessory products as specified herein and indicated on project drawings.

  - Submittals

- Prior to commencement of the work, process submittals in accordance with the “Conditions of the Contract”.

- Submit manufactures product data complete with general and specific installation instructions, recommendations and limitations.

- Submit product samples representative of the waterproofing membrane, protection layer, insulation, filter fabric, and ballast.

- Submit material certification(s) signed by manufacturer certifying materials comply with specific performance characteristics and physical requirements. Certification must verify that all materials are supplied by a single source manufacturer.

- Submit manufactures written document that installer is certified as a current approved Applicator with manufacturer.

- Submit sample copy of manufacturer’s waterproofing warranty identifying the terms and conditions.

  - Quality Assurance

- Installer must be a company with a minimum of at least three (3) years experience in work of the type required by this section, who can comply with the manufacturers warranty requirements, and who is an Approved Applicator as determined by manufacturer.

- Manufacturer must be a company with a minimum of forty (40) years in the direct production and sales of waterproofing materials. Manufacturer shall be capable of providing field service representation during construction, and recommending installation methods. Manufacturer shall have certified, approved applicators for membrane installation.

- Conduct a pre-installation conference at least two weeks prior to commencement of field installation to review conditions, establish procedures to maintain required working conditions and to coordinate this work with related and adjacent work. Representatives of the General Contractor, Architect, Installer, and Manufacturer shall be present at pre-installation conference.

- Construct mock-up of waterproofing membrane incorporating all of the components including: deck, waterproofing membrane, water management layer, filter fabric, growing media, and vegetation. Successful mock-up may remain as part of work.

- Maintain copy of manufacturer’s installation instructions and MSDS for all products on job-site as well as allow access to the job-site by Owner’s Independent Inspector, and Manufacturer Agent.

- Owner shall make arrangements and payments for cost associated with testing the integrity of the waterproofing membrane installation utilizing a proven low-voltage Electronic Leak Detection (ELD) method as approved by waterproofing manufacturer.  The ELD testing method shall be selected and approved prior to waterproofing membrane installation, conducted after waterproofing membrane installation is completed and prior to subsequent assembly materials and/or overburden placement. ELD firm shall produce reports and digital photographs documenting the inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

- Owner shall make arrangements and payments for an independent inspection service to monitor installation compliance with the project documents and Manufacturer’s published literature, installation instructions, and site specific details. Independent inspection firm shall be a company participating with the Manufacturer’s Certified Inspection Program. Inspection service shall produce reports and digital photographs documenting each inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

- Documentation of Maintenance Contract: Owner shall provide proof of a 2 year min. maintenance contract with a qualified landscaper or horticulturist in order to insure that every effort is made to provide professional care to the vegetation and the system supporting the vegetation.  This will insure the viability of the vegetation until it is established and matured.

  - Delivery, Storage and Handling

- Deliver materials in original unopened packaging, clearly labeled with manufacturers’ labels indicating name of manufacturer, product and all identifying numbers.

- Storage of materials must be in an appropriate location and manner as to protect from any construction damage, as well as damage from weather, prolonged sunlight, excessive temperature and sources of ignition. Remove of any damaged material from job-site and dispose of in accordance with applicable regulations. Do not double stack pallets during shipping or storage. Allow adequate ventilation.

- Handling of materials to be in accordance with manufacturers instructions.

  - Project Conditions

- All federal, state and local regulations, codes, and safety standards must be adhered to at all times.

- Do not apply waterproofing system on frost or wet covered surfaces.

- Horizontal deck or roof concrete surfaces should be sloped for proper drainage.

- The deck must be properly cleaned and prepared free of any and all contaminations.

- Form fins, ridges, ponding ridges and other protrusions should be level and smooth with monolithic concrete surface. Honeycombing, aggregate pockets, tie-rod holes and other voids should be completely filled with non-shrink cementitious grout and level with monolithic concrete surface.

- All expansion joints should receive applicable expansion joint sealant product manufactured by others prior to the installation of the CoreFlex Waterproofing System. Expansion joint material is the primary seal at the expansion joint and the expansion joint material manufacturer is responsible for water tightness of the joint.

- Protect adjoining surfaces not to be waterproofed against damage or soiling, including plants, which may be affected by the waterproofing operations.

- Provide adequate protection for membrane after installation. Do not allow any foot or vehicular traffic on unprotected membrane. Do not allow any material or waste products to contaminate membrane. If contamination should occur contact Manufacturer.

  - Warranty

- Warranty must be validated by Manufacturer confirming acceptance of installation, including independent inspection reports, in accordance with all applicable instructions; as well as the final Electronic Leak Detection report per section 1.06 Quality Assurance.

- Manufacturer’s HydroShield Warranty.

    - Waterproofing Warranty: Upon completion and acceptance of the work required by this section, the waterproofing materials manufacturer will provide a written fifteen (15) year warranty, covering both materials and labor to the project owner. Issuance of Manufacturer's HydroShield Warranty requires the following: (1) Waterproofing system products, drainage and insulation course products, and subsequent assembly products shall have been provided by a single manufacturer; (2) Installation of waterproofing products, drainage and insulation course products and subsequent products by Manufacturer's Approved Applicator; in accordance with Hydroshield Program, (3) Installation inspected by Independent Inspection Firm per Section 1.06; (4) As applicable, installation of Waterstop-RX in all concrete pour joints. Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties.

    - Plant Coverage Warranty: Upon completion and acceptance of the work required by this section, the greenroof materials manufacturer will provide a written two (2) year warranty, covering the growth and establishment of the vegetative greenroof cover to 80% coverage of the greenroof planted surface.  Issuance of the Manufacturer’s Vegetative Coverage Warranty requires the following: (1) Waterproofing system products, root barrier, drainage, insulation, growing media and plant material shall have been provided by a single manufacturer, (2) Installation of growing media and plant material shall have been performed by Manufacturer's Approved Applicator or Landscaper; (3) Installation inspected by Independent Inspection Firm per Section 1.06; (4) Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties; (5) Two-year Vegetation Maintenance Program shall be implemented.

- PRODUCTS (edit to requirements)

  - General - All components must be single source from membrane manufacturer to ensure system compatibility.

- Provide waterproofing and greenroof assembly materials manufactured or supplied by CETCO:

CETCO

2870 Forbs Avenue

Hoffman Estates, Illinois 60192 USA

800-527-9948 Toll free

847-851-1800 Phone

847-851-1899 Fax

www.cetco.com/BMG

2.011		DISTRIBUTOR

Bowman Construction Supply

10801 E. 54th Avenue

Denver, CO 80239

Phone: (303) 696-8960

  - Materials

- CoreFlex-60 MEMBRANE: 60 mil (1.5 mm) nominal thick Elvaloy KEE based thermoplastic membrane reinforced with a 5.0 oz. weft inserted knit polyester fabric integrally bonded to an Active Polymer Core (APC). Roll size: 54” x 50′ (1.4 m x 15 m). 54” wide thermoplastic membrane with APC layer offset 6” (150 mm) along the long roll edges.

| Physical Properties |  |  |
| --- | --- | --- |
| Property | Test Method | Typical Value |
|  |  | CoreFlex 60 |
| Membrane Composite Thickness | ASTM D751 | 150 mil (3.8 mm) |
| Hydrostatic Pressure Resistance (min 1 hour @ 100 psi) | ASTM D5385 | 231 ft (70 m) |
| Puncture Resistance | ASTM D4833 | 228 lbf (1014 N) |
| Breaking Yield Strength | ASTM D751 | 318 lbf/in (62.2 N/mm) |
| Low Temperature Flexibility (-30°F) | ASTM D2136 | Pass |
| Resistance to Wicking (max. 0.125” (3.2 mm)) | ASTM D751 | Pass |
| Tear Strength | ASTM D4533 | 95 lbf (423 N) |
| Hydrostatic Resistance | ASTM D751 | 756 psi (4.7 mPa) |
| Membrane Bursting Strength | ASTM D751 | 627 lbs (284 kg) |
| Water Vapor Retarder | ASTM E1745 | Class A |
| Water Vapor Transmission | ASTM E96 | 0.1 perms (0.036 gr/m/hr) |
| Tensile Strength | ASTM E154 | 387 lbf/in (68 kN/m) |
| Puncture Resistance | ASTM D1709 | 12 lbs (5500 grams) |

- CoreFlash-60: 60 mil (1.5 mm) nominal reinforced thermoplastic membrane used for non-exposed flashing applications including curbs, walls, field wraps and patches.  Membrane is yellow top coat and black bottom coat. Available in 54” x 50’ (1.4 m x 15.2 m) rolls.

- CoreFlash-UV:  60 mil (1.5 mm) nominal reinforced UV stable thermoplastic membrane (white top coat) used for flashing applications exposed to direct UV and or weathering conditions. Including curbs, walls, field wraps and patches. Available in54” x 50’ (1.4 m x 15.2 m) rolls.

- CoreFlash-NR:  60 mil (1.5 mm) nominal UV stable non-reinforced extruded white thermoplastic membrane used for above or below grade flashing applications including curbs, walls, field wraps and patches.  Available in 4’ x 24’ (1.2 m x 7.3 m) rolls.

- CoreClad:  24 ga. (0.61 mm) stainless steel sheet laminated with a 20 mil (0.50 mm) nominal thick UV stable compatible thermoplastic coating on one side for above or below grade flashing and detail applications. Available in 4’ x 10’ (1.2 X 3 m) sheets.

- CoreDisc:  4” (100 mm) diameter thermoplastic discs.  Used for attaching CoreFlex membranes to vertical surfaces prior to concrete pour; and also for finishing T-Joints.

- Universal Corner:  Preformed injection molded thermoplastic flashings that will accommodate inside and outside corner details of any dimension. CoreFlex Universal Corners come as one piece and are trimmed to fit the appropriate condition.

- Adhesive SB-100:  Solvent-based adhesive for securing CoreFlash membranes to various substrates, including cured concrete, wood, metal and cementitious boards.

- AkwaSwell:  Hydrophilic polyurethane caulk used for detail work.

- Cortex:  A low permeable geotextile waterproofing material that utilizes Active Polymer Core (APC) technology.

- Termination Bar:	1/8” x 1” (3.2 mm x 25 mm) stainless steel termination bar punched 6” (150 mm) O. C.

- CETSEAL:  A multipurpose UV stable single component polyether moisture cure sealant / adhesive.  Primary applications are Grade termination Sealant, Membrane Lap Sealant and Waterstop Adhesive.

- Insulation shall be one of the following: (edit to project requirements) (optional)

  - XPS40 – 1.0” , 1.5” or 2” (25 mm, 38 mm or 51 mm) thick extruded polystyrene meeting ASTM C-578 Type VII with a minimum compressive value of 40PSI and a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu (0.88 m2 / kelvins / watt).

  - XPS60- 1.5” or 2.0” (38 mm or 51 mm) thick extruded polystyrene meeting ASTM C-578 Type VII with a minimum compressive value of 60PSI and a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu (0.88 m2 / kelvins / watt).

- Filter Fabric: BB-200 is a non-woven polypropylene geotextile filter fabric that protects the insulation layer by preventing stone and gravel as well as migration of particle fines from dropping between the joints of the insulation. It also can serve as a temporary confining layer for the insulation course when spot ballast is placed over it.

- Aeration Layer: Aquadrain G20 prefabricated 3-dimensional composites meeting the following physical properties: 40,000 PSF (1,915,212 n / m2) compressive strength per ASTM D1621 (mod); thickness of 0.25” (6.35 mm); 7 gpm/ft (87 lpm/m) width flow capacity per ASTM D4716. (edit to project requirements) (required with combination of moisture retention mat and insulation)

- Moisture Retention Mat: GS-232 with a weight of 32-oz/sq-yd (1.085 kg/m2). (Aeration layer required between insulation and Moisture Retention mat)

- Drainage: Aquadrain GS-300 – having a compressive strength per ASTM D1621 (mod) of 30,000 PSF (1,436,407 n/M2) and a thickness of 0.45 inches (11.4 mm) with a flow capacity per ASTM D4716 of 22.5 gpm/ft. (276 lpm/m) of width.  GS-300 has a 120 g/m2 spunbond filter fabric on the upper side.

- Drainage / Retention: Aquadrain GS-310 – having a compressive strength per ASTM D1621 (mod) of 9,500 PSF (454 kPa) and a thickness of 1.0” (25 mm) with a flow capacity per ASTM D4716 of 30 gpm/ft (376 lpm/m)of width.  GS-310 has a 4 oz/sq-yd (94.8 g/m2) weight non-woven fabric on the underside and a 100 g/m2 weight spun bond filter fabric on the topside.

- Drainage / Retention: Aquadrain GS-315 – having a compressive strength per ASTM D1621 (mod) of  864 PSF (4,218 kg/m2) when empty and thickness of 1.5 inches (38 mm) with a flow capacity per ASTM D4716 of 23.5 gpm/ft (291.6 l/m width).  Filling the cups of the GS-315 with lightweight aggregate greatly increases the compressive strength.

- Filter Fabric: GS-404 with a weight of 4.0 oz/sq. yd. (94.8 g/sq. m)   For use over the Aquadrain GS-315, not for use over over the GS-310.

- Geocell Cellular Soil Confinement: For areas where high slope is of concern  the CETCO High Slope Cellular Confinement Assembly will be added over the filter fabric or drainage/retention/filter fabric composite.  The assembly consists of high density polyethylene panels that form cells when expanded in place.  The panel height should be ½ to 1 inch lower than the intended growing media depth to hide the top of the panel.  The panels are held in place with 3/16 inch stainless steel cable tendons that are attached to the structure by looping them through a minimum ¼ inch OD eyebolts.  Subsequent topping (erosion control blankets or pre-vegetated tiles or mats) are secured to the panels with heavy gauge aluminum wire placed through perforations in the panel and twisted into place over the topping material.

- Growing Media:  GreenScapes GS-500 series that meets the following performance parameters per project specifications and design. Growing media shall be capable of supporting the project’s specified vegetation.

| Property | GS-500 Extensive | GS-510 Intensive |
| --- | --- | --- |
| Grain Size Distribution |  |  |
| clay fraction | < 5 % | 0-10 % |
| passing #200 sieve | 1-10 % | 5-20 % |
| passing #60 sieve | 10-25 % | 20-35 % |
| passing #18 sieve | 20-50 % | 35-65 % |
| passing 1/8-inch sieve | 50-80 % | 65-90 % |
| passing 3/8-inch sieve | 80-100 % | 90-100 % |
| Density |  |  |
| Application Density | 0.6 - 1.1 g/cm3 (38 lbs – 69 lbs/cf) | 0.7 - 1.1 g/cm3 (44 lbs – 68 lbs/cf) |
| Saturated Density | 0.9 - 1.44 g/cm3 (56 lbs – 90 lbs/cf) | 1.0 - 1.57 g/cm3 (62 lbs - 98 lbs/cf) |
| Dry Density | 0.58 -1.07 g/cm3 (36 lbs – 67 lbs/cf) | 0.67 -1.15 g/cm3 (42 lbs - 72 lbs/cf) |
| Water & Air Management (% vol.) |  |  |
| saturated water capacity | >30 % | >40 % |
| saturated air content | >10 % | >8 % |
| Saturated Hydraulic Conductivity | .004-012 cm/s (5.4-.16.8 in/hr) | .002-..008 cm/s (2.88-11.3 in/hr) |
| pH, Lime, and Salt Content |  |  |
| pH (saturated paste) | 6.0 - 7.8 | 5.5 - 7.5 |
| carbonate content | <25 g/l | <25 g/l |
| salts content (water extract) | <2.5 g/l (<2.0 mmhos/cm) | <3.0 g/l (2.0 mmhos/cm) |
| Organics* |  |  |
| OM content | 3 – 6 mass % | 5 – 15 mass % |
| C/N ratio | <20 | <20 |
| Nutrients** (plant available) | in lb/1,000 ft3 | in lb/1,000 ft3 |
| nitrogen (NO3) | 3 – 15 | 3 – 15 |
| phosphorus | 1 – 7 | 1 – 7 |
| potassium | 6 – 15 | 6 – 15 |
| CEC Capacity | >5 cmol/kg | >10 cmol/kg |

- Values may be adjusted due to availability of local materials or special project conditions related to plant selection and/or environmental conditions.

- ** Nutrients shall be adjusted with appropriate slow-release fertilizer with micronutrient additions if below lower target range.

- Erosion Control Blanket: GS-624 100% biodegradable erosion control blanket designed to provide heavy-duty wind and water surface erosion protection.  GS-624 is used over the GS-500 series growing media when planting CETCO Greenroof Plugs or CETCO Greenroof Sedum Cuttings.   GS-624 is not for use when planting CETCO Pre-Vegetated Tiles or Mats.

- CETCO Extensive Greenroof Plants: Specified plants supplied by CETCO via qualified growers per project specifications.

- Source Responsibility: The vegetated roof plant material shall be (edit to requirements) Greenroof Plugs (72-cell; 24-cell), Bulk Sedum Cuttings, Sedum Tiles, Sedum Carpet

- Contact: 	CETCO

2870 Forbs Avenue

Hoffman Estates, IL 60192

847-851-1823

steve.skinner@cetco.com

- Plant Material

        - CETCO Greenroof Plugs CETCO Greenroof Plugs shall be healthy, vigorous, well rooted and established in the container in which they are growing.  They shall have tops of good quality and be in a healthy growing condition.  They shall have a well-established root system reaching the sides of the container and maintain a firm, complete root ball upon removal from the container. CETCO Greenroof Plugs shall be grown and delivered in a continuous plug tray and conform to the following cell count and plug size. (edit to requirements)	24-cell plugs  2 5/8” w x 2 ½” d 72-cell plugs 1 ½’ w x 2” d.

        - CETCO Sedum Cuttings CETCO Sedum Cuttings shall be harvested from healthy, vigorous plants while in a vegetative growth mode.  They shall range in length from ½” to 3” and possess sufficient rooting nodes to allow for rapid root development once sown.  CETCO Greenroof Cuttings shall be harvested, cooled and dried for 24 hours prior to boxing for shipment and delivered in an insulated box with enclosed ice packs to ensure the cuttings remain cool until they are delivered.

        - CETCO Sedum Pre-Vegetated Tiles:

- CETCO Sedum Tiles are made up of a coconut fiber base filled with a planting substrate, and pre-cultivated with a layer of low-profile, drought-tolerant vegetation adapted to rooftop conditions.  They measure 15” x 20” (2.08 square feet)

        - CETCO Pre-Vegetated Sedum Mat

- CETCO Sedum Mat are made up of a coconut fiber base filled with a planting substrate, and pre-cultivated with a layer of low-profile, drought-tolerant vegetation adapted to rooftop conditions.  They measure 1m X 2m (25 square feet)

- CETCO Sedum Mats are made up of a coconut fiber base covered with a planting substrate, and pre-cultivated with a layer of low-profile, drought-tolerant vegetation adapted to rooftop conditions.

- Each Sedum Mats measure approximately 48” wide by 75” long and ranges from 1” to 2” in height on delivery

- CETCO Sedum Mats maximum wet weight is 150 lbs. each (6.0 lbs/sf).

- CETCO Sedum Mats shall have a minimum 85% vegetation coverage upon delivery to the site using a succulent plant mix of 8-11 varieties of Sedum.

Part 3   EXECUTION

  - INSPECTION

    - The Installer, with the Owner’s Independent Inspector, shall examine all surfaces and other conditions under which this section of work is to be performed and notify the contractor in writing of circumstances detrimental to the proper completion of the work. Do not proceed with work until unsatisfactory conditions are corrected and are acceptable for compliance with Manufacturer’s warranty requirements. General conditions acceptable for the installation are list below. For conditions not covered in this Section contact CETCO for application guidance.

  - PREPARATION

- Cast-in-place concrete or composition decks must be monolithic, smooth, and free of voids, spalled areas, laitance, honeycombs, and protrusions. New concrete should be cured 28-days with a light brush or wood float finish texture. A steel float finish will provide too smooth of a surface for proper adhesion of the waterproofing materials, therefore concrete surfaces that have a steel float finish must be mechanically treated prior to the application of the waterproof material.

- Precast concrete decks shall be mechanically secured to minimize movement. All joints must be grouted.

- Metal decks must be a minimum of 22 gauge (0.76 mm) steel decking with adequate structural support according to all applicable codes and include gypsum board a minimum thickness of 5/8” (15.8mm) fire rated type “X” and mechanically fastened accordingly to all applicable codes.

- If the project is a re-roof or tear-off, then all existing roofing material must be removed down to the bare deck. The deck must be an acceptable deck type as stated below.

  - Concrete decks must be mechanically cleaned to ensure adequate adhesion of the waterproofing material.

  - Metal decks must be inspected for any signs of deterioration or rust. Remove and replace any sections that have any indication of deterioration or rust.

- Remove all dirt, debris, oil, grease, cement laitance or other foreign matter which will impair the performance of the waterproofing membrane.

- Protect adjacent work areas and finished surfaces from damage or contamination during installation operations.

- Expansion joints should be sealed with applicable expansion joint material. Detail waterproofing membrane to expansion joint per manufacturer’s standard details.

- It is the responsibility of the Installer and Designer to verify load limits for the roof structure prior to installation of the greenroof elements.

  - MEMBRANE WELDING PROCEDURES

- Welding equipment shall be approved by CETCO. Contact CETCO for a list of suitable equipment

- All welding shall be performed only by qualified personnel trained by CETCO prior to field welding.  The technician performing the welding shall supply documentation of individual certification issued by CETCO.

- Use of automated welding equipment is recommended for all CoreFlex and CoreFlash membrane overlap seams exceeding 10 feet (3 m) in length. Automated equipment can either be hot air welding machine or a wedge welding machine. All welds shall be continuous and without interruption or defect.

- Prior to welding, start welding equipment and allow it to warm up to optimum welding temperature. Equipment warming period may vary depending on weather conditions and will need to be verified each day and after equipment has been cooled down and restarted and must be confirmed with a test weld.

- Hot Air Welders: For all field seams use a 1-1/2” (40 mm) wide nozzle to create a nominal 1-1/2” (40 mm) wide homogeneous thermoplastic weld.  Use a minimum ¾ “ (20 mm) wide nozzle for corners, T-joints, patches and other field detailing, maintaining a nominal ¾” (20 mm) wide homogeneous thermoplastic weld. All welds shall be continuous and without interruption or defect.

- All seams must be clean and dry prior to initiating any field welding procedures. Remove all foreign materials from the seams (dirt, oils, etc.) using CLEAN WHITE COTTON cloths. Do not use denim or synthetic, synthetic blend or paper rags for cleaning.  For detailed cleaning procedures consult CETCO.

- Contamination occurring within a seam shall be patched to insure water-tight integrity of the weld.

- Follow equipment manufacturer’s instructions and observe local codes and site requirements for electricity supply, grounding, GFI and other current protection. Dedicated circuit, house power or a dedicated portable generator is required. No other equipment (including but not limited to hand welders) shall be operated off the dedicated power source.

- T-Joints (multiple overlaps)

- A 4” (100 mm) CoreDisc is required centered and hot air welded at the T-Joint intersection using the following steps.

- All membrane edges forming the T-Joint that will be covered by the CoreDisc, plus 1” (25 mm) beyond, must be feathered to provide a smooth transition for the CoreDisc. The feathering can be accomplished with a hot nozzle of hand welding tool.

- While hand welding the CoreDisc, use the edge of the hand roller to conform the CoreDisc completely to the thermoplastic membrane overlaps to prevent voids at the feathered membrane edges.

- Hand Welding seams shall be competed per the following three steps.

- Step One:  Intermittently tack weld the overlap to hold the thermoplastic membrane overlap in place and maintain a uniform overlap width (minimum 4” (100 mm)).

- Step Two:  Insert the nozzle into the back of the overlap.  With a silicone roller pinch off the back edge to trap the hot air and make a thin pre-weld. The pre-weld will serve to concentrate heat along the exterior edge of the overlap during step three.

- Step Three:  Insert the nozzle of the hand welder into the lap at a 45° angle relative to the sheet edge. As the thermoplastic membrane surface begins to flow, apply light pressure with a hand roller oriented at a right angle to the tip of the hand welder.  As rolled, a small bead of molten material should bleed out of the seam edge.

- Machine Welding

- Automated Hot-Air Welders

- Use a 1-1/2” (40 mm) wide nozzle to create a nominal 1-1/2” (40 mm) wide homogeneous thermoplastic weld. Depending on the location of the bearing weight and design of the equipment, a sheet metal track may be required. Welds shall be continuous and without interruption or defect.

- Wedge Welders

- Use a minimum 2” (50 mm) wide wedge to create a nominal 2” (50 mm) wide homogeneous thermoplastic weld without interruption or defect.

- Membrane overlap assembly may need to be increased according to the requirements of the equipment.

- Prior to wedge welding, fold the APC geotextile selvege edge of the bottom sheet back under and out of the way in order for the thermoplastic membrane of the bottom sheet to make contact with the wedge. Fold back the APC selvege edge for the entire length to be welded.

- After completing thermoplastic weld, lift up membrane and unfold the APC geotextile selvege edge to provide minimum 4” (100 mm) APC to APC overlap at the membrane overlap assembly.

  - Quality Control/Inspection of Welded Seams

    - All welds shall be inspected by the waterproofing applicator’s job foreman and/or supervisor daily after cooling. Weld continuity inspection shall include, but not be limited to, the probing of all field welds with a rounded screwdriver or other dull pointed instrument.  Immediately mark and remediate any deficiencies per CETCO guidelines.

    - Each days welding should begin with an evaluation of welded seams conducted on a test strip of membrane. Adjust equipment speed and or heat/power settings as necessary to achieve proper welds. Cut out and retain a 2” – 4” (50 mm – 100 mm) wide seam sample, date it and retain for the independent inspector/owners rep. from the test weld. Further testing may be required as conditions change during the day, as problems arise or at the independent inspector/owners rep. discretion. Taking samples of completed waterproofing should be avoided whenever possible. However, when necessary, each test cut shall be filled with Cortex and patched with CoreFlash extending 4” (100 mm) beyond the edges of the cut opening and completed with a homogeneous thermoplastic weld.  Each test cut shall be patched by the waterproofing applicator at no additional cost to the owner.

    - Ensure that all aspects of the installation (sheet layout, attachment, welding, flashing details, etc.) are in strict accordance with the most current CETCO Specifications and Details. Excessive patching of field seams because of inexperienced or poor workmanship will not be accepted at time of FINAL INSPECTION FOR WARRANTY ACCEPTANCE. Deviations from this specifications and/or details must be authorized in writing by CETCO, prior to execution.  Deviations from this procedure may result in forfeiture of warranty eligibility.

  - Perform Electronic Leak Detection test over the entire waterproofing membrane installation per Quality Assurance Section 1.06F.  For areas to receive ELD testing provide the following

    - Prior to installation of the waterproofing membrane a complete installation and field testing procedure guideline, as provided by the ELD system manufacturer,  shall be provided to the Installer, General Contractor, Manufacturer, Architect and Owner.

    - Thoroughly wet the waterproofing membrane in area of test.  Wetting can be accomplished by hand or mechanical spray devises.  Membrane must be wet during the testing procedures.  Ponded water is not necessary.

    - Visually inspect and perform ELD testing to locate membrane breaches, if any. Document location of breaches found by the ELD test and visual inspections.

    - Repair all breaches found per waterproofing manufacturer’s guidelines. Leave ELD conductor wire grid in place as secured to waterproofing membrane.

    - Once membrane ELD testing is concluded and all repairs are complete, the membrane shall be immediately protected. General Contractor shall prohibit non-waterproofing construction traffic, activity and material storage on the tested membrane.

  - Insulation

    - Install the insulation loose over the waterproofing membrane, firmly butting each adjacent board. Do not leave gaps between adjacent boards.

    - If multiple layers of insulation are required, then install the thicker layer on the bottom. Rotate the direction of each layer 90° and stager seams. All layers of insulation must be un-adhered to each other.

    - Cut insulation to fit close to all cants, protrusions, and obstructions.

    - Install BB-200 over the insulation overlapping the seams 6” (150mm) Cut to fit tightly at perimeters, corners and at all penetrations (optional)

  - Aeration Layer (required above insulation when Moisture Retention Mat is used)

    - Install Aquadrain G20 on horizontal and vertical surfaces over insulation in accordance with Manufacturers installation procedures. Abut all drainage sheet edges for continuous layer.  Seal all edges by overlapping and then bonding extra fabric flap edges to adjacent drainage course fabric with a general construction adhesive to ensure integrity.

    - Cut aeration sheets to fit close to all perimeter, protrusions and obstructions.

  - Moisture Retention Mat (optional per project plans and specifications)

    - Place the moisture retention mat over the Aeration Layer.

    - Overlap all edges a minimum of 4” (100 mm). Extend 6” (150 mm) beyond growing medium laying up all vertical surfaces. Trim to just below level of soil avoiding exposure.

  - Drainage Layer (edit to requirements)

    - Install Aquadrain (GS-300, GS-310 or GS-315) course over the insulation or moisture retention mat, if used, in accordance with Manufacturers installation procedures.

    - Cut drainage to fit close to all perimeter, protrusions and obstructions.

    - Place subsequent ballast materials on as soon as possible.

  - Filter Fabric (GS-404 should be added when using GS-315).

    - Place the GS-404 filter fabric over the GS-315 drainage retention layer.

    - Overlap all edges 6” (150 mm) with a minimum of 6” (150 mm) between all overlaps.  Keep overlaps a minimum of 6” from all perimeters.  Secure filter fabric under any perimeter metal counter flashings,

    - Cut filter fabric around any drainage openings so to not restrict water flow to the drain.  Cut filter fabric around any penetrations in such a manner as to prevent any stone ballast from entering between penetration and insulation.

  - Geocell Cellular Soil Confinement

    - Install Geocell Cellular Confinement directly on top of the filter fabric or drainage/retention/filter fabric composite.  Thread the specified stainless steel cable tendons through the panels, placing uncrimped copper stops along the tendons beneath the designated cell rows as per project design, prior to expanding to conform to nominal cell dimensions.

    - Place a copper oval through one end of each tendon and loop the tendon through the previously installed upslope anchor connection eyebolts attached to the structure.  Secure the loop on the tendon by placing the end through the second opening in the copper oval and crimp the oval to the tendon using the crimping tool and in a manner scecified by the manufacturer for the specified cable tendon.

    - Expand and position the first panel such that the edge wing sections run parallel to the parapet or other edge.  Measure the distance along each tendon from the top of the first cell to coorespond to the nominal cell dimensions per the project design.  Crimp the copper stops that have been previously thread along the tendon at the point where all upslope cells will conform to the nominal dimension making sure all cell dimensions are consistent and the wing edges remain in position.  Continue to crimp the copper stops along all tendons of the first panel.

    - Attach subsequent downslope panels by threading the cable tendons through the panel and using a copper stop crimped to the cable tendon, with the specified crimping tool and in the manner specified by the manufacturer, in the first cell of the subsequent panel.  Expand the second panel to the nominal cell size and repeat as per 2.13 C above until all subsequent panels are placed.

    - Attach the ‘wing” edges of laterally adjacent panels by attaching the wings with heavy-duty zip ties after expanding the adjacent panles to nominal cell size and installing the required copper stops.

    - Panels can be cut at full cell points to conform to project dimensions, penetrations, etc.

    - At the end of the last subsequent downslope panel placed, the cable tendon may be attached to  anchor connection eyebolts at the end of the panel run in the manner described in 2.13 B above or simply terminated against the parapet or other edge. (edit to requirements)

    - The aluminum wire tie-downs shall be looped through the lower row of perforations in the cell walls on 2-foot centers and twisted 3-4 times to secure them at the top of the panels leaving a minimum of 6 inches on two ends of the wire above the panel.  The two wire ends will be used to secure the erosion control blanket or pre-vegetated tile or mat after it is placed.

  - Growing Media

    - Install specified growing media in strict accordance with the project and design requirements.  Avoid damage or displacement of other components including filter fabric, insulation, drainage composite, wall, hardscape and roofing.

    - Filling of the Geocell Cellular Confinement with growing media must start at the top of the slope working downward to avoid displacement of the panel.  Care should be taken to ballast the panel to maintain nominal cell dimensions and position along the edges while filling.

    - The Geocell Cellular Confinement panels shall be overfilled approximately 1 inch over the top of the panel top edge. Hand tamp growing media into the cells until the top of the panel appears.

    - An additional ½-1 inch of growing media should be added to conceal the top of the panel and establish final grade once tamping is completed.

  - Vegetation

    - Environmental Conditions:

      - Greenroof Plants should be installed after the 90% probability date of last frost in the spring (36 degree F temperature threshold) and before the 90% probability date of first frost in the fall (36 degree F temperature threshold) in the site area or nearest reporting station.  See Climatography of the US No. 20 at: www.ncdc.noaa.gov/oa/climate/freezefrost/freezefrost.pdf for statistical interpretation of date of last frost/date of first frost.

      - Greenroof Plants should not be installed in waterlogged media

      - Greenroof Plants should not be installed during prolonged periods of drought unless irrigation is available.

      - Greenroof Plants must be installed within two days of delivery or contractor must maintain their healthy condition until planted

    - Securing Vegetation to Geocell Cellular Confinement. (Optional: edit to requirements)

      - Plugs/Cuttings with Erosion Control Blanket

        - Position erosion control blanket over the growing media prior to planting plugs making sure the two ends of the tie down wire protruded through the blanket. (Erosion control blanket is not used for pre-vegetated tiles or mats)

        - Secure the erosion control blanket by gently twisting the wire 3-4 times over the blanket.  The twisted wire tie down should be bent downward to bury the end into the blanket.

        - For plugs X-cuts shall be made with a ultlity or other sharp knife in locations where plug planting will occur to accommodate installation into the growing media.

        - For cuttings the erosion control blanket is secured after the cuttings are placed over the growing media.

        - Install the plugs or cuttings in strict accordance with the landscape architect or landscape designer’s instructions and plans following proper landscape planting techniques.

      - Pre-Vegetated Tiles or Mats

        - Install the specified Tiles or Mats in strict accordance with the landscape architect or landscape designer’s instructions and plans following proper landscape planting techniques.

        - The tiles or mats are to be secured to the underlying cellular confinement panels by running the two loose ends of the aluminum wire through the tile or mat and securing by twisting the wire over the top of the tile or mat.  The twisted wire ends shall then be bent down to bury the end such that it is covered by the vegetation.

  - IRRIGATION

    - Irrigation water must be applied until the roots are established in the growing media on the roof (6-8 weeks after installation).

      - Thoroughly water entire vegetated roof surface immediately after installation.

      - Deliver ≥ ¼” water, 2 times per week for the first 2 weeks.

      - Deliver ≥ ¼” water, 1 time per week for the next 6-8 weeks.

      - Extended irrigation requirements are dependent upon project location, conditions, and plant selection. It is recommended that if a permanent irrigation system is not installed, that a backup system (such as hose bibs located on the roof) be available for use during prolonged periods of drought (>4 weeks with less than a total of ¼” precipitation

  - MAINTENANCE

    - System installer shall maintain the vegetated roof for a period of at least [XXX] (edit to requirements) days after essential completion.

    - Maintenance activities shall include:

      - Initial Establishment

        - Water the vegetated roof system 2 times a week for the first two (2) weeks and 1 times a week for the next 6-8 weeks as needed to maintain a moist condition to aid in root establishment. Water the system more frequently during extended periods of hot, dry weather conditions and less frequently if periodic rains maintain a moist surface condition.

        - Provide hand weeding as necessary to remove undesirable species as they appear.

        - Replace areas of damaged plants or bare spots using additional plant material.

        - Remove any debris that appears on the roof.

        - Observe surface for any erosion of the growing media and repair/replace growing media as needed.  Plant additional plants on any disturbed areas.

      - Mature Coverage Establishment

        - Continue weekly visits for a minimum of 2 months after essential completion.  Perform watering, weed removal, repair of eroded or non-vegetated areas and debris removal as needed.

        - After the first two months, evaluate conditions and if plant growth is progressing well, reduce frequency of visits to monthly (during the growing season) for the remainder of the first year (note: the first year may span two growing seasons).  If plants appear weak or are not developing well, apply a slow-release fertilizer with an analysis of 5-3-4 (N-P-K) + micronutrients or similar.  Fertilizer can be applied in a time period between April – August but only if same day temperatures are expected to remain below 90 degrees F.

        - After first year, evaluate conditions and if plant growth is progressing well, continue monthly visits or reduce frequency as needed to maintain a vigorous plant condition and achieve and maintain a minimum of 80% plant coverage.   Each visit should include watering, weed removal, repair of eroded or non-vegetated areas and debris removal as needed.

      - Hardscape/Pavers

        - Install hardscapes and/or architectural pavers per project specifications and layout drawings. Install in strict accordance with manufacturer’s installation guidelines.

  - Job Completion

    - Clean-Up

        - In areas where adjacent finished surfaces are soiled by work of this Section, consult Manufacturer of surfaces for cleaning advice and conform to their recommendations and instructions.

        - Remove all debris, tools, equipment and remaining product on-site. Dispose of debris and damaged product following all applicable regulations.

    - Inspection

      - The Installer with the Owner’s Independent Inspector shall examine all completed work.

END OF SECTION 0711354