This guide specification was issued January 2010 and may be superseded without notice at any time. Therefore, please confirm that this specification is still current and has not been superseded by checking at www.cetco.com/bmg or by calling 1-847-851-1800.

CAST-IN-PLACE CONCRETE CONSTRUCTION SPECIFICATION

This guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute and is intended for use with cast-in-place concrete structures. This specification is not intended for use with shotcrete. Contact CETCO regarding installation and application guidelines for CoreFlex Waterproofing System when used with below-grade shotcrete, masonry block, or precast concrete construction. CETCO, Building Materials Group – 1- 800-527-9948.

This master guide specification contains work sections in PART 3 – Execution – pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project.

SECTION 071354 – JANUARY 2010 (Supersedes All Previous Versions)

- COREFLEX® 60 WATERPROOFING AND METHANE RESISTANCE SYSTEM MASTER GUIDELINE SPECIFICATION FOR CAST-IN-PLACE CONCRETE PROPERTY LINE AND BACKFILLED WALLS  UNDER HYDROSTATIC CONDITIONS

- Part 1 – GENERAL

- RELATED DOCUMENTS

    - All of the Contract Documents, including General and Supplementary Conditions, and Division 1 General requirements, apply to the work of this section.

- WORK SUMMARY

    - The work of this section includes, but is not limited to the furnishing and installing of the following materials, per project specifications and drawings, or as directed by waterproofing manufacturer:

- CoreFlex  60 waterproofing membrane with all applicable accessory products.

- RELATED SECTIONS

    - Related Work not in this section: excavation and backfilling, concrete, retention wall construction, expansion joint seals, flashing and sheet metal, joint sealants, vapor extraction system, gas monitoring, soil sterilant, and drainage. Other specification Sections which directly relate to the work of this section include, but are not limited to, the following:

      - Division 2: Subsurface and Geotechnical Investigations

      - Division 3: Waterstops

      - Division 5: Expansion Joint Products

      - Division 7: Joint Treatment/ Sealants, Flashing and sheet metal, and Insulation

      - Division 22: Deck and Floor Drains and other Mechanical Penetrations

      - Division 26: Conduit and other Electrical Penetrations

      - Division 31: Earthwork, Excavation and Fill, Shoring,

      - Division 33: Geocomposite Foundation Drainage

- SYSTEM DESCRIPTION

    - Provide and install waterproofing system, without defects and damage, to prevent the passage of liquid water and promote the resistance of methane gas in concentrations up to 20,000 ppm. Waterproofing shall be a 60 mil thick PVC, Elvaloy KEE thermoplastic membrane reinforced with a 5.0 oz. weft inserted knit polyester fabric integrally bonded to an Active Polymer Core (APC) layer. All thermoplastic field seams shall be continuously welded and supported with all applicable accessory products installed.

  - SUBMITTALS

    - General: Prepare and submit specified submittals in accordance with "Conditions of the Contract" and Division 1 Submittals Sections.

    - Product Data: Submit manufacturer’s product data, with complete general and specific installation instructions, recommendations, and limitations.

    - Product Samples: Submit representative samples of the following for approval:

      - CoreFlex 60 and CoreFlash waterproofing membranes.

    - Waterproofing Material and Labor Warranty: At time of bid, submit a sample copy of the Manufacturer’s Waterproofing Warranty complete with all coverage’s, limitations and conditions.

    - Methane Barrier Product Warranty: At time of bid, submit a sample copy of the Manufacturer’s  Methane Barrier Product Warranty complete with all coverage’s, limitations and conditions.

    - Material Certificates: Submit certificate(s) signed by manufacturer certifying materials comply with specified performance characteristics and physical requirements. Submit certification that waterproofing system and components, drainage and protection materials are supplied by a single-source manufacturer.

    - Contractor Certificate: At time of bid, submit written certification that installer has current Approved Applicator status with waterproofing material manufacturer.

  - QUALITY ASSURANCE

    - Installer Qualifications: Installing Company should have at least three (3) years experience in work of the type required by this section, who can comply with manufacturer's warranty requirements, and who is an Approved Applicator as determined by waterproofing/drainage system manufacturer.

    - Manufacturer Qualifications:  Waterproofing membranes and all accessory products shall be provided by a single manufacturer with a minimum of 30 years experience in the direct production and sales of waterproofing systems. Manufacturer shall be capable of providing field service representation during construction, approving an acceptable installer, and recommending appropriate installation methods.

    - Pre-Installation Conference: A pre-installation conference shall be held at least two weeks prior to commencement of field installation to establish procedures to maintain required working conditions and to coordinate this work with related and adjacent work. Confirm that all parties understand what is required to provide a substrate that is suitable to receive the CoreFlex Waterproofing System. Verify that final waterproofing and waterstop details comply with waterproofing manufacturer's current installation requirements and guidelines. Pre-con meeting attendees should include representatives for the owner, architect, inspection firm, general contractor, waterproofing contractor, concrete contractor, excavating/backfill contractor, and mechanical and electrical contractors if work penetrates the waterproofing.

    - Materials: Obtain waterproofing membrane with accessory products from a single manufacturer to assure material compatibility.

    - Independent Inspection: Owner shall make all arrangements and payments for an independent inspection service to verify and approve substrate prior to installation; monitor waterproofing material installation compliance with the project contract documents and manufacturer’s published literature and site specific details. Independent Inspection Firm shall be an approved company participating with the waterproofing manufacturer’s Certified Inspection Program. Inspection service shall produce reports and digital photographs documenting each inspection. Reports shall be made available to the Contractor, waterproofing installer, waterproofing material manufacturer, and Architect. Inspections should include substrate examination, beginning of waterproofing installation, periodic intervals, seam welding and final inspection prior to concrete or backfill placement against the waterproofing.

    - Water Sample Test: Waterproofing contractor shall supply project site water sample to waterproofing membrane manufacturer for analysis. Manufacturer shall conduct test free of charge. Contractor is responsible for collection and shipment of one liter of actual site water. Water should be shipped in uncontaminated, sealed plastic container to: CETCO Technical Center, Attn: BMG Field Services, 2870 Forbs Ave., Hoffman Estates, IL 60192. Also provide project name, city and state along with return address to forward test results.

  - PRODUCT DELIVERY, STORAGE AND HANDLING

    - Delivery and Handling: Deliver materials in factory sealed and labeled packaging. Sequence deliveries to avoid delays, while minimizing on-site storage. Handle and store following manufacturer's instructions, recommendations and material safety data sheets. Protect from construction operation related damage, as well as, damage from weather, excessive temperatures and prolonged sunlight. Remove damaged material from site and dispose of in accordance with applicable regulations.

- Storage: Do not double-stack pallets during shipping or storage. Protect waterproofing materials from moisture, excessive temperatures and sources of ignition. Provide cover, top and all sides, for materials stored on-site, allowing for adequate ventilation. Canvas tarps are recommended.

  - PROJECT CONDITIONS

    - Substrate Condition: Proceed with work only when substrate construction and preparation work is complete and in condition to receive waterproofing system. All plumbing, electrical, mechanical and structural items to be under or passing through the waterproofing shall be positively secured in their proper positions prior to membrane application. Substrate preparation shall be per waterproofing manufacturer’s guidelines.

    - Weather Conditions: Perform work only when existing and forecasted weather conditions are within the guidelines established by the manufacturer of the waterproofing materials. Do not apply waterproofing materials into standing or active water; over ice and snow. Though exposure to precipitation and ground water seepage typically will not adversely affect CoreFlex, the General Contractor shall maintain site conditions to remove standing water from precipitation or ground water seepage in a timely manner. Should CoreFlex be subjected to prehydration as a result of prolonged immersion (prior to completion and final detailing), inspection of the material and written acceptance from CETCO is required prior to concrete or backfill placement.

  - WARRANTY

    - Warranty eligibility for the project must be validated by Manufacturer; confirming acceptance of the installation and independent inspection reports are in accordance with the manufacturer’s quality assurance program requirements.

    - Waterproofing Material and Labor Warranty:

Upon installation completion and manufacturer acceptance of the work required by this section, the waterproofing materials manufacturer will provide to the project Owner, a written fifteen (15) year non-prorated waterproofing warranty, covering both materials and labor.  Issuance of Manufacturer's Waterproofing Warranty requires the following: (1) Waterproofing system products shall have been provided by a single manufacturer; (2) Installation of waterproofing products by Manufacturer's Approved Applicator in full accordance with the manufacturer’s quality assurance program requirements; (3) installation inspected by an approved and trained Independent Inspection Firm participating with the waterproofing manufacturer’s Certified Inspection Program; (4) In Division 3 work, Waterstop manufactured and supplied by the waterproofing membrane manufacturer must be installed in all applicable concrete construction joints and around applicable penetrations. Manufacturer's waterproofing warranty shall be independent from methane gas resistance product warranty and any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties.

- Methane Gas Barrier Product Warranty:

Upon delivery and acceptance of the methane gas-barrier materials specified by this Section, the materials manufacturer will provide to the Owner, a written fifteen (15) year standard material warranty indicating that the materials, as supplied to the subject project, conform to the materials manufacturer specifications and are free of material defects.

Manufacturer shall have no liability if the materials fail to perform as a result of (A) accident, neglect, abuse or mishandling of the materials, including failure of Owner to use reasonable care in maintaining the materials; (B) natural occurrences and acts of God, including without limitation, earth quakes or explosions; (C) structural defects, cracks or alternations of the building on which the materials are applied; (D) the failure of or improper preparation or application of any material or component underlying or adjacent to the materials; (E) subsequent work performed on, to or through the materials unless done in a manner prescribed and accepted by manufacturer; (F) acts of vandalism; or (G) chemical attacks on the materials.

Under the scope of the Methane Gas Barrier Product Warranty, Manufacturer’s liability will be limited to the cost of replacement of defective materials (in the form originally shipped), or at manufacturer’s election, the repayment or crediting to Owner of an amount equal to the cost of replacement (in the form originally shipped) of defective materials.

- PART 2 - PRODUCTS

  - MANUFACTURER

- Provide CoreFlex 60 waterproofing membrane and applicable accessories as manufactured by Colloid Environmental Technologies Company (CETCO), 2870 Forbs Avenue, Hoffman Estates, Illinois 60192 USA. Phone: (847)851-1800; Fax: (847)851-1899; Web-site: http://www.cetco.com/bmg

- 2.011	DISTRIBUTOR

- Bowman Construction Supply

- 10801 E. 54th Avenue

- Denver, CO 80239

- Phone: (303) 696-8960

  - MATERIALS

- COREFLEX MEMBRANE WATERPROOFING

- CoreFlex 60 MEMBRANE: 60 mil (1.5 mm) nominal thick PVC, Elvaloy KEE thermoplastic membrane reinforced with a 5.0 oz. weft inserted knit polyester fabric integrally bonded to an Active Polymer Core (APC). CoreFlex 60 is designed for use on backfilled foundation walls, plaza decks, structural podium slabs, under floor slabs, property line retention walls, earth-covered structures, tunnels and greenroofs. Roll size: 54” x 50′ (1.4 m x 15 m). 54” wide thermoplastic membrane with APC layer offset 6” (150 mm) along the long roll edges.

- COREFLEX  60 MEMBRANE PHYSICAL PROPERTIES:

| - Physical Properties |  |  |
| --- | --- | --- |
| - Property | - Test Method | - Typical Value |
|  |  | - CoreFlex 60 |
| - Membrane Composite Thickness | - ASTM D751 | - 150 mil (3.8 mm) |
| Hydrostatic Pressure Resistance - (min 1 hour @ 100 psi) | - ASTM D5385 | - 231 ft (70 m) |
| - Puncture Resistance | - ASTM D4833 | - 224 lbs (996 N) |
| - Tensile Strength | - ASTM D751 | - 549 lbs (2,442 N) |
| - Bonded Seam Strength | - ASTM D751 | - 705 lbs (3,136 N) |
| - Peel Adhesion to Concrete | - ASTM D903 (mod) | - 10 lbs/in (1,751 N/m) |
| - Methane Permeability | - ASTM D1434 | - 25 mL (STP)/m2/day |
| - Oil Resistance | - ASTM D543 | - Passed |
| - Micro organism Resistance | - ASTM D4068-88 | - Passed |
| - Environmental Stress Cracking | - ASTM D1693 | - Passed |
| - Water Vapor Retarder | - ASTM E1745 | - Class A |
| - Water Vapor Transmission | - ASTM E96 | - 0.1 perms (0.036 gr/m/hr) |
| - Tensile Strength | - ASTM E154 | - 387 lbf/in (68 kN/m) |
| - Puncture Resistance | - ASTM D1709 | 12.0 lbs (5,500 grams)* - *Maximum of Test Equipment |

- ACCESSORY WATERPROOFING PRODUCTS: All accessory waterproofing materials shall be provided by the waterproofing manufacturer or shall have manufacturer’s written approval for substitution.

      - CoreFlash-60: 60 mil nominal reinforced thermoplastic membrane used for non-exposed flashing applications including curbs, walls, field wraps and patches.  Membrane is yellow top coat and black bottom coat.

      - CoreFlash-UV:  60 mil nominal reinforced UV stable thermoplastic membrane (white top coat and black bottom coat) used for flashing applications exposed to direct UV and or weathering conditions. Including curbs, walls, field wraps and patches.

      - GF-60:  60 mil nominal 18” x 50’ reinforced UV stable thermoplastic flashing membrane (white top coat and black bottom coat) used for flashing applications exposed to direct UV and or weathering conditions. Including Grade Termination, curbs, walls, field wraps and patches.

      - CoreFlash-NR:  60 mil nominal UV stable non-reinforced extruded white thermoplastic membrane used for above or below grade flashing applications including curbs, walls, field wraps and patches.  Available in 4’ x 24’ rolls.

      - CoreClad-A:  0.040 in thick 3003H14 Aluminum sheet laminated with a 20 mil (0.50 mm) nominal thick UV stable compatible thermoplastic coating on one side for above or below grade flashing and detail applications. Available in 47.5-in x 120-in (1.2 m x 3.0 m) sheets.

      - CoreClad:  24 ga. stainless steel sheet laminated with a 20 mil (0.50 mm) nominal thick UV stable compatible thermoplastic coating on one side for above or below grade flashing and detail applications. Available in 47.5-in x 120-in (1.2 X 3.0 m) sheets.

      - CoreDisc:  4” (100 mm) diameter thermoplastic discs.  Used for attaching CoreFlex membranes to vertical surfaces prior to concrete pour and for finishing T-Joints.

      - Universal Corner:  Preformed injection molded thermoplastic flashings that will accommodate inside and outside corner details of any dimension. CoreFlex Universal Corners come as one piece and are trimmed to fit the appropriate condition.

      - Adhesive SB-100: Solvent-based adhesive for securing CoreFlash membranes to various substrates, including cured concrete, wood, metal and cementitious boards.

      - AkwaSwell:  Hydrophilic polyurethane caulk used for detail work.

      - Cortex: A low permeable geotextile waterproofing material that utilizes Active Polymer Core (APC) technology.

      - TB-Boot: Pre-formed, single piece tie-back cover with welding collar flange. Three sizes available: TB-6SNF, TB-8F, and TB-10F.

      - Termination Bar: Minimum 1/8” thick x 1” wide stainless steel or aluminum termination bar punched 6” (150 mm) o. c. or approved equal.

      - CETSEAL:  A multipurpose UV stable single component polyether moisture cure sealant / adhesive.  Primary applications are Grade termination Sealant, Membrane Lap Sealant and Waterstop Adhesive.

      - Hydrobar Tubes: 2” (50 mm) diameter x 2’ (600 mm) long, water soluble tube container filled with granular sodium bentonite.

      - Protection Course: CoreFlash-60 or other CETCO approved protection layer products.

PART 3- EXECUTION contains work sections pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project. Sections 3.01, 3.02, 3.03, 3.04 and 3.05 pertain to all applications. Sections 3.06 through Section 3.10 pertain only to zero-lot line construction. Sections 3.05B, through Section 3.10B pertain only to backfilled cast-in-place concrete wall applications.

- PART 3 – EXECUTION

    - Comply with contract documents and manufacturer's product data, including product application and installation instructions.

  - SUBSTRATE INSPECTION AND CONDITIONS

    - The installer, with the Owner’s Independent Inspector present, shall examine conditions of substrates and other conditions under which this section work is to be performed and notify the contractor, in writing, of circumstances detrimental to the proper completion of the work. Do not proceed with work until unsatisfactory substrate conditions are corrected and are acceptable for compliance with manufacturer's warranty requirements. General substrate conditions acceptable for the waterproofing installation are listed below. For conditions not covered in this Section, contact the waterproofing manufacturer for guidance.

    - WORKING MUD SLAB: Working concrete mud slabs should have a float finish to provide a planar surface; without sharp angular depressions, voids or raised features.

    - COMPACTED SOIL OR GRAVEL SUB-GRADE: Sub-grade shall be compacted to a minimum relative compaction of 85% or greater as specified by civil/geotechnical engineer. The finished surface shall be smooth, uniform, free of debris and standing water or ice. Aggregate sub-grades shall consist of ¾” (19 mm) stone or smaller and rolled flat, free from any protruding sharp edges. Specific sub-grade preparation shall be designed by a qualified civil or geotechnical engineer. For compacted soil or gravel sub-grade a flat, ridged piece of plywood or sheet metal wide enough to accommodate the welding equipment must be placed under the membrane overlap in order to run the welding equipment. Several may be used in-line to insure that the equipment always runs on the ridged planar surface.

    - WOOD TIMBER SHORING: Wood lagging shoring should extend to the lowest level of the waterproofing installation with any voids or cavities exterior of the lagging timbers filled with compacted soil or cementitious grout. Interior surface of lagging boards should be planar and tight together with gaps less than 1” (25 mm). Gaps in excess of 1” should be filled with cementitious grout, compacted soil, extruded polystyrene (20 psi min.) or CETCO approved spray polyurethane foam. Do not use plywood or other surface treatment over large lagging gaps that leave the cavity void. (In areas where lagging gaps are 2-1/2” (63 mm) or less, Aquadrain sheet drain may be placed over lagging gaps to provide a suitable substrate for the CoreFlex 60 membrane.) All lagging board nails and other mechanical projections shall be removed or pounded in flush.  Install a protection material over all soldier piles with raised lagging hanger bolts, form tie rods, or other irregular surface;  protection material should extend a minimum 6" (150 mm) to both sides of the steel piling.

- METAL SHEET PILING SHORING WALL: Metal sheet pile shoring requires minimum ½” (12 mm) plywood fastened to create a flat surface for CoreFlex membrane installation.  Install plywood with all edges tightly abutted and all fasteners flush with plywood surface.  All void spaces between the plywood and the sheet piling must be filled with compacted earth or concrete. Any areas of water seepage at the sheet piling interlocks can be sealed prior to CoreFlex installation by injecting Bentogrout to the outside of the sheet piling interlocks.

- F.	CUT ROCK FACE OR AUGER CAST CAISSON SHORING WALLS: Interior surface of cut rock and concrete auger pile retention walls should be planar without irregular surface conditions, voids, and sharp transitions that would leave a void space to the outside of the drainage and waterproofing installation. Irregular rock, void pockets, cracks, sharp concave transitions should be completely filled or smoothed with cementitious grout, shotcrete, or other approved solid material.

- G.	MECHANICAL OR OTHER PENETRATIONS: Mechanical, structural, or architectural materials that will pass through the plane of the waterproofing membrane shall be properly installed and secured in their final position prior to installation of the waterproofing system.

- H.	SHORING WALL BRACING: Whenever possible, shoring wall bracing shall be constructed with circular pipe elements in lieu of steel H-Piles or other irregular fixture if bracing is not removed prior to waterproofing system installation. Circular steel pipe elements provide a more uniform surface to detail with the waterproofing.

- I.	CONCRETE:  Concrete to be waterproofed shall be properly placed and consolidated. Reinforced structural slabs should be a minimum of 6" (150 mm) thick when placed over CoreFlex membrane. When hydrostatic conditions exist, install CoreFlex under all footings, elevator pits and grade beams. Cast-in-place concrete to receive waterproofing shall be of sound structural grade with a smooth finish, free of debris, oil, grease, laitance, dirt, dust, or other foreign matter which will impair the performance of the waterproofing and drainage system and which do not comply with manufacturer's warranty requirements. CoreFlex can be installed on green structural concrete as soon as the forms are removed provided the contractor gains written approval from project structural engineer listing  any site specific concrete curing time requirement prior to waterproofing installation. Do not apply CoreFlex waterproofing over lightweight insulating concrete, wood or steel decking.

      - Remove dirt, debris, oil, grease, cement laitance, or other foreign matter which will impair or negatively affect the performance of the waterproofing and drainage system.

      - Protect adjacent work areas and finished surfaces from damage or contamination from waterproofing products during installation operations.

      - Form fins, ridges, ponding ridges and other protrusions should be level and smooth with monolithic concrete surface.

      - Honeycombing, aggregate pockets, tie-rod holes and other voids should be completely filled with non-shrink cementitious grout and level with monolithic concrete surface.

      - Horizontal deck or roof concrete surfaces should be sloped for positive drainage to the deck drains or the perimeter edges. Deck drain positions should be designed with an appropriate sump depression surrounding the drain.

      - Precast concrete deck units shall be installed and secured to structural supports in accordance with the concrete panel manufacturer’s requirements and industry practice. All joints between precast units shall be completely grouted and flush with deck. Any differential in elevation between precast units shall be feathered for a smooth transition.

- 5.	All expansion joints should receive applicable expansion joint sealant product manufactured by others prior to the installation of the CoreFlex Waterproofing System. Expansion joint material is the primary seal at the expansion joint and the expansion joint material manufacturer is responsible for water tightness of the joint.

NOTE: Related work to be completed under Division 3. Waterstop-RX shall be installed in all applicable vertical and horizontal concrete construction cold pour joints and around applicable penetrations and structural members. Refer to Waterstop-RX Product Manual for further installation procedures and guidelines.

- 3.02	GENERAL WATERPROOFING INSTALLATION GUIDELINES

    - Install CoreFlex 60 in strict accordance with the manufacturer's installation guidelines using accessory products, protection and drainage layers, as specified or detailed. Install membrane in a flat, relaxed position avoiding wrinkles and stretching. Apply in standard roll size or longest workable cut length to reduce the number of T-Joints (three-way overlaps). Overlap membrane a minimum of 4 inches (100 mm) and construct all seams with a continuous thermoplastic weld. Installation of the waterproofing material should be scheduled in order to permit prompt placement of concrete or backfill following installation of the CoreFlex 60 membrane. For all applications, install CoreFlex 60 membrane with the grey APC geotextile side directly in contact with the concrete surface to be waterproofed or to receive the concrete pour; yellow thermoplastic membrane side outward toward positive water pressure.

    - CoreFlash 60 Installation guideline:  Install CoreFlash 60 membrane with the black side oriented toward the concrete to be waterproofed.

    - GF-60: Install GF-60 flashing membrane adhered to concrete substrate per manufacturers guidelines with SB-100 Adhesive;  optional color, white or black side, exposed to UV and or weathering conditions per project design.

    - CoreFlash UV: Install CoreFlash UV membrane with the black side oriented toward the concrete to be waterproofed. For non confined conditions adhere to concrete substrate per manufacturers guidelines with SB-100 Adhesive; optional color, white or black side, exposed to UV and or weathering conditions.

    - CoreFlash NR: Install CoreFlash NR membrane with the either side oriented toward the side to be exposed to direct UV and or weathering conditions.

    - Workman and all others that walk on waterproofing should wear clean, soft-soled shoes so as not to damage materials.

    - Lay out work to minimize traffic over installed areas. Membrane may be slippery when wet or covered with frost, snow or ice. Take proper precautions and heed all manufacturers’ warnings in regard to product use.

    - Where applicable, daily production schedules shall be limited to only that which can be made watertight at the end of the day or prior to inclement weather, including all flashing and night seals.

    - Expansion Joints: CoreFlex waterproofing is not an expansion joint filler or sealant, but may be used as an expansion joint cover over a properly installed expansion joint material placed during substrate preparation.

- 3.03	COREFLEX 60 OVERLAP ASSEMBLY PROCEDURES

    - General: Assemble CoreFlex 60 membrane overlaps with both the thermoplastic membrane and the Active Polymer Core (APC) layers overlapping a minimum 4” (100 mm) with all thermoplastic membrane edges continuously welded per CETCO guidelines. Membrane overlaps shall be oriented to shed water (shingle style) where ever possible. Specific equipment, especially wedge welders, may require greater overlap dimensions to facilitate welding.

    - CoreFlex 60 Seam Assembly:  Prior to welding, the following steps are required.

      - Along the long roll edges, CoreFlex 60 is produced with APC layer offset 6” (150 mm) from the thermoplastic membrane to facilitate thermoplastic welding. To facilitate thermoplastic welding along roll end edges or field cut roll dimensions, peel the APC back away from the thermoplastic membrane edge as required to accommodate various welding equipment and field conditions. Do not cut off the peeled APC geotextile. After peeling, fold back and temporarily secure the peeled APC layer with duct tape or other similar non-penetrating method to suspend it out of the way for the overlap thermoplastic welding process.  The adjacent CoreFlex 60 membrane APC layer edge does typically not need to be peeled.

- 2.	Overlap the adjacent membrane edges, thermoplastic to thermoplastic, and maintain a uniform minimum thermoplastic overlap width of 4” (100 mm).

- 3.	Following the overlap thermoplastic welding process, fold back any peeled APC layer material to its approximate original position, whereas it overlaps the adjacent membrane APC layer a minimum 4” (100 mm), and secure it with a continuous bead of CETSEAL.

- 4.	Depending on site and detail specific conditions, alternate membrane overlap/weld methods may be required. Consult manufacturer for alternate membrane installation techniques, procedures, and details to properly provide a 4” (100 mm) membrane overlap and a continuous thermoplastic weld.

- 3.04	THERMOPLASTIC MEMBRANE WELDING PROCEDURES

    - Strictly adhere to manufacturers membrane welding guidelines (refer to CoreFlex Welding Guide). All welds shall be continuous and without interruption or defect. Welding equipment shall be approved by waterproofing material manufacturer. Contact manufacturer to verify project welding equipment is suitable for CoreFlex membrane welding.

    - All welding shall be performed only by qualified personnel trained by CETCO representative prior to field welding.

    - Use of automated welding equipment is recommended for all CoreFlex and CoreFlash membrane overlap seams exceeding 10 feet (3 m) in length. Automated equipment can either be hot air welding machine or a wedge welding machine.

    - Prior to welding, start welding equipment and allow it to warm up to optimum welding temperature. Equipment warming period may vary depending on weather conditions and will need to be verified each day and after equipment has been cooled down and restarted and must be confirmed with a test weld.

    - Hot Air Welders: For all field seams use a 1-1/2” (40 mm) wide nozzle to create a nominal 1-1/2” (40 mm) wide homogeneous thermoplastic weld.  Use a minimum ¾ “ (20 mm) wide nozzle for corners, T-joints, patches and other field detailing, maintaining a nominal ¾” (20 mm) wide homogeneous thermoplastic weld.

    - Wedge Welders: For all field seams use e a minimum 2” (50 mm) wide wedge to create a nominal 2” (50 mm) wide homogeneous thermoplastic weld without interruption or defect. Membrane overlap assembly may need to be increased according to the requirements of the equipment.

    - All seams must be clean and dry prior to initiating any field welding procedures. Remove all foreign materials from the seams (dirt, oils, etc.) using CLEAN WHITE COTTON cloth. Do not use denim or synthetic, synthetic blend or paper rags for cleaning.  For detailed cleaning procedures consult CETCO.

    - Including but not limited to under slab and property line installations, move the peeled APC geotextile out of the way (do not cut it off) in order for welding equipment to run unobstructed and uninterrupted. Weld the thermoplastic membrane overlap following Section 3.04 instructions. Following the welding process, fold back the peeled APC geotextile to complete the 4” (100 mm) overlap assembly and secure with CETSEAL.

    - Contamination occurring within a seam shall be patched to insure water-tight integrity of the weld.

    - Follow equipment manufacturer’s instructions and observe local codes and site requirements for electricity supply, grounding, GFI and other current protection. Dedicated circuit, house power or a dedicated portable generator is required. No other equipment (including but not limited to hand welders) shall be operated off the dedicated power source.

    - T-JOINTS (multiple thermoplastic membrane overlaps)

- A 4” (100 mm) CoreDisc or piece of CoreFlash NR is required centered and hot air welded at the T-Joint intersection using the following steps.

- All membrane edges forming the T-Joint that will be covered by the CoreDisc, plus 1” (25 mm) beyond, must be feathered to provide a smooth transition for the CoreDisc. The feathering can be accomplished with a hot nozzle of hand welding tool.

- While hand welding the CoreDisc, use the edge of the hand roller to conform the CoreDisc completely to the thermoplastic membrane overlaps to prevent voids at the feathered membrane edges.

    - QUALITY CONTROL / INSPECTION OF WELED SEAMS

- All welds shall be inspected by the waterproofing applicator’s job foreman and/or supervisor daily after cooling. Weld continuity inspection shall include, but not be limited to, the probing of all field welds with a rounded screwdriver or other dull pointed instrument.  Immediately mark and remediate any deficiencies per CETCO guidelines.

- Each days welding should begin with an evaluation of welded seams conducted on a test strip of membrane. Adjust equipment speed and or heat/power settings as necessary to achieve proper welds. From the test weld, cut out and retain a 2” – 4” (50 mm – 100 mm) wide seam sample, date it and retain for the independent inspector/owners rep. Further testing may be required as conditions change during the day, as problems arise or at the independent inspector/owners rep. discretion. Taking samples of completed waterproofing should be avoided whenever possible. However, when necessary, each test cut shall be filled with Cortex and patched with CoreFlash extending 4” (100 mm) beyond the edges of the cut opening and completed with a homogeneous thermoplastic weld.  Each test cut shall be patched by the waterproofing applicator at no additional cost to the owner.

- Ensure that all aspects of the installation (sheet layout, attachment, welding, flashing details, etc.) are in strict accordance with the most current CETCO Specifications and Details. Excessive patching of field seams because of inexperienced or poor workmanship will not be accepted at time of FINAL INSPECTION FOR WARRANTY ACCEPTANCE. Deviations from this specification and/or details must be authorized in writing by CETCO, prior to execution.  Deviations from this procedure may result in forfeiture of warranty rights.

- 3.05	SLAB TO ZERO LOT LINE SHORING WALL TRANSITION COURSE – COREFLEX 60

- A.	At base of shoring wall, install CoreFlex 60 sheet horizontally oriented with the thermoplastic membrane offset edge side up (APC geotextile side inward facing installer; yellow side toward shoring wall); position the bottom thermoplastic edge extending out onto the horizontal substrate a minimum 12" (300 mm). Approximately 1-1/2” (38 mm) down from the top edge, secure the thermoplastic membrane offset to the shoring wall with washer-head mechanical fasteners spaced a maximum of 24” (600 mm) on center. Install adjacent membrane sheets with the thermoplastic membrane and APC layers overlapped a minimum 4” (100 mm). Assemble and weld laps per Sections 3.03 and 3.04; secure any loose or peeled APC layer material with continuous bead of CETSEAL.

- Install CoreFlex 60 membrane horizontally oriented on the shoring wall to position the top thermoplastic membrane edge a minimum 18" (450 mm) above of the top slab elevation. For thick slabs this minimum 18” (450mm) requirement can be met by installing additional membrane courses oriented horizontally. Overlap all adjacent membrane edges a minimum 4" (100 mm); assemble and weld laps per Sections 3.03 and 3.04; secure any loose or peeled APC layer material with continuous bead of CETSEAL.

- Weld a CoreDisc or equivalent size CoreFlash NR reinforcement piece centered over the welded membrane overlap directly at the point where the CoreFlex 60 membrane transitions from the horizontal to the shoring wall.

- 3.06	UNDER SLAB INSTALLATION – COREFLEX 60

    - Reinforced structural foundation slabs should be a minimum of 6" (150 mm) thick where CoreFlex 60 is installed. Install CoreFlex 60 under all footings, elevator pits and grade beams when hydrostatic conditions exists or are anticipated per the historical high ground water elevation reported in the project’s geotechnical documents.

    - Place CoreFlex 60 directly on properly prepared mud slab substrate (APC geotextile side facing up; yellow side down) with adjoining thermoplastic membrane edges overlapped a minimum of 4” (100 mm). Assemble and weld laps per Sections 3.03 and 3.04; secure any loose or peeled APC layer material with continuous bead of CETSEAL. When the slab is poured in sections, extend CoreFlex 60 a minimum 12" (300 mm) beyond the slab section edge to enable proper membrane overlapping. At the slab perimeter overlap the corner transition sheet installed per section 3.06 a minimum 4" (100 mm); assemble and weld laps per Sections 3.03 and 3.04.

    - Slab Penetrations: For all pipe, rebar, structural or other penetrations install waterproofing system per manufacturer’s standard detail for specific project condition(s).

    - Grade Beams: Install CoreFlex 60 under the entire grade beam by lining the form work prior to placing the reinforcing steel. Line the grade beam formwork with CoreFlex 60 prior to placement of reinforcing steel. Leave a minimum 12" (300 mm) of CoreFlex 60 at the top of the form to tie into under slab waterproofing. Overlap adjacent membrane edges a minimum 4" (100 mm); assemble and weld laps per Sections 3.03 and 3.04.

    - Inside and Outside Corners:  Install CoreFlex 60 membrane per manufacturer’s standard detail with applicable universal corner piece welded.

    - Inspect finished CoreFlex 60 installation and repair any damaged material prior to concrete slab placement.

    - NOTE: Related work to be completed under Division 3. Waterstop-RX shall be installed in all slab joints, around applicable slab penetrations and structural members. Refer to Waterstop-RX Product Manual for further installation procedures and guidelines.

- 3.07	SHORING RETENTION WALL INSTALLATION – COREFLEX 60

- Shoring retention wall shall be prepared per Section 3.01 guidelines prior to installation of CoreFlex 60 system.

- Apply CoreFlex 60 membrane in standard roll size or longest workable cut length. At base of shoring wall, install CoreFlex 60 sheet welded to top edge of corner transition sheet applied per Section 3.06 work. Install CoreFlex 60 sheets horizontally oriented with the thermoplastic membrane offset edge side up (APC geotextile side inward facing installer; yellow side toward shoring wall). Approximately 1-1/2” (38 mm) down from the top edge, secure the thermoplastic membrane offset to the shoring wall with washer-head mechanical fasteners spaced maximum 24” (600 mm) on center; refrain from placing a fastener within 6” (150 mm) of each roll end. Install subsequent CoreFlex 60 sheets in vertical sequence up wall with membrane roll ends matched to within 1” (25 mm); trim roll ends as applicable to meet the 1” (25 mm) tolerance. Assemble and weld membrane overlaps per Sections 3.03 and 3.04; secure any loose or peeled APC layer material with continuous bead of CETSEAL. Extend membrane installation minimum 12” (300 mm) above planned concrete lift joints to provide access.

- At both CoreFlex 60 roll ends, install a minimum 9” (450 mm) wide strip of CoreFlash 60 extending up the face of the lagging wall from the top of the CoreFlex 60 corner transition sheet to the grade elevation detail.  Tuck edge of CoreFlash 60 strip behind the CoreFlex 60 roll edge a minimum 4” (100 mm) and secure flashing strip with washer-head fasteners along both edges staggered each side 3-ft (0.9m) or less. Do not secure CoreFlash 60 strip fastened through CoreFlex 60 membrane. As applicable, overlap flashing membrane strip edges a minimum 4” (100 mm) and weld to provide continuous strip.

- Install adjacent CoreFlex 60 membrane sheets overlapping CoreFlash 60 flashing strip with rolls ends closely matched to 1” (25 mm) of adjacent CoreFlex 60 roll end.   Hot air weld both CoreFlex 60 matched roll ends to the CoreFlash 60 strip; both welds must be inside of all strip fasteners. Finish strip welding by hot air welding a CoreDisc or CoreFlash NR patch to all T-Joints per Section 3.04. Complete CoreFlash strip detail by installing a minimum 9” (450 mm) wide strip of Cortex overlapping the welded strip. Cortex strip shall extend a minimum 4” (100 mm) over both CoreFlex 60 membrane edges and be secured with CETSEAL.

- Alternate Membrane Installation: Install adjacent CoreFlex 60 membrane sheets horizontally oriented with roll ends of subsequent membrane courses staggered minimum 12” (300 mm). Assemble and weld membrane overlaps per Sections 3.03 and 3.04. Extend membrane installation minimum 12” (300 mm) above planned concrete lift joints to provide access. Detail T-Joints with CoreDisc or CoreFlash NR patch per Section 3.04.  Secure any loose or peeled APC layer material with continuous bead of CETSEAL.

- Continue membrane installation up shoring wall to project grade detail elevation. Secure top membrane edge with washer-head mechanical fasteners maximum 12” (300 mm) on center.

- Tie-Back Heads: Install applicable size TB-Boot tie-back head cover with welding collar flange per manufacturer’s detail for specific project condition(s). For irregular shoring wall conditions at tie-backs or oversize tie-back heads consult manufacturer for alternate detail for specific project condition(s).

- Wall Penetrations: For all pipe, rebar, structural and other penetrations install CoreFlex 60 system per manufacturer’s detail for specific project condition(s).

- Inside and Outside Corners:  Install CoreFlex 60 membrane with welded universal corner piece per manufacturer’s detail for specific project condition(s).

- Inspect completed CoreFlex 60 system installation and repair any damaged material prior to concrete placement.

- 3.08	SHORING WALL EXCAVATION, GRADE TERMINATION AND BACKFILL

- Coordinate work with excavation and backfill operations conducted under Division 31 by others to remove the top elements of the shoring retention wall per local building code or as specified in the contract documents. Identify and repair any waterproofing and drainage sheet damaged by excavation and removal of the top shoring retention wall elements.

- Terminate CoreFlex 60 membrane 12” (300 mm) below finished grade elevation with washer-head fasteners maximum 12” (300 mm) on center.

- Install GF-60 grade flashing membrane with bottom edge overlapping CoreFlex-60 membrane a minimum 4” (100 mm); use Adhesive SB-100 to adhere GF-60 flashing membrane continuously to substrate (except for top 2” (50 mm)). Secure bottom edge GF-60 to CoreFlex 60 with a continuous thermoplastic weld per manufacturer’s guidelines.  Overlap adjacent GF-60 roll ends a minimum 4” (100 mm) and seal with continuous thermoplastic weld.

- Terminate top edge of GF-60 flashing membrane at elevation per project details and specifications. Apply CETSEAL 2” x 90 mil thick behind the top, non-adhered edge of GF-60 grade flashing.  Then secure top edge of GF-60 with termination bar fastened into substrate maximum 12” (300 mm) on center. Complete grade termination detail with tooled bead of CETSEAL along the top edge, at all penetrations through the flashing, and all exposed overlap seams. Counter flash or cover the termination per project specifications.

- Inspect finished CoreFlex-60 / GF-60 termination and repair any damaged material. After installed it is the responsibility of the General Contractor to insure that the membrane and system components are protected and not penetrated or damaged. Keep membrane free of dirt and debris, and traffic until protection or topping material is in place.

3.09	BACKFILL

A.	Backfill shall be placed promptly after CoreFlex 60 waterproofing has been installed. Closely coordinate with contractor responsible for Backfill work by informing them each time a waterproofed area is ready for backfill. Care should be used during backfill operation to avoid damage to the waterproofing system. Backfill operations shall follow generally accepted practices for placement and compaction. Backfill should be added in 6" to 12" (150 - 300 mm) lifts and compacted to a minimum 85% Modified Proctor density. If gravel backfill, specify angular aggregate <3/4” (18mm) with fines.

- 3.10	CLEAN UP

    - In areas where adjacent finished surfaces are soiled by work of this Section, consult manufacturer of surfaces for cleaning advice and conform to their recommendations and instructions. Remove all tools, equipment and remaining product on-site. Dispose of section work debris and damaged product following all applicable regulations.

The following Sections 3.05B, through Section 3.10B pertain only to backfilled cast-in-place hydrostatic concrete wall applications.

- 3.05B	BACKFILLED C-I-P CONCRETE WALL– HYDROSTATIC CONDITIONS -- COREFLEX 60

    - At the wall/footing intersection, install continuous line of Hydrobar Tubes prior to the placement of the CoreFlex 60 membrane. Apply CoreFlex 60 membrane in standard roll size or longest workable cut length. Install bottom course of CoreFlex 60 membrane horizontally oriented (grey APC geotextile side against concrete; yellow side facing installer) with the bottom edge extending out onto the footing minimum 8” (200 mm) or further as required to overlap leading edge of CoreFlex 60 membrane previously installed under the footing as part of underslab work a minimum 4” (100 mm).  Approximately 1-1/2” (38 mm) down from the top edge of the yellow thermoplastic membrane, mechanically attach membrane to the concrete wall with washer-head fasteners spaced maximum 24” (600 mm) on center; refrain from placing a fastener within 6” (150 mm) of each roll end.

    - Install subsequent CoreFlex 60 sheets in vertical sequence up wall with membrane roll ends matched to within 1” (25 mm); trim roll ends as applicable to meet the 1” (25 mm) tolerance. Assemble and weld membrane overlaps per Sections 3.03 and 3.04; secure any loose or peeled APC layer material with continuous bead of CETSEAL.

- At both CoreFlex 60 roll ends, install a minimum 9” (450 mm) wide strip of Cortex extending up the face of the concrete wall from top of the footing to the grade elevation detail.  Tuck edge of Cortex  strip behind the CoreFlex 60 roll edge a minimum 4” (100 mm) and secure Cortex strip with washer-head fasteners along both edges staggered each side 3-ft (0.9m) or less. Do not secure Cortex strip fastened through CoreFlex 60 membrane. As applicable, overlap Cortex strip edges a minimum 4” (100 mm) to provide continuous strip.

- Install adjacent CoreFlex 60 membrane sheets overlapping Cortex strip with rolls ends closely matched to 1” (25 mm) of adjacent CoreFlex 60 roll end. Secure CoreFlex 60 roll ends with washer-head fasteners placed through the Cortex strip.

- Install minimum 9” (450 mm) wide strip of CoreFlash 60 flashing centered over Cortex strip detail (yellow side facing installer).  Hot air weld CoreFlash 60 strip to both CoreFlex 60 matched roll ends; both continuous welds must be outside of all fasteners (no exposed Fasteners). CoreFlash 60 strip shall extend a minimum 4” (100 mm) over both CoreFlex 60 membrane edges.  Finish CoreFlash 60 strip welding by hot air welding a CoreDisc or CoreFlash NR patch over all T-Joints per Section 3.04.

- Alternate Membrane Installation: Install adjacent CoreFlex 60 membrane sheets horizontally oriented with roll ends of subsequent membrane courses staggered minimum 12” (300 mm). Assemble and weld membrane overlaps per Sections 3.03 and 3.04. Secure any loose or peeled APC layer material with continuous bead of CETSEAL Detail T-Joints with CoreDisc or CoreFlash NR patch per Section 3.04.

- Continue membrane installation up concrete wall to project grade detail elevation. Secure top membrane edge with washer-head mechanical fasteners maximum 12” (300 mm) on center.

- Wall Penetrations: For all pipe, rebar, structural and other penetrations install CoreFlex 60 system per manufacturer’s detail for specific project condition(s).

- Inside and Outside Corners:  Install CoreFlex 60 membrane with welded universal corner piece per manufacturer’s detail for specific project condition(s).

- Inspect completed CoreFlex 60 system installation and repair any damaged material prior to concrete placement. After installed it is the responsibility of the General Contractor to insure that the membrane and system components are protected and not penetrated or damaged. Keep membrane free of dirt and debris, and traffic until protection or topping material is in place.

- 3.06B	BACKFILLED WALL GRADE TERMINATION   COURSE – COREFLEX  60

- A.	Coordinate work with excavation and backfill operations conducted under Division 31 by others.

- B.	Terminate CoreFlex 60 membrane 12” (300 mm) below finished grade elevation with washer-head fasteners maximum 12” (300 mm) on center.

- C.	Install GF-60 grade flashing membrane with bottom edge overlapping CoreFlex-60 membrane a minimum 4” (100 mm); use Adhesive SB-100 to adhere GF-60 flashing membrane continuously to substrate (except for top 2” (50 mm)). Secure bottom edge GF-60 to CoreFlex 60 with a continuous thermoplastic weld per manufacturer’s guidelines.  Overlap adjacent GF-60 roll ends a minimum 4” (100 mm) and seal with continuous thermoplastic weld.

- D.	Terminate top edge of GF-60 flashing membrane at elevation per project details and specifications. Apply CETSEAL 2” x 90 mil thick behind the top, non-adhered edge of GF-60 grade flashing.  Then secure top edge of GF-60 with termination bar fastened into substrate maximum 12” (300 mm) on center. Complete grade termination detail with tooled bead of CETSEAL along the top edge, at all penetrations through the flashing, and all exposed overlap seams. Counter flash or cover the termination per project specifications.

- E.	Inspect finished CoreFlex-60 / GF-60 termination and repair any damaged material.

- Backfill should consist of compactable soils or crushed stone (¾" or less). Care should be used during Division 31 backfill operation work to avoid damage to the drainage and waterproofing system. Division 31 backfill Work should follow generally accepted practices for backfilling and compaction. Backfilled soils should be added in 6" to 12" (150 - 300 mm) lifts and compacted to a minimum 85% Modified Proctor density. If gravel backfill, specify angular aggregate <3/4” (18mm) with fines.

- 3.07B	PROTECTION COURSE

- Install CoreFlash or other protection material approved by waterproofing manufacturer over completed CoreFlex membrane installation as soon as possible.  Coordinate this work with third-party inspector to allow inspection and acceptance of membrane work before installation of protection layer.

3.08B	INSULATION

A.	Always apply CoreFlex 60 waterproofing directly to properly prepared structural concrete substrates. Insulation, if used, should be installed to the exterior of the waterproofing.

3.09B	BACKFILL EXCAVATED CAST-IN-PLACE CONCRETE WALLS

A.	Backfill shall be placed promptly after CoreFlex 60 waterproofing has been installed. Closely coordinate with contractor responsible for Backfill work by informing them each time a waterproofed area is ready for backfill. Care should be used during backfill operation to avoid damage to the waterproofing system. Backfill operations shall follow generally accepted practices for placement and compaction. Backfill should be added in 6" to 12" (150 - 300 mm) lifts and compacted to a minimum 85% Modified Proctor density. If gravel backfill, specify angular aggregate <3/4” (18mm) with fines.

- 3.10B	CLEAN UP

    - In areas where adjacent finished surfaces are soiled by work of this Section, consult manufacturer of surfaces for cleaning advice and conform to their recommendations and instructions. Remove all tools, equipment and remaining product on-site. Dispose of section work debris and damaged product following all applicable regulations.

End of Section 071354