This guide specification was issued January 2011 and may be superseded without notice at any time. Therefore, please confirm that this specification is still current and has not been superseded by checking at www.cetco.com/bmg or by calling CETCO at 1-847-851-1800.

CAST-IN-PLACE CONCRETE CONSTRUCTION SPECIFICATION

This guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute and is intended for use with cast-in-place concrete structures. This specification is not intended for use with shotcrete construction. Contact CETCO regarding installation and application guidelines for Strataseal HR Waterproofing System when used with shotcrete construction. CETCO, Building Materials Group – 1- 800-527-9948.

This master guide specification contains work sections in PART 3 – Execution – pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project.

STRATASEAL HR HOT RUBBERIZED ASPHALT WATERPROOFING GUIDES SPECIFICATION

Split-Slab Construction Assembly

STRATASEAL HR HOT RUBBERIZED ASPHALT WATERPROOFING GUIDE SPECIFICATION

Split-Slab Construction Assembly

STRATASEAL HR® HOT-APPLIED RUBBERIZED ASPHALT

WATERPROOFING SYSTEM GUIDELINE SPECIFICATION

FOR SUPER LIGHTWEIGHT EXTENSIVE GREENROOFS

Part I	General

  - Related Documents

- All of the contract documents, including General and Supplementary General Conditions and Division 1 General Requirements, apply to the work of this section.

  - Description of Work

- The work of this section includes, but is not limited to the furnishing and installing the following materials, per project specifications and drawings, or as directed by the hot-applied rubberized asphalt membrane manufacturer.

  - Related Sections

- Carefully examine all of the Contract Documents for requirements which affect the work of this section.

- Other specification Sections which directly relate to the work of this section include, but are not limited to, the following:

  - Section 03 50 00 Cast Decks and Underlayment

  - Section 05 30 00 Metal Decking

  - Section 06 10 00 Rough Carpentry

  - Section 07 10 00 Dampproofing and Waterproofing

  - Section 07 25 00 Weather Barriers

  - Section 07 60 00 Flashing and Sheet Metal

  - Section 07 70 00 Roof and Wall Specialties and Accessories

  - Section 07 90 00 Joint Protection

  - System Description

- Provide an extensive greenroof with 215-mil (5.5mm) thick, reinforced hot-applied rubberized asphalt waterproofing membrane assembly with applicable detailing and accessory products as specified herein and indicated on project drawings.

  - Submittals

- Prior to commencement of the work, process submittals in accordance with the “Conditions of the Contract”.

- Submit manufacturer’s product data complete with general and specific installation instructions, recommendations and limitations.

- Submit product samples representative of the hot applied rubberized asphalt, reinforcement fabric, protection layer, insulation, filter fabric, and ballast.

- Submit material certification(s) signed by manufacturer certifying waterproofing materials comply with specific performance characteristics and physical requirements. Certification must verify that all materials are supplied by a single source manufacturer.

- Submit manufacturer’s written document that installer is certified as a current Approved Applicator with manufacturer.

- Submit sample copy of manufacturer’s waterproofing warranty identifying the terms and conditions.

  - Quality Assurance

- Installer must be a company with a minimum of at least three (3) years experience in work of the type required by this section, who can comply with the manufacturers warranty requirements, and who is an Approved Applicator as determined by manufacturer.

- Manufacturer must be a company with a minimum of forty (40) years in the direct production and sales of waterproofing materials. Manufacturer shall be capable of providing field service representation during construction, and recommending installation methods. Manufacturer shall have certified, approved applicators for membrane installation.

- Conduct a pre-installation conference prior to commencement of field installation to review conditions, establish procedures to maintain required working conditions and to coordinate this work with related and adjacent work. Representatives of the General Contractor, Architect, Installer, and Manufacturer shall be present at pre-installation conference.

- Construct mock-up of waterproofing membrane incorporating all of the components including: concrete deck, primer, hot applied rubberized asphalt, reinforcement fabric, protection layer, root barrier, water management layer, filter fabric, growing media, and vegetation. Successful mock-up may remain as part of work.

- Maintain copy of manufacturer’s installation instructions and MSDS for all products on job-site as well as allow access to the job-site by Owner’s Independent Inspector, and Manufacturer Agent.

- Owner shall make arrangements and payments for cost associated with testing the integrity of the waterproofing membrane installation utilizing a proven low voltage Electronic Leak Detection (ILD) method as approved by waterproofing manufacturer.  ELD testing method shall be selected and approved prior to waterproofing membrane installation, conducted after waterproofing membrane installation is completed and prior to subsequent assembly materials and/or overburden placement. ELD  firm shall produce reports and digital photographs documenting the inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

- Owner shall make arrangements and payments for an independent inspection service to monitor installation compliance with the project documents and Manufacturer’s published literature, installation instructions, and site specific details. Independent inspection firm shall be a company participating with the Manufacturer’s Certified Inspection Program. Inspection service shall produce reports and digital photographs documenting each inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

- Documentation of Maintenance Contract: Owner shall provide proof of a 2 year min. maintenance contract with a qualified landscaper or horticulturalist in order to insure that every effort is made to provide professional care to the vegetation and the system supporting the vegetation.  This will insure the viability of the vegetation until it is established and matured.

  - Delivery, Storage and Handling

- Deliver materials in original unopened packaging, clearly labeled with manufacturer’s labels indicating name of manufacturer, product and all identifying numbers.

- Storage of materials must be in an appropriate location and manner as to protect from any construction damage, as well as damage from weather, prolonged sunlight, excessive temperature and sources of ignition. Remove of any damaged material from job-site and dispose of in accordance with applicable regulations. Do not double stack pallets during shipping or storage. Allow adequate ventilation.

- Handling of materials to be in accordance with manufacturers instructions. Melting equipment shall consist of double jacketed, oil bath melter with mechanical agitator. Avoid overheating of hot applied rubberized asphalt. Do not use direct fire melting equipment.

  - Project Conditions

- All federal, state and local regulations, codes, and safety standards must be adhered to at all times.

- Do not apply waterproofing system if temperature is less than 0ºF (-18ºC). Application of hot applied rubberized asphalt shall not be performed during rain, snow or inclement weather; or on frost or wet covered surfaces.

- The deck must be properly cleaned and prepared free of any and all contaminations.

- The work area must be adequately ventilated. Warn personnel against breathing of vapors and contact of material with skin and eyes.  Limit access to required personnel during the installation process. Do not use flammable products near spark or an open flame. Do not allow the use of spark producing equipment during application until all vapors have dissipated.  Post “NO SMOKING” signs. Wear appropriate protective clothing and respiration protection gear at all times.

- Protect adjoining surfaces not to be waterproofed against damage or soiling, including plants, vegetation which may be affected by the waterproofing operations.

- Provide adequate protection for membrane after installation. Do not allow any foot or vehicular traffic on unprotected membrane. Do not allow any material or waste products to contaminate membrane. If contamination should occur contact manufacturer.

  - Warranty

- Warranty must be validated by Manufacturer confirming acceptance of installation, including independent inspection reports, in accordance with all applicable instructions; as well as final Electronic Leak Detection report per section 1.06.

- Manufacturer’s HydroShield Warranty.

  - HydroShield Warranty: Upon completion and acceptance of the work required by this section, the waterproofing materials manufacturer will provide a written five (5) year warranty, covering both materials and labor to the project owner. Issuance of Manufacturer's HydroShield Warranty requires the following: (1) Waterproofing system products, drainage and insulation course products, and subsequent assembly products shall have been provided by a single manufacturer; (2) Installation of waterproofing products, drainage and insulation course products and subsequent products by Manufacturer's Approved Applicator; (3) Installation inspected by Independent Inspection Firm per Section 1.06G; (4) As applicable, installation of Waterstop-RX in all concrete pour joints. Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties.

  - Plant Coverage Warranty:  Upon completion and acceptance of the work required by this section, the greenroof materials manufacturer will provide a written two (2) year warranty, covering the growth and establishment of the vegetative greenroof cover to 80% coverage of the greenroof planted surface.  Issuance of the Manufacturer’s Vegetative Coverage Warranty requires the following: (1) Waterproofing system products, root barrier, drainage, insulation, growing media and plant material shall have been provided by a single manufacturer, (2) Installation of growing media and plant material shall have been performed by Manufacturer's Approved Applicator or Landscaper; (3) Installation inspected by Independent Inspection Firm per Section 1.06; (4) Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties; (5) Two-year Vegetation Maintenance Program shall be implemented.

Part II	Products

  - General

    - All components must be single source from membrane manufacturer to ensure system compatibility.

- Provide waterproofing and greenroof assembly materials manufactured or supplied by CETCO:

CETCO

2870 Forbs Avenue

Hoffman Estates, Illinois 60192 USA

800-527-9948 Toll free

847-851-1800 Phone

847-851-1899 Fax

www.cetco.com/BMG

2.011		DISTRIBUTOR

Bowman Construction Supply

10801 E. 54th Avenue

Denver, CO 80239

Phone: (303) 696-8960

2.02	Materials

- Membrane shall be STRATASEAL HR, a hot applied rubberized asphalt meeting the following physical properties.

| Property | Test Standard | Typical Result |
| --- | --- | --- |
| Color | No standard test | Black |
| Solids Content | ASTM D1353 | 100% |
| Softening point | ASTM D96 | 190ºF |
| Flash Point | ASTM D92 | 464ºF |
| Water Vapor Permeance | ASTM E96e | 0.7 ng/Pa*s*m2 |
| Toughness | CGSB 37.50-M89 | 10.2 Joules |
| Ratio of Toughness to Peak Load | CGSB 37.50-M89 | 0.07 |
| Adhesion | CGSB 37.50-M89 | Pass |
| Low temperature crack bridging capacity | CGSB 37.50-M89 | No cracking/no adhesion no splitting |
| Penetration 0.1mm | ASTM D1191(1/10mm) | 69 @ 77ºF 137 @ 120ºF |
| Flow, MM | CGSB-37.50-M89 | 2 mm @ 60ºC |
| Water resistance | CGSB-37.50-M89 50ºC for 4 days | No delamination No blistering No emulsification No deterioration No pin holes |
| Heat stability | CGSB-37.50-M89 | Aged samples No change in viscosity Penetration flow or Low temp flexibility |
| Low temperature | CGSB-37.50-M89 | No cracking |
| Flexibility & adhesion |  | No delamination No adhesion loss |

- Primer shall be a surface conditioner for concrete surfaces. Acceptable products include: (select product(s) per project requirements)

  - Strataprime WB – water based concrete surface conditioner.

  - Strataprime SB – solvent based concrete surface conditioner.

- Membrane Reinforcement shall be per manufacturer’s standard details: (select product(s) per project requirements)

  - Stratabond 100 – 1.5-oz (42.5 g) non-woven, spunbond polyester fabric.

  - N-Flash – 60-mil (1.5 mm) uncured neoprene rubber sheet.

- Protection layer shall be one of the following: (select product(s) per project requirements)

  - RAP 200 – 90-mil (2.3 mm) rubberized asphalt protection course reinforced with synthetic fibers with a sand surface.

  - RAP 250FR – 140-mil (3.6 mm) fire resistant rubberized asphalt protection course reinforced with fiberglass with a granulated surface.

  - RAP 400 – 40-mil (0.9 mm) protection membrane derived from recycled tire crumb rubber reinforced with a high tensile strength fabric layer.

- Flashing shall be one of the following: (select product(s) per project requirements)

  - N-Flash – 60-mil (1.5 mm) uncured neoprene rubber sheet. N-FLASH flashing applications require the use of bonding adhesive, splicing cement, and lap sealant.

  - Flash SA – 70-mil (1.8 mm) self-adhering rubberized asphalt reinforced with a fiberglass mat with a sand surface.

- Root Barrier GS-110: GS-110 Root Barrier is a 10-mil (0.25 mm) thick, single ply polyethylene sheet used as a root barrier layer within waterproofing assemblies. GS-110 is manufactured with polyethylene resins that provide high tensile strength, high puncture resistance, low moisture vapor permeability, as well as excellent resistance to roots and decay. Seal over laps with CETCO SeamTape.

- Insulation shall be one of the following: (edit to project requirements)

  - XPS40 – 1.0” , 1.5” or 2” (25 mm, 38 mm or 51 mm) thick extruded polystyrene meeting ASTM C-578 Type VII with a minimum compressive value of 40PSI and a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu.

  - XPS60- 1.5” or 2.0” (38 mm or 51 mm) thick extruded polystyrene meeting ASTM C-578 Type VII with a minimum compressive value of 60PSI and a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu.

- Filter Fabric: BB-200 (optional) is a non-woven polypropylene geotextile filter fabric that protects the insulation layer by preventing stone and gravel as well as migration of particle fines from dropping between the joints of the insulation. It also can serve as a temporary confining layer for the insulation course when spot ballast is placed over it.

- (Optional) Aeration Layer: Aquadrain G20 prefabricated 3-dimensional composites meeting the following physical properties: 40,000 PSF (1,915,212 n / m2) compressive strength per ASTM D1621 (mod); thickness of 0.25” (6.35 mm); 7 gpm/ft (87 lpm/m) width flow capacity per ASTM D4716. (edit to project requirements) (required with combination of moisture retention mat and insulation).

- (Optional) Moisture Retention Mat: GS-232 (optional) with a weight of 32-oz/sq-yd (1.085 kg/m2). (Aeration Layer required between insulation and Moisture Retention mat).

- Drainage: Aquadrain GS-300 – having a compressive strength per ASTM D1621 (mod) of 30,000 PSF (1,436,407 n/M2) and a thickness of 0.45 in. (11.4 mm) with a flow capacity per ASTM D4716 of 22.5 gpm/ft. (276 lpm/m) of width.  GS-300 has a 120 g/m2 spunbond filter fabric on the upper side.

- Growing Media:  GreenScapes GS-505  that meets the following performance parameters per project specifications and design. Growing media shall be capable of supporting the project’s specified vegetation.

| Property | GS-500 Extensive |
| --- | --- |
| Grain Size Distribution |  |
| clay fraction | < 5 % |
| passing #200 sieve | 1-10 % |
| passing #60 sieve | 10-25 % |
| passing #18 sieve | 20-50 % |
| passing 1/8-inch sieve | 50-80 % |
| passing 3/8-inch sieve | 80-100 % |
| Density |  |
| Application Density | 0.54 - 0.77 g/cm3 (34 lbs – 48 lbs/cf) |
| Saturated Density | 0.86 - 1.0 g/cm3 (54 lbs – 63 lbs/cf) |
| Dry Density | 0.48 -0.72 g/cm3 (30 lbs – 45 lbs/cf) |
| Water & Air Management (% vol.) |  |
| saturated water capacity | >25 % |
| saturated air content | >10 % |
| Saturated Hydraulic Conductivity | .004-012 cm/s (5.4-.16.8 in/hr) |
| pH, Lime, and Salt Content |  |
| pH (saturated paste) | 6.0 - 7.8 |
| carbonate content | <25 g/l |
| salts content (water extract) | <2.5 g/l (<2.0 mmhos/cm) |
| Organics* |  |
| OM content | 3 – 6 mass % |
| C/N ratio | <20 |
| Nutrients** (plant available) | in lb/1,000 ft3 |
| nitrogen (NO3) | 3 – 15 |
| phosphorus | 1 – 7 |
| potassium | 6 – 15 |
| CEC Capacity | >5 cmol/kg |

- Values may be adjusted due to availability of local materials or special project conditions related to plant selection and/or environmental conditions.

- ** Nutrients shall be adjusted with appropriate slow-release fertilizer with micronutrient additions if below lower target range.

- CETCO Extensive Greenroof Plants: Specified plants supplied by CETCO via qualified growers per project specifications.

- Source Source Responsibility: The vegetated roof plant material shall be (edit to requirements) Greenroof Plugs (72-cell; 24-cell), Bulk Sedum Cuttings, Sedum Tiles, Sedum Carpet

- Contact: 	CETCO

2870 Forbs Avenue

Hoffman Estates, IL 60192

847-851-1823

steve.skinner@cetco.com

- Plant Material

        - CETCO Greenroof Plugs CETCO Greenroof Plugs shall be healthy, vigorous, well rooted and established in the container in which they are growing.  They shall have tops of good quality and be in a healthy growing condition.  They shall have a well-established root system reaching the sides of the container and maintain a firm, complete root ball upon removal from the container. CETCO Greenroof Plugs shall be grown and delivered in a continuous plug tray and conform to the following cell count and plug size. (edit to requirements)	24-cell plugs  2 5/8” w x 2 ½” d 72-cell plugs 1 ½’ w x 2” d.

        - CETCO Sedum Cuttings CETCO Sedum Cuttings shall be harvested from healthy, vigorous plants while in a vegetative growth mode.  They shall range in length from ½” to 3” and possess sufficient rooting nodes to allow for rapid root development once sown.  CETCO Greenroof Cuttings shall be harvested, cooled and dried for 24 hours prior to boxing for shipment and delivered in an insulated box with enclosed ice packs to ensure the cuttings remain cool until they are delivered.

        - CETCO Sedum Pre-Vegetated Tiles:

- CETCO Sedum Tiles are made up of a coconut fiber base filled with a planting substrate, and pre-cultivated with a layer of low-profile, drought-tolerant vegetation adapted to rooftop conditions.  They measure 15” x 20” (2.08 square feet)

        - CETCO Pre-Vegetated Sedum Mat

- CETCO Sedum Mat are made up of a coconut fiber base filled with a planting substrate, and pre-cultivated with a layer of low-profile, drought-tolerant vegetation adapted to rooftop conditions.  They measure 1m X 2m (25 square feet)

- CETCO Sedum Mats are made up of a coconut fiber base covered with a planting substrate, and pre-cultivated with a layer of low-profile, drought-tolerant vegetation adapted to rooftop conditions.

- Each Sedum Mats measure approximately 48” wide by 75” long and ranges from 1” to 2” in height on delivery

- CETCO Sedum Mats maximum wet weight is 150 lbs. each (6.0 lbs/sf).

- CETCO Sedum Mats shall have a minimum 85% vegetation coverage upon delivery to the site using a succulent plant mix of 8-11 varieties of Sedum.

Part III	Execution

  - Inspection

- The Installer, with the Owner’s Independent Inspector, shall examine all surfaces and other conditions under which this section of work is to be performed and notify the contractor in writing of circumstances detrimental to the proper completion of the work. Do not proceed with work until unsatisfactory conditions are corrected and are acceptable for compliance with Manufacturer’s warranty requirements. General conditions acceptable for the installation are list below. For conditions not covered in this Section contact the Manufacturer for application guidance.

  - Preparation

- Cast-in-place concrete or composition decks must be monolithic, smooth, and free of voids, spalled areas, laitance, honeycombs, and protrusions. New concrete should be cured 28-days with a light brush or wood float finish texture. A steel float finish will provide too smooth of a surface for proper adhesion of the waterproofing materials, therefore concrete surfaces that have a steel float finish must be mechanically treated prior to the application of the waterproof material.

- Precast concrete decks shall be mechanically secured to minimize movement. All joints must be grouted.

- Plywood decks shall be a minimum thickness of ½” (12.7mm), exterior grade tongue & groove and mechanically secured with structural support according to all applicable codes. All butt joints shall be supported by framing.

- Metal decks must be a minimum of 22 gauge (0.76 mm) steel decking with adequate structural support according to all applicable codes and include gypsum board a minimum thickness of 5/8” (15.8mm) fire rated type “X” and mechanically fastened accordingly to all applicable codes.

- If the project is a re-roof or tear-off, then all existing roofing material must be removed down to the bare deck. The deck must be an acceptable deck type as stated below.

  - Concrete decks must be mechanically cleaned to ensure adequate adhesion of the waterproofing material.

  - Plywood decks must be inspected for any signs of mold or mildew and remove and replace any boards that have any amount of mold or mildew. Remove and replace any boards that have any delaminating, deterioration or have excessive warping or curling.

  - Metal decks must be inspected for any signs of deterioration or rust. Remove and replace any sections that have any indication of deterioration or rust.

- Remove all dirt, debris, oil, grease, cement laitance or other foreign matter which will impair the adhesion and performance of the waterproofing membrane.

- Protect adjacent work areas and finished surfaces from damage or contamination during installation operations.

- Expansion joints 2” (50 mm) or greater should be sealed with applicable expansion joint material by others. Detail waterproofing membrane to expansion joint per manufacturer’s standard details.

  - General Installation Guidelines

    - Primer

  - Apply primer per manufacturer’s guidelines to all surfaces to receive Strataseal HR hot applied rubberized asphalt membrane. Allow primer to dry prior to installing the membrane. The surface of the concrete will look discolored, but not blackened. Do not allow the primer to pool or become contaminated. Note: Membrane will not adhere properly to wet primer.

- Strataseal HR Membrane Preparation

  - The membrane is heated in a double jacketed, oil bath type tank with mechanical agitation designed for hot applied rubberized asphalt membrane. Avoid overheating of hot applied rubberized asphalt. Do not use direct fire melting equipment.

  - Heat membrane until membrane can be drawn free flowing and lump free at a temperature range of 320°F to 340ºF (160°C to 170ºC). Do not exceed safe operating temperature of 375° F (190° C).

- Details & Flashing

  - All details and flashings must be completed in accordance with Manufacturers most recent installation guidelines and detail drawings. Non-moving cracks and joints up to 1/16” (1.6mm) require no special treatment.

  - Reinforce all non-moving cracks and joints 1/16” (1.6mm) to 3/16” (4.8mm) in width with minimum 6” (150mm) wide strip of FLASH SA or a minimum 6” (150mm) wide strip of STRATABOND 100 fabric reinforcement embedded in 90-mil (2.3mm) thick by 9” (225mm) wide tack coat of STRATASEAL HR. Embed the reinforcing while the tack coat is still warm and tacky. Overlap reinforcing strip ends a minimum 2” (50mm), ensuring lap receives rubberized asphalt.

  - Reinforce all non-moving cracks and joints 3/16” (4.8mm) to 1/2” (12mm) in width with minimum 6” (150mm) wide strip of N-FLASH or FLASH SA embedded in 90-mil (2.3mm) thick by 9” (225mm) wide tack coat of STRATASEAL HR. Embed the reinforcing while the tack coat is still warm and tacky. Overlap reinforcing strip ends a minimum 2” (50mm), ensuring lap receives rubberized asphalt.

  - Precast Deck Joints: Reinforce all non-moving, grouted precast deck joints with a minimum 6” (150mm) wide strip of N-FLASH or FLASH SA embedded in 90-mil (2.3mm) thick by 9” (225mm) wide tack coat of STRATASEAL HR. Embed the reinforcing while the tack coat is still warm and tacky. Overlap reinforcing strip ends a minimum 2” (50mm), ensuring lap receives rubberized asphalt.

  - Deck-to-Deck Wall Transitions: Install FLASH TG/TS/SA up face of wall per project requirements and extend flashing onto deck a minimum 6” (150mm) without wrinkles or fishmouths. Overlap flashing end laps a minimum 6” (150mm). Apply STRATASEAL HR membrane to deck corner over flashing extending onto horizontal deck; with STRATABOND 100 reinforcing fabric terminating minimum 1” (25mm) prior to membrane termination at deck corner. For deck termination incorporating N-FLASH, refer to manufacturer’s current N-FLASH details and guideline instructions.

  - Deck-to-Below Grade Property Line Wall Transitions: Install minimum 90-mil (2.3mm) thick by 12” (300mm) wide tack coat of STRATASEAL HR at perimeter deck edge along property line wall.  Apply minimum 90-mil (2.3mm) base layer of Strataseal HR membrane as a continuous monolithic coat over entire deck area to be waterproofed. Fully embed a layer of Stratabond 100 reinforcement fabric into the top surface of the base coat. Apply minimum 125-mil (3.2mm) top layer of Strataseal HR hot applied rubberized asphalt membrane over the reinforcing fabric in a continuous monolithic coat.  While the top layer is still warm and tacky, lay down and embed the minimum 12” (300mm) exposed section of the property line wall waterproofing membrane into the top coat of the STRATASEAL HR. Finally, apply a minimum 60-mil (1.6mm) thick by 18” (450mm) wide seal coat of STRATASEAL HR at perimeter deck edge along property line wall.

- Reinforced Rubberized Asphalt Membrane Installation

  - Apply minimum 90-mil (2.3mm) base layer of Strataseal HR hot applied rubberized asphalt membrane as a continuous monolithic coat over entire area to be waterproofed; including all crack and joint detailing and flashing interfaces.

  - While the base layer is still warm and tacky, fully embed a layer of Stratabond 100 reinforcement fabric into the top surface of the base coat; overlapping fabric seams a minimum ½” to 1” (25mm) and ensuring a layer of membrane between overlaps. Firmly press the reinforcing fabric into the base layer of Strataseal HR membrane.

  - Apply minimum 125-mil (3.2mm) top layer of Strataseal HR hot applied rubberized asphalt membrane over the reinforcing fabric in a continuous monolithic coat.  Total minimum membrane thickness shall be 215-mils (5.5mm) over entire area to be waterproofed.

- Protection Layer

  - While the top layer of Strataseal HR hot applied rubberized asphalt membrane is still warm and tacky, unroll and embed the specified protection layer sheet into the membrane ensuring a good bond.

    - Apply RAP 400 after the rubberized asphalt waterproofing membrane has cooled below, 200° F (93° C).  Apply RAP 400 directly to top surface of the rubberized asphalt waterproofing membrane with fabric layer side down.

  - Overlap the laps and seams of the protection layer 3” (75mm) and seal with Strataseal HR hot applied rubberized asphalt in the seams and laps as specified.

- Perform Electronic Leak Detection (ELD) test over the entire waterproofing membrane installation per Quality Assurance Section 1.06F.  For areas to receive ELD testing provide the following:

  - Prior to installation of the waterproofing membrane a complete installation and field testing procedure guideline, as provided by the ELD system manufacturer, shall be provided to the Installer, General Contractor, Manufacturer, Architect and Owner.

  - Thoroughly wet the waterproofing membrane in area of test.  Wetting can be accomplished by hand or mechanical spray devises.  Membrane must be wet during the testing procedures.  Ponded water is not necessary.

  - Visually inspect and perform ELD testing to locate membrane breaches, if any. Document location of breaches found by the ELD test and visual inspections.

  - Repair all breaches found per waterproofing manufacturer’s guidelines. Leave ELD conductor wire grid in place as secured to waterproofing membrane.

  - Once membrane ELD testing is concluded and all repairs are complete, the membrane shall be immediately protected. General Contractor shall prohibit non-waterproofing construction traffic, activity and material storage on the tested membrane.

- Root Barrier

  - Install Root Barrier over protection layer to provide a continuous layer to stop root penetration.  Overlap all root barrier sheet edges a minimum 6” (150 mm) and a minimum of 4’ (1.2 m) between all overlaps. Keep overlaps a minimum of 4’ (1.2 m) from all perimeters. Secure root barrier under any perimeter metal counter flashings. Seal all edges with CETCO Seamtape for GS-110).

  - Cut root barrier sheet to fit close to all perimeter, protrusions and obstructions. Seal cut sheet of overlap flashing patch of Root Barrier with CETCO Seamtape GS-110 .

  - Provide spot ballast (i.e. sand bags) as required to hold Root Barrier in place prior to landscape topping installation.  Remove spot ballast as landscape topping work proceeds.

- Insulation

  - Install the insulation loose over the root barrier, firmly butting each adjacent board. Do not leave gaps between adjacent boards.

  - If multiple layers of insulation are required, then install the thicker layer on the bottom. Rotate the direction of each layer 90° and stager seams. All layers of insulation must be un-adhered to each other.

  - Cut insulation to fit close to all cants, protrusions, and obstructions.

- Filter Fabric (optional)

  - Install BB-200 filter fabric over the insulation board overlapping all seams 6” (150 mm).  Cut to fit tightly at perimeters, corners and at all penetrations.

- Aeration Layer (required above insulation when Moisture Retention Mat is used)

  - Install Aquadrain G20 on horizontal and vertical surfaces over insulation course in accordance with Manufacturers installation procedures. Abut all drainage sheet edges for continuous layer.  Seal all edges by overlapping and then bonding extra fabric flap edges to adjacent drainage course fabric with a general construction adhesive to ensure integrity.

  - Cut aeration sheets to fit close to all perimeter, protrusions and obstructions.

- Moisture Retention  Mat (optional)

  - Place the moisture retention mat over the aeration layer (on insulated assemblies).

  - Overlap all edges a minimum of 4” (100 mm). Extend 6” (150 mm) beyond growing medium laying up all vertical surfaces. Trim to just below level of soil avoiding exposure.

- Drainage Layer (edit to requirements)

  - Install Aquadrain GS-300 course over the insulation or Moisture Retention Mat, if used, in accordance with Manufacturer’s installation procedures.

  - Cut drainage to fit close to all perimeter, protrusions and obstructions.

  - Place subsequent ballast materials on as soon as possible.

- Growing Media

  - Install growing media in strict accordance with the project specifications and design requirements. Avoid damage or displacement of other components including filter fabric, insulation, drainage composite, wall, hardscape and roofing.

- Vegetation

  - Environmental Conditions:

    - Greenroof Plants should be installed after the 90% probability date of last frost in the spring (36 degree F temperature threshold) and before the 90% probability date of first frost in the fall (36 degree F temperature threshold) in the site area or nearest reporting station.  See Climatography of the US No. 20 at: www.ncdc.noaa.gov/oa/climate/freezefrost/freezefrost.pdf for statistical interpretation of date of last frost/date of first frost.

      - Greenroof Plants should not be installed in waterlogged media

      - Greenroof Plants should not be installed during prolonged periods of drought unless irrigation is available.

      - Greenroof Plants must be installed within two days of delivery or contractor must maintain their healthy condition until planted.

  - IRRIGATION

    - Irrigation water must be applied until the roots are established in the growing media on the roof (6-8 weeks after installation).

      - Thoroughly water entire vegetated roof surface immediately after installation.

      - Deliver ≥ ¼” water, 2 times per week for the first 2 weeks.

      - Deliver ≥ ¼” water, 1 time per week for the next 6-8 weeks.

      - Extended irrigation requirements are dependent upon project location, conditions, and plant selection. It is recommended that if a permanent irrigation system is not installed, that a backup system (such as hose bibs located on the roof) be available for use during prolonged periods of drought (>4 weeks with less than a total of ¼” precipitation

  - MAINTENANCE

    - System installer shall maintain the vegetated roof for a period of at least [XXX] (edit to requirements) days after essential completion.

    - Maintenance activities shall include:

      - Initial Establishment

      - Water the vegetated roof system 2 times a week for the first two (2) weeks and 1 times a week for the next 6-8 weeks as needed to maintain a moist condition to aid in root establishment. Water the system more frequently during extended periods of hot, dry weather conditions and less frequently if periodic rains maintain a moist surface condition.

      - Provide hand weeding as necessary to remove undesirable species as they appear.

      - Replace areas of damaged plants or bare spots using additional plant material.

      - Remove any debris that appears on the roof.

      - Observe surface for any erosion of the growing media and repair/replace growing media as needed.  Plant additional plants on any disturbed areas.

      - Mature Coverage Establishment

      - Continue weekly visits for a minimum of 2 months after essential completion.  Perform watering, weed removal, repair of eroded or non-vegetated areas and debris removal as needed.

      - After the first two months, evaluate conditions and if plant growth is progressing well, reduce frequency of visits to monthly (during the growing season) for the remainder of the first year (note: the first year may span two growing seasons).  If plants appear weak or are not developing well, apply a slow-release fertilizer with an analysis of 5-3-4 (N-P-K) + micronutrients or similar.  Fertilizer can be applied in a time period between April – August but only if same day temperatures are expected to remain below 90 degrees F.

      - After first year, evaluate conditions and if plant growth is progressing well, continue monthly visits or reduce frequency as needed to maintain a vigorous plant condition and achieve and maintain a minimum of 80% plant coverage.   Each visit should include watering, weed removal, repair of eroded or non-vegetated areas and debris removal as needed.

- Hardscape/Pavers

  - Install hardscapes and/or Architectural pavers in strict accordance with the project specifications and design.  Follow manufacturer’s installation guidelines with all applicable accessory products.

  - Job Completion

    - Clean-Up

- In areas where adjacent finished surfaces are soiled by work of this Section, consult Manufacturer of surfaces for cleaning advice and conform to their recommendations and instructions.

- Remove all debris, tools, equipment and remaining product on-site. Dispose of debris and damaged product following all applicable regulations.

    - Inspection

  - The Installer with the Owner’s Independent Inspector shall examine all completed work.

END OF SECTION  071413