This guide specification was issued February 2009 and may be superseded without notice at any time. Therefore, please confirm that this specification is still current and has not been superseded by checking at www.cetco.com or by calling CETCO at 1-847-851-1800.

CAST-IN-PLACE CONCRETE CONSTRUCTION SPECIFICATION

This guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute and is intended for use with cast-in-place concrete structures. This specification is not intended for use with shotcrete construction. Contact CETCO regarding installation and application guidelines for Strataseal HR Waterproofing System when used with shotcrete construction. CETCO, Building Materials Group – 1- 800-527-9948.

This master guide specification contains work sections in PART 3 – Execution – pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project.

STRATASEAL HR HOT RUBBERIZED ASPHALT WATERPROOFING GUIDE SPECIFICATION

Split-Slab Construction Assembly

STRATASEAL HR® HOT-APPLIED RUBBERIZED ASPHALT

WATERPROOFING SYSTEM  MASTER GUIDELINE SPECIFICATION

FOR PLAZA DECKS WITH ARCHITECTURAL PAVERS

Part I	General

  - Related Documents

- All of the contract documents, including General and Supplementary General Conditions and Division 1 General Requirements, apply to the work of this section.

  - Related Sections

- Carefully examine all of the Contract Documents for requirements which affect the work of this section.

- Other specification Sections which directly relate to the work of this section include, but are not limited to, the following:

  - Section 03 50 00 Cast Decks and Underlayment

  - Section 05 30 00 Metal Decking

  - Section 06 10 00 Rough Carpentry

  - Section 07 10 00 Dampproofing and Waterproofing

  - Section 07 25 00 Weather Barriers

  - Section 07 60 00 Flashing and Sheet Metal

  - Section 07 70 00 Roof and Wall Specialties and Accessories

  - Section 07 90 00 Joint Protection

  - System Description

- Furnish and install a 215-mil (5.5mm) thick, reinforced hot-applied rubberized asphalt waterproofing membrane assembly with applicable detailing and accessory products per project specifications and drawings, or per waterproofing membrane manufacturer details approved by architect. Waterproofing assembly shall be covered with precast architectural pavers per project specifications, layout and pattern.

  - Submittals

- Prior to commencement of the work, process submittals in accordance with the “Conditions of the Contract”.

- Submit manufactures product data complete with general and specific installation instructions, recommendations and limitations.

- Submit product samples representative of the hot applied rubberized asphalt, reinforcement fabric, protection layer, insulation, filter fabric, and ballast.

- Submit material certification(s) signed by manufacturer certifying materials comply with specific performance characteristics and physical requirements. Certification must evident that all materials are supplied by a single source manufacturer.

- Submit at time of bid, manufacturer’s written document that installer is certified as a current  Approved Applicator with manufacturer.

- Submit sample copy of manufacturer’s waterproofing warranty identifying the terms and conditions.

  - Quality Assurance

- Installer must be a company with a minimum of at least three (3) years experience in work of the type required by this section, who can comply with the manufacturers warranty requirements, and who is an Approved Applicator as determined by manufacturer.

- Manufacturer must be a company with a minimum of forty (40) years in the direct production and sales of waterproofing materials. Manufacturer shall be capable of providing field service representation during construction, and recommending installation methods. Manufacturer shall have certified, approved applicators for membrane installation.

- Conduct a pre-installation conference prior to commencement of field installation to review conditions, establish procedures to maintain required working conditions and to coordinate this work with related and adjacent work. Representatives of the General Contractor, Architect, Installer, and Manufacturer shall be present at pre-installation conference.

- Construct a minimum 10-ft x 10-ft mock-up of waterproofing membrane incorporating all of the components including: concrete deck, primer, hot applied rubberized asphalt, reinforcement fabric, and protection layer. Successful mock-up may remain as part of work.

- Maintain copy of manufacturer’s installation instructions and MSDS for all products on job-site as well as allow access to the job-site by Owner’s Independent Inspector, and Manufacturer Agent.

- Owner shall make arrangements and payments for an independent inspection service to monitor installation compliance with the project documents and Manufacturer’s published literature, installation instructions, and site specific details. Independent inspection firm shall be a company participating with the Manufacturer’s Certified Inspection Program. Inspection service shall produce reports and digital photographs documenting each inspection. Reports shall be made available in a timely manner to the Installer, General Contractor, Manufacturer, Architect and Owner.

  - Delivery, Storage and Handling

- Deliver materials in original unopened packaging, clearly labeled with manufacturers labels indicating name of manufacturer, product and all identifying numbers.

- Storage of materials must be in an appropriate location and manner as to protect from any construction damage, as well as damage from weather, prolonged sunlight, excessive temperature and sources of ignition. Remove of any damaged material from job-site and dispose of in accordance with applicable regulations. Do not double stack pallets during shipping or storage. Allow adequate ventilation.

- Handling of materials to be in accordance with manufacturers instructions. Melting equipment shall consist of double jacketed, oil bath melter with mechanical agitator. Avoid overheating of hot applied rubberized asphalt.

  - Project Conditions

- All federal, state and local regulations, codes, and safety standards must be adhered to at all times.

- Do not apply waterproofing system if temperature is less than 0ºF (-18ºC). Application of hot applied rubberized asphalt shall not be performed during rain, snow or inclement weather; or on frost or wet covered surfaces.

- The deck must be properly cleaned and prepared free of any and all contaminations.

- The work area must be adequately ventilated. Warn personnel against breathing of vapors and contact of material with skin and eyes.  Limit access to required personnel during the installation process. Do not use flammable products near spark or an open flame. Do not allow the use of spark producing equipment during application and until all vapors have dissipated.  Post “NO SMOKING” signs. Wear appropriate protective clothing and respiration protection gear at all times.

- Protect adjoining surfaces not to be waterproofed against damage or soiling, including plants, vegetation and animals which may be affected by the waterproofing operations.

- Provide adequate protection for membrane after installation. Do not allow any foot or vehicular traffic on unprotected membrane. Do not allow any material or waste products to contaminate membrane. Contact Manufacturer to determine performance impedance, if any, caused by contamination of the membrane.

  - Warranty

- Upon completion of work, contractor to provide owner with a single source warranty.

- Warranty must be validated by Manufacturer confirming acceptance of installation, including independent inspection reports, in accordance with all applicable instructions.

- Manufacturer’s HydroShield Warranty.

  - HydroShield Warranty: Upon completion and acceptance of the work required by this section, the waterproofing materials manufacturer will provide a written five (5) year warranty, covering both materials and labor to the project owner. Issuance of Manufacturer's HydroShield Warranty requires the following: (1) Waterproofing system products, drainage and insulation course products, and subsequent assembly products shall have been provided by a single manufacturer; (2) Installation of waterproofing products, drainage and insulation course products and subsequent products by Manufacturer's Approved Applicator; (3) Installation inspected by Independent Inspection Firm per Section 1.05F; (4) As applicable, installation of Waterstop-RX in all concrete pour joints. Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties.

Part II	Products

  - General

    - All components must be single source from membrane manufacturer to ensure system compatibility.

- Provide waterproofing and assembly materials manufactured or supplied by CETCO:

CETCO – Building Materials Group, 2870 Forbs Avenue, Hoffman Estates,

Illinois 60192 USA 800-527-9948 Toll free; 847-851-1800 Phone; 847-851-1899 Fax

www.cetco.com/BMG

2.011		DISTRIBUTOR

Bowman Construction Supply

10801 E. 54th Avenue

Denver, CO 80239

Phone: (303) 696-8960

2.02	Materials

- Membrane shall be STRATASEAL HR, a hot applied rubberized asphalt meeting the following physical properties.

Property	Test Standard	Typical Result

Color	No standard test	Black

Solids Content	ASTM D1353	100%

Softening point	ASTM D96	185ºF

Flash Point	ASTM D92	525ºF

Water Vapor Permeance	ASTM E96e	<0.01 perms-inch

Toughness	CGSB 37.50-M89	>5.5 Joules

Ratio of Toughness to Peak Load	CGSB 37.50-M89	>0.040

Adhesion	CGSB 37.50-M89	Pass

Low temperature crack	CGSB 37.50-M89	No cracking/no adhesion

bridging capacity		no splitting

Penetration 0.1mm	ASTM D1191	< 100 @ 77ºF

(1/10mm)	< 220 @ 120ºF

Flow, MM	CGSB-37.50-M89	Max 3 @ 60ºC

ASTM D1191	0 @ 120ºF

Water resistance	CGSB-37.50-M89	No delamination

50ºC for 4 days	No blistering

No emulsification

No deterioration

No pin holes

Heat stability	CGSB-37.50-M89	Aged samples

No change in viscosity

Penetration flow or

Low temp flexibility

Low temperature	CGSB-37.50-M89	No cracking

flexibility & adhesion		No delamination

No adhesion loss

- Primer shall be a surface conditioner for concrete surfaces. Acceptable products include: (select product(s) per project requirements)

  - Strataprime WB – water based concrete surface conditioner.

  - Strataprime SB – solvent based concrete surface conditioner.

- Membrane Reinforcement shall be per manufacturer standard details: (select product(s) per project requirements)

  - Stratabond 100 – 1.5-oz non-woven, spunbonded polyester fabric.

  - N-Flash – 60-mil uncured neoprene rubber sheet.

  - FLASH SA – 70-mil self-adhered rubberized asphalt reinforced with a fiberglass mat with a sand surface.

- Protection/Separation layer shall be: (select product(s) per project requirements)

  - RAP 200 – 90-mil rubberized asphalt protection course reinforced with synthetic fibers with a sand surface.

  - RAP 250FR – 140-mil fire resistant rubberized asphalt protection course reinforced with fiberglass with a granulated surface.

  - RAP 350FR – 160-mil fire resistant rubberized asphalt protection course reinforced with fiberglass with a granulated surface.

- Flashing shall be: (select product(s) per project requirements)

  - N-Flash – 60-mil uncured neoprene rubber sheet. N-FLASH flashing applications require the use of bonding adhesive, splicing cement, and lap sealant.

  - Flash TS – 150-mil torch weld rubberized asphalt reinforced with a fiberglass mat with a sand surface.

  - Flash TG - 160-mil torch weld rubberized asphalt reinforced with a fiberglass mat with a granulated surface.

  - Flash SA – 70-mil self-adhering rubberized asphalt reinforced with a fiberglass mat with a sand surface.

- Insulation shall be Styrofoam Brand (Type) as manufactured by The Dow Chemical Company, marketed by CETCO: (edit to project requirements)

  - XPS60 – 60PSI minimum compressive value extruded polystyrene rigid insulation meeting ASTM C-578 Type VII with a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu.

  - XPS100- 100PSI minimum compressive value extruded polystyrene rigid insulation meeting ASTM C-578 Type VII with a maximum water absorption value per ASTM C272 of less than 0.1% and having an R value per inch of 5.0 °F ft2 h/Btu.

- Drainage course shall consist of a HDPE geonet core with a geotextile fabric integrally bonded to both sides of the core meeting the following physical properties :

  - Aquadrain G20 - 40,000 PSF compressive strength per ASTM D1621 (mod) ;  thickness of 0.25” ; 7 gpm/ft width flow capacity per ASTM D4716.

- Filter fabric layer shall be BB-200 having a 2.65-oz weight non-woven, spunbonded polyester water permeable fabric.

- Architectural Pavers placed per project specifications.

  - Furnish and install concrete pavers per project design. Paver type, size, color, thickness, and surface texture as specified by architect. Pavers shall be manufactured by Wausau Tile Inc., Wausau, WI (1-800-388-8728, 715-359-3121, Fax: 715-359-7456) or approved equal that meets waterproofing system warranty requirements.

  - Precast Concrete Pavers: Paver units shall be type __________, sized 23-13/16” x 23-13/16” x 2” thick with surface texture  ______ and color ________ (Note: edit this section for paver(s) type, size, surface texture and color to meet project requirements. Refer to specific manufacturer’s paver part numbers, sizes, texture and color codes).

1. Compressive Strength: Each paver unit shall have a compressive strength of 8,000 psi

with no individual unit less than 6,500 psi when tested in accordance with ASTM C140.

2. Flexural Strength: Each unit shall have a flexural strength of 700 PSI when tested

in accordance with ASTEM C293.

3. Water absorption: Shall not be greater than 6% according to ASTM C140.

4. Freeze/thaw: Durability of the paver shall meet the freeze/thaw tests in accordance

with Section 8 of ASTM C67. Specimens, when tested, shall have no breakage and not

greater that 1% loss in dry weight of any individual unit when subject to 50 cycles of

freeze/thaw.

5. Center load: Pavers shall support a minimum concentrated load of 1,850 lbs. When

pressure is applied to a paver supported on four (4) corners. WT CL96

6. Sizing: Permissible variations in dimensions shall not differ by more than 1/16” from

width, height, length or thickness. Standard units are manufactured with a 3/16” bevel

on all four (4) sides of finished surface. Unit shall conform to a true plane and not differ

by more than 1/16”in either concave and/or convex warpage.

7. Coloring: Coloring used shall conform to ASTM Standards where applicable.

  - Pedestals and all other paver accessories shall be obtained through paver manufactuer or approved equal but must meet paver manufacturer’s installation and warranty criteria. Pedestals shall be adjustable height or fixed height as required by paver manufacturer.

  - Architectural Precast Site Amenities to compliment finish of Architectural Pavers per project design (edit to project requirements).

- Aggregates/Ballast: Well screened and washed stone gravel conforming to ASTM C33 or as specified per project; placed and spread evenly at a rate specified per project   (edit to project requirements).

- Portland Cement: Conforms to ASTM C150 specifications.

Part III	Execution

  - Inspection

- The Installer, with the Owner’s Independent Inspector, shall examine all surfaces and other conditions under which this section of work is to be performed and notify the contractor in writing of circumstances detrimental to the proper completion of the work. Do not proceed with work until unsatisfactory conditions are corrected and are acceptable for compliance with Manufacturer’s warranty requirements. General conditions acceptable for the installation are list below. For conditions not covered in this Section contact the Manufacturer for application guidance.

  - Preparation

- Cast-in-place concrete or composition decks must be monolithic, smooth, and free of voids, spalled areas, laitance, honeycombs, and protrusions. New concrete should be cured 28-days with a light brush or wood float finish texture. A steel float finish will provide too smooth of a surface for proper adhesion of the waterproofing materials, therefore concrete surfaces that have a steel float finish must be mechanically treated prior to the application of the waterproof material.

- Precast concrete decks shall be mechanically secured to minimize movement. All joints must be grouted.

- Plywood decks shall be a minimum thickness of ½” (12.7mm), exterior grade tongue & groove and mechanically secured with structural support according to all applicable codes. All butt joints shall be supported by framing.

- Metal decks must be a minimum of 22 gauge steel decking with adequate structural support according to all applicable codes and include gypsum board a minimum thickness of 5/8” (15.8mm) fire rated type “X” and mechanically fastened accordingly to all applicable codes.

- If the project is a re-roof or tear-off, then all existing roofing material must be removed down to the bare deck. The deck must be an acceptable deck type as stated below.

  - Concrete decks must be mechanically cleaned to ensure adequate adhesion of the waterproofing material.

  - Plywood decks must be inspected for any signs of mold or mildew and remove and replace any boards that have any amount of mold or mildew. Remove and replace any boards that have any delamination or have excessive warping or curling.

  - Metal decks must be inspected for any signs of deterioration or rust. Remove and replace any sections that have any indication of deterioration or rust.

- Remove all dirt, debris, oil, grease, cement laitance or other foreign matter which will impair the adhesion and performance of the waterproofing membrane.

- Protect adjacent work areas and finished surfaces from damage or contamination during installation operations.

- Expansion joints should be sealed with applicable expansion joint material. Detail waterproofing membrane to expansion joint per manufacturer’s standard details.

  - General Installation Guidelines

    - Primer

  - Apply primer per manufacturer’s guidelines to all surfaces to receive Strataseal HR waterproofing membrane. Allow primer to dry prior to installing the membrane. The surface of the concrete will look discolored, but not blackened. Do not allow the primer to pool or become contaminated. Note: Membrane will not adhere properly to wet primer.

- Strataseal HR Membrane Preparation

  - Heat Strataseal HR in a double jacketed, oil bath type tank with mechanical agitation designed for hot applied rubberized asphalt membrane. Do not use single wall, direct fire equipment to heat  rubberized asphalt membrane.

  - Heat Strataseal HR until membrane can be drawn free flowing and lump free at a temperature range of 320°F to 340ºF (160°C to 170ºC). Do not exceed safe operating temperature of 375° F (190° C).

- Details & Flashing

  - All details and flashings must be completed in accordance with Manufacturers most recent installation guidelines and detail drawings. Non-moving cracks and joints up to 1/16” (1.6mm) require no special treatment.

  - Reinforce all non-moving cracks and joints 1/16" (1.6mm) to 3/16" (4.8mm) in width with minimum 6" (150mm) wide strip of FLASH SA or a minimum 6” (150mm) wide strip of STRATABOND 100 fabric reinforcement embedded in 90-mil (2.3mm) thick by 9” (225mm) wide tack coat of STRATASEAL HR. Embed the reinforcing while the tack coat is still warm and tacky. Overlap reinforcing strip ends a minimum 2" (50mm), ensuring lap receives rubberized asphalt.

  - Reinforce all non-moving cracks and joints 3/16" (4.8mm) to 1/2" (12mm) in width with minimum 6" (150mm) wide strip of N-FLASH or FLASH SA embedded in 90-mil (2.3mm) thick by 9" (225mm) wide tack coat of STRATASEAL HR. Embed the reinforcing while the tack coat is still warm and tacky. Overlap reinforcing strip ends a minimum 2" (50mm), ensuring lap receives rubberized asphalt.

  - Precast Deck Joints: Reinforce all non-moving, grouted precast deck joints with a minimum 6" (150mm) wide strip of N-FLASH or FLASH SA embedded in 90-mil (2.3mm) thick by 9" (225mm) wide tack coat of STRATASEAL HR. Embed the reinforcing while the tack coat is still warm and tacky. Overlap reinforcing strip ends a minimum 2" (50mm), ensuring lap receives rubberized asphalt.

  - Deck-to-Deck Wall Transitions: Install FLASH TG/TS/SA up face of wall per project requirements and extend flashing onto deck a minimum 6" (150mm) without wrinkles or fishmouths. Overlap flashing end laps a minimum 6" (150mm). Apply STRATASEAL HR membrane to deck corner over flashing extending onto horizontal deck; with STRATABOND 100 reinforcing fabric terminating minimum 1" (25mm) prior to membrane termination at deck corner. For deck termination incorporating N-FLASH, refer to manufacturer’s current N-FLASH details and guideline instructions.

  - Deck-to-Below Grade Property Line Wall Transitions: Install minimum 90-mil (2.3mm) thick by 12" (300mm) wide tack coat of STRATASEAL HR at perimeter deck edge along property line wall.  Apply minimum 90-mil (2.3mm) base layer of Strataseal HR membrane as a continuous monolithic coat over entire deck area to be waterproofed. Fully embed a layer of Stratabond 100 reinforcement fabric into the top surface of the base coat. Apply minimum 125-mil (3.2mm) top layer of Strataseal HR hot applied rubberized asphalt membrane over the reinforcing fabric in a continuous monolithic coat.  While the top layer is still warm and tacky, lay down and embed the minimum 12" (300mm) exposed section of the property line wall waterproofing membrane into the top coat of the STRATASEAL HR. Finally, apply a minimum 60-mil (1.6mm) thick by 18" (450mm) wide seal coat of STRATASEAL HR at perimeter deck edge along property line wall.

- Reinforced Rubberized Asphalt Membrane Installation

  - Apply minimum 90-mil (2.3mm) thick base layer of Strataseal HR hot applied rubberized asphalt membrane as a continuous monolithic coat over entire area to be waterproofed; including all crack and joint detailing and flashing interfaces.

  - While the base layer is still warm and tacky, fully embed a layer of Stratabond 100 reinforcement fabric into the top surface of the 90-mil base coat; overlapping fabric seams a minimum ½" to 1" (25mm) and ensuring a layer of membrane between overlaps. Firmly press the reinforcing fabric into the base layer of Strataseal HR membrane.

  - Apply minimum 125-mil (3.2mm) thick top layer of Strataseal HR hot applied rubberized asphalt membrane over the reinforcing fabric in a continuous monolithic coat.  Total minimum membrane thickness shall be 215-mils (5.5mm) thick over entire area to be waterproofed.

- Separation/Protection Layer

  - While the top layer of Strataseal HR hot applied rubberized asphalt membrane is still warm and tacky, unroll and embed the specified protection layer/separation sheet into the membrane ensuring a good bond.

  - Overlap the laps and seams of the protection layer 3" (75mm) and seal with Strataseal HR hot applied rubberized asphalt in the seams and laps.

- Water Test

  - Verify that the structure can withstand the deadload weight of the water test prior to commencement of the water test. If not, then confer with the Manufacturer for alternate testing procedure.

  - Allow Strataseal HR hot applied rubberized asphalt membrane to cool.

  - Plug all drains and provide barriers necessary to contain water. Allow for overflow to protect the building in the event of rain.

  - Pond water to a depth of 2" (50mm) for a period of 48 hours. Inspect for leaks and repair membrane if leaks are found. Repeat water test process after making repairs.

  - Water test must be witnessed, documented and approved by Independent Inspector.

- Drainage Course (required at membrane level installed over protection course)

  - Install Aquadrain G20 drainage course on horizontal and vertical surfaces over protection course in accordance with Manufacturers installation procedures. Abutt all drainage core edges and secure with plastic wire straps as required to maintain a continuous layer.  Seal all edges by overlapping and then bonding extra fabric flap edges to adjacent drainage course fabric with a general construction adhesive to ensure integrity.

  - Cut drainage sheet to fit close to all perimeter, protrusions and obstructions.

- Insulation

  - Install the rigid insulation loose laid over the drainage composite layer to the specified thickness per project requirements. Firmly abutt each adjacent board without gaps between adjacent boards.

  - If multiple layers of insulation are required, then install the thicker layer on the bottom. Rotate the direction of each layer 90° and stager board seams. All layers of insulation must be unadhered to each other.

  - Cut insulation to fit close to all curbs, walls, drain boxes, protrusions, and other structural elements and obstructions as required.

- Filter Fabric (required when using insulation)

  - Place the BB-200 filter fabric over the insulation layer with all edges overlapped a minimum 12” (300mm) and a minimum of 6’ between all overlaps. Keep overlaps a minimum of 6’ from all perimeters. Secure filter fabric under any perimeter metal counter flashings.

  - Cut filter fabric around any drainage openings so to not restrict water flow to the drain. Cut filter fabric around any penetrations in such a manner as to prevent any stone ballast from entering between penetration and insulation.

  - Provide spot ballast (ie sand bags) as required to hold filter fabric in place prior to architectural topping assembly installation.  Remove spot ballast as architectural topping (concrete pavers) work proceeds.

- Drainage/Air Course (specify as required above filter fabric level where Architectural Pavers will be set in grout or sand leveling bed in lieu of approved pedestals or spacers)

  - Install Aquadrain G20 drainage course on horizontal surfaces over insulation/filter fabric layers in accordance with project design. Install Aquadrain G20 drainage composite per manufacturer’s instructions, abutting all adjacent drainage core edges and secure with plastic wire straps as required to maintain a continuous layer.  Seal all edges by overlapping and then bonding extra fabric flap edges to adjacent drainage course fabric with a general construction adhesive to ensure integrity.

  - Cut drainage sheet to fit close to all perimeter, protrusions and obstructions.

- Installation of Architectural Concrete Pavers

  - Furnish and install concrete pavers per project design. Pavers shall be specific brand, type, size, color, thickness, and surface texture as specified by architect.

  - Inspect deck and fixed elevation changes. All deck surface defects, height or location problems to be corrected before paver installation.

  - Compare deck layout to architectural and shop drawings. All variances of field conditions to drawings to be reviewed and corrected prior to starting installation.

  - Place concrete pavers, where indicated by project design layout and patterns, accurately aligned and leveled with upper surface of pavers in plane with adjacent units. Cut pavers to fit irregularly shaped areas and around protrusions. Install concrete pavers per manufacturer’s instructions on approved pedestals or leveling bed per project design. Install pedestals in strict accordance with paver manufacturer’s installation guidelines. No variance to system allowed.

  - Tolerances: Maximum 1/16” height variation between adjacent pavers. Individual pavers shall not vary more than 1/16” from level across width of the paver. Paved areas shall not vary more than ¼” from level in a distance of 10 feet measured at any location in any direction. Joints between adjacent pavers shall be 3/16” or 1/8”.

  - Damaged Pavers: Remove and replace pavers which are loose, chipped, broken, stained, or otherwise damaged, or if its units do not match adjoining units as intended. Provide new units to match adjoining units and install in the same manner as original units, with same joint treatment to eliminate evidence of replacement.

  - Cleaning: Wash and scrub clean exposed paver surfaces. Remove mortar stains and all other types of soiling from exposed paver surfaces.

  - Provide applicable means to protect paver work from damage or deterioration until time of substantial completion.

  - Job Completion

    - Clean-Up

- In areas where adjacent finished surfaces are soiled by work of this Section, consult Manufacturer of surfaces for cleaning advice and conform to their recommendations and instructions.

- Remove all debris, tools, equipment and remaining product on-site. Dispose of debris and damaged product following all applicable regulations.

    - Inspection

1. 	The Installer with the Owner’s Independent Inspector shall examine all completed work.

END OF SECTION  07 10 000