# ULTRASEAL® WATERPROOFING DIRECTIVES FOR SHOTCRETE PROPERTY LINE  FOUNDATIONS UNDER NON-HYDROSTATIC CONDITIONS

(JUNE 2010 – Supersedes All Previous Versions)

The accompanying guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute. This guide specification is intended to be adapted by the design professional to suit the requirements of individual projects. This specification provides an outline covering Parts 1, 2, & 3 with specific information about standards, quality assurance, product description, warranty requirements, and application. Specifically Part 3, Execution, contains special installation and application guidance of the Ultraseal Waterproofing System when used with below-grade shotcrete foundations planned for non-hydrostatic conditions.

This shotcrete waterproofing directive is provided in three parts as follows:

1. SHOTCRETE SUMMARY

2. SPECIFICATION COORDINATION – conveying important directives that should appear in other pertinent Sections of the Project Specifications Documents.

3. SHOTCRETE GUIDE SPECIFICATION SECTION 071700 – Ultraseal Guideline Specification for Shotcrete Applications with Aquadrain Water Collection System.

SHOTCRETE SUMMARY

Shotcrete is concrete pneumatically projected onto a surface at high velocity. It is typically blown through a hand-held nozzle, where water is added to the small aggregate concrete mix just prior to being applied and consolidated. Using shotcrete for constructing property line below-grade structural walls has become more common over the last ten years. Shotcrete typically costs less and takes less time to complete than a comparable sized cast-in-place concrete project.

However, application of shotcrete can create difficult conditions for insuring the performance of below-grade waterproofing systems. Improperly mixed or placed shotcrete can among other problems, create voids between the shotcrete and the waterproofing membrane, develop shadow voids or poor consolidation behind steel reinforcement, low moisture content can promote excessive cracking, improper cleaning during application can produce rebound pockets, unbonded areas, sags and other defects, and overspray contamination can minimize the excellent structural bond that occurs between the Ultraseal membrane surface and shotcrete.

Unlike cast-in-place concrete, the success in applying shotcrete is mostly dependent on the skill and experience of the shotcrete installation crew, especially the nozzleman. Although it may be reassuring to have a properly qualified nozzleman on the project, it cannot be assumed that the quality of in-place shotcrete will be consistently good unless there is continued attention to, and inspection of, the preparation of surfaces to be shotcrete, the position, size and anchorage of steel reinforcement, material quality, mixing of materials, equipment operation and gunning technique, removal of rebound and sand pockets, encapsulation of steel reinforcement, and proper curing.

Furthermore, even properly applied shotcrete is more likely to develop shrinkage cracks than cast-in-place concrete during curing due to the lower water to cement ratio, and the lack of actual field practice of moisture curing the shotcrete for several days as recommended in American Concrete Institute (ACI) 506.2-95.

To address the difficult conditions of waterproofing shotcrete, CETCO has developed special product installation guidelines and drafted specification coordination directives for design professionals to consider when specifying the Ultraseal System to waterproof below-grade, blind-side shotcrete foundations.

SPECIFICATION COORDINATION

Section 071700 defines the requirements for the Ultraseal waterproofing system that includes an initial course of Cortex installed over the shoring wall. Most projects require coordination with several other Sections of the Project Specifications to assure proper waterproofing system installation and to meet the requirements for the issuance of the Manufacturer’s HydroShield Warranty. Following are the typical Specification Sections pertinent to coordinate with Section 071700 that CETCO recommends the project design team review and include the following directives in the project design and specifications:

SECTION 316616 – Special Foundation Walls: Shoring and Cementitious Protection Board

1. Specify that the wood lagging shoring is carried to the lowest level of the waterproofing installation. Require that the lagging boards be tight together and secure enough to receive the shotcrete application against the waterproofing system. Require that voids and cavities exterior of the lagging be filled with engineered soil or cementitious grout.

2. As part of the waterproofing Work, specify that ½” (12 mm) cementitious wall board be installed over the top end of each metal soldier pile prior to installing the waterproofing system. Cementitious wall board will function as a protection course during the excavation and removal of the top several feet of the metal soldier pile and wood lagging as required by local building codes.

SECTION 031500 – Concrete Joint Waterstops

1. HydroShield Warranty requires the application of two (2) strips of Waterstop-RX in all horizontal and vertical shotcrete construction stop joints, require concrete surface to be reasonably smooth such as a float finish or formed surface.

2. HydroShield Warranty requires the application of one (1) strip of Waterstop-RX in all shotcrete lift joints after the joint surface has been cleaned of rebound, poorly bonded material, or any other defect. Secure by pushing Waterstop-RX half-way down into fresh shotcrete.  For shotcrete surfaces specified to be very rough to enhance interlocking with the succeeding shotcrete placement, require that a 1-1/2” (38mm) wide strip of flat surface be tooled or formed into the shotcrete surface to facilitate proper installation of the waterstop. Maintain a 3” (75mm) minimum embedment depth to exterior face of concrete.

3. HydroShield Warranty requires the application of one (1) strip of Waterstop-RX around all mechanical penetrations extending through the shotcrete foundation.

4. HydroShield Warranty requires the application of one (1) strip of Waterstop-RX around all steel reinforcement anchorage.

5. Waterstop-RX is not designed for use in expansion joints. Expansion joints should be sealed with proper expansion joint sealant product by Others.

SECTION 033000 – Cast-in-Place Columns and Pilasters

1. It is extremely difficult to properly apply and consolidate shotcrete behind heavy or closely spaced steel reinforcement. Thereby, HydroShield warranty coverage requires that all heavily reinforced columns and pilasters integrated with or attached to the structural shotcrete foundation wall be formed and cast-in-place.

2. Concrete work should use conventional cast in place forms that produce a smooth surface. Do not use stay-in place concrete forming; use removable forming products only.

SECTION 033700 – Wet Mix Shotcrete / Pneumatically-Placed Concrete

It is important that all the elements which will aid in providing a well designed and correctly executed shotcrete job be written into the specification. Specification should explicitly detail type of shotcrete process (wet mix only), contractor and nozzleman experience and qualifications, materials, design mix, admixtures, acceptance/rejection criteria, quality and method of substrate preparation, steel reinforcing details and anchorage, construction joints, finish, curing procedure, and testing requirements.

1. Specify that wet mix shotcrete walls be placed in strict accordance with ACI 506.2-95, which includes, but not limited to, gunning all walls from the bottom up to their full design thickness in a single application, minimizing the lift height, dampening absorptive substrates before placing shotcrete, removing rebound and sand pockets, properly encasing steel reinforcement, and properly curing the shotcrete installation.

2. Specify a shotcrete subcontractor qualification submittal. Require the shotcrete subcontractor to have a minimum of three (3) years successful experience in structural shotcrete work of similar scope, wet mix type, and project size.

3. Specify a shotcrete crew qualification submittal. Require shotcrete subcontractor to submit written evidence giving qualifications and experience of foreman, delivery equipment operator, nozzle helper (rebound cleaner), and nozzleman certifying that each has experience with the specified shotcrete mix type and the application technique required for the Work. Require that the nozzleman be ACI 506.3R-91 certified or other equivalent certification.

4. Specify Quality Assurance panel mock-up test conducted with the waterproofing applied to the substrate. Cores should be taken of the mock-up and analyzed to ensure that the shotcrete conforms to Core Grade 1 or 2 as defined in ACI 506.2-95 Section 1.7.

A. Construct minimum 8 ft. by 8 ft. test panel using the same equipment, materials, and mix proportions, typical reinforcement, waterproofing membrane system substrate proposed for the Project. Conduct test utilizing each shooting position expected in the Work.

B. Conduct panel test where two lifts of shotcrete are applied.

C. Three (3) days after shotcrete is placed, a minimum of six 4-inch diameter cores through the test panel shall be taken by the Owner’s testing agency. The cores shall cut near the rebar for visual inspection to determine shotcrete core grade of Grade 1 or Grade 2 as defined in ACI 506.2-95, Section 1.7. If the shotcrete core grade is worse than a Grade 2, the Quality Assurance Manager should require another mock-up test until satisfactory results are achieved.

D. Application of shotcrete in the Work shall not proceed until the test panels have been inspected, cored, tested, and approved.

5. Specify as part of the shotcrete Work, the installation of temporary protective sheeting (min. 18” (450 mm)) over adjacent substrate areas, including above shotcrete lift lines during application, to provide protection from shotcrete overspray contamination. It is extremely important to keep the overspray from contaminating (coating) the surface of the Ultraseal. Protective sheeting should be employed above and aside all known shotcrete lift stops, as well as, horizontal and vertical construction stops. Protective sheeting must be removed prior to application of succeeding shotcrete lift or construction area. Specify any rebound or overspray from previously applied area must be removed prior to succeeding shotcrete placement. Protective sheeting materials include, but may not be limited too, 6-mil visqueen, geotextiles, felt, and construction paper.

6. Specify that the wet mix shotcrete walls should be gunned to their full design thickness in a single application and not gunned in layers, thereby reducing the possibility of cold joints and laminations. Where a finer interior finish is desired a thin “flash finish” coat may be applied.  ACI 506R Section 8.6.2 provides guidance for finish coats.

7. Specify the maximum shotcrete lift height and the minimum interval cure time between succeeding shotcrete lift. Specify that the shotcrete lift joints not match the Ultraseal membrane overlap edges. Experience has shown to limit the practical shotcrete lift heights to less than 4’ (1.2 m) and require sufficient time between lifts to allow the applied shotcrete to set.

8. Specify as part of the steel reinforcement Work, rebar anchorage shall be “all-thread or threaded rod” with a 1” (25 mm) fender washer and wing nut assembly to compress and hold Waterstop-RX around outer end of rod against the waterproofing membrane.

9. Require that expanded metal stay-in-place forming not be used to form shotcrete construction stops. Stay-in-place forming can be an unstable substrate to shoot shotcrete against, thus creating voids or poor consolidation. Use solid removable wood or metal forms to provide stable form edge for shotcrete construction stops.

10. Specify as part of the shotcrete Work, the installation of two Waterstop-RX strips at all construction cold joints regardless of whether the joint will encounter hydrostatic or non-hydrostatic conditions. Applicable construction cold joints include the shotcrete wall to slab/footing; vertical formed work edge joints; shotcrete to cast-in-place columns; and daily shotcrete lift joint stops.

11. Specify as part of the shotcrete Work, the installation of one Waterstop-RX strip into each shotcrete lift joint, regardless of whether the lift joint is considered a cold joint or not; or whether the wall will encounter hydrostatic or non-hydrostatic conditions.

12. Require that shotcrete operations should be suspended during high winds, rain, or near freezing temperatures.

13. Require placement of wet mix shotcrete first in corners, recesses, and other areas where rebound or overspray cannot escape or be removed easily.

14. Specify that the Owner shall hire an independent, third party inspection service to monitor the waterproofing and shotcrete installation to ensure that both the waterproofing and shotcrete are being applied as specified and administer a shotcrete quality control/quality assurance testing program.

## HydroShield Warranty Requirements for Shotcrete Property Line Foundations Under Non-Hydrostatic Conditions

The specification coordination directives and Section 071700 Guide Specification herein provide the construction documents framework for a successful Ultraseal waterproofing system application with wet mix shotcrete foundation walls planned for hydrostatic conditions. All projects that intend to apply for HydroShield Warranty covering both the material and labor must meet the following:

1.) Utilize the directives and guide specification herein as a basis of design and product application.

2.) CETCO Approved Applicator must install the waterproofing and Aquadrain drainage system.

3.) Aquadrain system shall be connected to an operative water discharge system.

4.) Single strip of Waterstop-RX shall be installed in all shotcrete lift joints.

5.) Two strips of Waterstop-RX shall be installed in all shotcrete construction joints.

6.) Require Owner’s independent inspector to inspect the waterproofing installation just prior to shotcrete application to ensure that the waterproofing has not been damaged during steel reinforcement and anchorage installation.

7.) Concrete work shall use conventional cast-in-place forms that produce a smooth surface. Do not use stay-in place

concrete forming; use removable forming products only.

If you have any questions about these specification coordination directives, please contact your local CETCO authorized sales representative or CETCO Regional Manager.

This guide specification was issued June 2010 and may be superseded without notice at any time. Therefore, please confirm that this specification is still current and has not been superseded by checking at www.cetco.com or by calling 1-800-527-9948-.

SHOTCRETE CONSTRUCTION SPECIFICATION

This guide specification has been prepared according to the principles established in the Manual of Practice published by the Construction Specification Institute and is intended for use with below-grade structural shotcrete foundation walls. This specification is not intended for use with masonry block or precast concrete construction. Contact CETCO regarding installation and application guidelines for Ultraseal Waterproofing System when used with masonry block or precast concrete construction. CETCO, Building Materials Group – 1- 800-527-9948.

This master guide specification contains work sections in PART 3 – Execution – pertaining to both zero-lot line construction and backfilled foundation wall construction. Therefore, PART 3 should be edited to only include work sections specific to the job site conditions required on the project.

SECTION 071700 - JUNE 2010 (Supersedes All Previous Versions)

ULTRASEAL ®  MASTER GUIDELINE SPECIFICATION FOR

SHOTCRETE PROPERTY LINE FOUNDATION WALLS UNDER

NON-HYDROSTATIC CONDITIONS

PART 1 - GENERAL

1.01	 RELATED DOCUMENTS

A.  	All of the Contract Documents, including General and Supplementary Conditions, and Division 1 General requirements, apply to the work of this section.

B. 	Reference Documents

1. ACI 506R – Guide to Shotcrete

2. ACI 506.2-95 – Specification for Shotcrete

3. ACI 506.3R-91 – Guide to Certification of Shotcrete Nozzleman

1.02  	WORK SUMMARY

A. 	The work of this section includes, but is not limited to the furnishing and installing the following materials, per project specifications and drawings, or as directed by waterproofing manufacturer:

1. Ultraseal SP and Ultraseal BT waterproofing membrane with all applicable accessory products.

2. Aquadrain 15XP sheet drainage and Aquadrain 100BD base drain

1.03	RELATED SECTIONS

A.	Other specification Sections which directly relate to the work of this section include, but are not limited to, the following:

1. Division 2: Subsurface and Geotechnical Investigations

2. Division 3: Waterstops

3. Division 5: Expansion Joint Products

4. Division 7: Joint Treatment/ Sealants, Flashing and sheet metal, and Insulation

5. Division 22: Deck and Floor Drains and other Mechanical Penetrations

6. Division 26: Conduit and other Electrical Penetrations

7. Division 31: Earthwork, Excavation and Fill, Shoring,

8. Division 33: Geocomposite Foundation Drainage

071700 -1

1.04 	SYSTEM DESCRIPTION

A.	Provide Ultraseal membrane waterproofing and Aquadrain drainage system with all applicable accessory products to prevent the passage of liquid water under non-hydrostatic pressure and install without defects, damage or failure.  Waterproofing shall be an active-polymer core technology with all applicable accessory products.

1.05	SUBMITTALS

A.	General: Prepare and submit specified submittals in accordance with "Conditions of the Contract" and Division 1 Submittals Sections.

B.	Product Data: Submit manufacturer’s product data, with complete general and specific installation instructions, recommendations, and limitations.

C.	Product Samples: Submit representative samples of the following for approval:

1. Ultraseal SP and Ultraseal BT waterproofing membrane

2. Aquadrain 15XP drainage composite

D. 	Waterproofing Material and Labor Warranty: At time of bid, submit a sample copy of the Manufacturer’s Waterproofing warranty complete with all coverage’s, limitations, and conditions.

E.	Material Certificates: Submit certificate(s) by manufacturer certifying materials comply with specified performance characteristics and physical requirements. Submit certification that waterproofing system and components, and protection materials are supplied by a single-source manufacturer.

F.	Contractor Certificate: At time of bid, submit written certification that installer has current Approved Applicator status with waterproofing material manufacturer.

1.06 	QUALITY ASSURANCE

A. 	Installer Qualifications: Installing company should have at least three (3) years experience in work of the type required by this section, which can comply with manufacturer's warranty requirements, and is an Approved Applicator as determined by waterproofing system manufacturer.

B.	Manufacturer Qualifications:  Waterproofing and all accessory products shall be provided by a single manufacturer with a minimum of 30 years experience in the direct production and sales of waterproofing systems. Manufacturer shall be capable of providing field service representation during construction, approving an acceptable installer, and recommending appropriate installation methods.

C.	Pre-Installation Conference: A pre-installation conference shall be held prior to commencement of field installation to establish procedures to maintain required working conditions and to coordinate this work with shotcrete installation and adjacent work. Verify that final waterproofing and waterstop details comply with waterproofing manufacturer's current installation requirements and recommendations. Pre-con meeting attendees should include representatives for the owner, architect, inspection firm, general contractor, waterproofing contractor, concrete contractor, excavating/backfill contractor, and mechanical and electrical contractor if work penetrates the waterproofing.

D.	Materials: Obtain waterproofing membranes and accessories from a single manufacturer to assure material compatibility.

071700 -2

E.	Independent Inspection: Owner shall make all arrangements and payments for an independent inspection service to monitor waterproofing material installation compliance with the project contract documents and manufacturer’s published literature and site specific details. Independent Inspection Firm shall be an approved company participating with the waterproofing manufacturer’s Certified Inspection Program. Inspection service shall produce reports and digital photographs documenting each inspection. Reports shall be made available to the Contractor, waterproofing installer, waterproofing material manufacturer, and Architect. Inspections should include substrate examination, beginning of waterproofing installation, periodic intervals, and final inspection prior to shotcrete or backfill placement against the waterproofing.

F.	Water Sample Test: Waterproofing contractor shall supply project site water sample to waterproofing membrane manufacturer for analysis. Manufacturer shall conduct test free of charge. Contractor is responsible for collection and shipment of 64-fluid ounces (2-liters) of actual site water. Water should be shipped in uncontaminated, sealed plastic container to: CETCO, 2870 Forbs Ave., Hoffman Estataes, IL  60192, Attn: BMG Field Services. Also provide project name, city and state along with return address to forward test results.

1.07	PRODUCT DELIVERY, STORAGE AND HANDLING

A.	Delivery and Handling: Deliver materials in factory sealed and labeled packaging. Sequence deliveries to avoid delays, while minimizing on-site storage. Handle and store following manufacturer's instructions, recommendations and material safety data sheets. Protect from construction operation related damage, as well as, damage from weather, excessive temperatures and prolonged sunlight. Remove damaged material from site and dispose of in accordance with applicable regulations.

B. 	Storage: Do not double-stack pallets during shipping or storage. Protect waterproofing materials from moisture, excessive temperatures and sources of ignition. Provide cover, top and all sides, for materials stored on-site, allowing for adequate ventilation.

1.08	PROJECT CONDITIONS

A.	Substrate Condition: Proceed with work only when substrate construction and preparation work is complete and in condition to receive waterproofing system. All plumbing, electrical, mechanical and structural items to be under or passing through the waterproofing shall be positively secured in their proper positions prior to waterproofing system installation. Substrate preparation shall be per waterproofing manufacturer’s guidelines..

- Weather Conditions: Perform work only when existing and forecasted weather conditions are within the guidelines established by the manufacturer of the waterproofing materials. Do not apply waterproofing materials into standing or active water, nor over ice or snow. Though exposure to precipitation and ground water seepage typically will not adversely affect Ultraseal, the General Contractor shall maintain site conditions to remove standing water from precipitation or ground water seepage in a timely manner. Should Ultraseal be subjected to prehydration as a result of prolonged immersion, inspection of the material and written acceptance from CETCO is required prior to concrete or backfill placement.

1.09 	WARRANTY

- Warranty eligibility for the project must be validated by Manufacturer,  confirming acceptance of the installation and independent inspection reports are in accordance with the manufacturer’s quality assurance program requirements.

- Waterproofing Material and Labor Warranty: Upon completion and acceptance of the work required by this section, the waterproofing materials manufacturer will provide a written ten (10) year warranty, covering both materials and labor, to the project owner. Issuance of Manufacturer's HydroShield Warranty requires the following: (1) System waterproofing products and drainage composite products shall have been provided by a single manufacturer; (2) Installation of

071700-3

waterproofing products and prefabricated drainage composite by Manufacturer's Approved Applicator in full accordance with manufacturer’s quality assurance program requirements; (3) Installation inspected by Independent Inspection Firm participating with the waterproofing manufacturer’s Certified Inspection Program; (4) In Division 3 work, Waterstop-RX must be installed in all applicable horizontal and vertical cold pour concrete construction joints and lift joints; and around applicable penetrations. Manufacturer's warranty shall be independent from any other warranties made by the Contractor under requirements of the Contract Documents and may run concurrent with the other warranties.

PART 2 - PRODUCTS

2.01 	MANUFACTURER

A.	Provide Ultraseal waterproofing with applicable accessories as manufactured by Colloid Environmental Technologies Company (CETCO), 2870 Forbs Ave., Hoffman Estates, IL  60192. , USA. Toll Free: (800)527-9948; 0r  (847)851-1800; Web-site: http://www.cetco.com/bmg.

2.011	DISTRIBUTOR

Bowman Construction Supply

10801 E. 54th Avenue

Denver, CO 80239

Phone: (303) 696-8960

2.02 	MATERIALS

A.	ULTRASEAL – APC WATERPROOFING MEMBRANE

1. ULTRASEAL BT MEMBRANE: 100-mil (2.3 mm) thick composite membrane consisting of a active-polymer core (APC) integrally bonded to a geomembrane liner using a proprietary mechanical process. ULTRASEAL BT applications include backfilled walls, property line retention walls, and earth covered structures. Roll size: 4′ x 25′ (1.2 x 7.62 m)

1. ULTRASEAL SP MEMBRANE: 200-mil (4.7 mm) thick composite membrane consisting of a active-polymer core (APC) encapsulated by a geotextile and a geomembrane using a proprietary mechanical process. ULTRASEAL SP application -  under structural slabs. Roll size: 4′ x 25′ (1.2 x 7.62 m)

Typical Properties of ULTRASEAL BT Membrane:

| Property | Test Method | Typical Value |
| --- | --- | --- |
| Hydrostatic Head Resistance | ASTM D 5385 mod | 231 Ft. (70 m) |
| Permeability | ASTM D 5084 | <1 x 10-11cm/sec |
| Grab Tensile Strength | ASTM D 4632 | 150 lbs |
| Puncture Resistance | ASTM D 4833 | 70 lbs. |
| Low Temperature Flexibility | ASTM D 1970 | Unaffected at -25F (-32C) |
| Elongation | ASTM D 4632 | 50 % |
| Peel Strength to Concrete | ASTM D 903 MOD | 10 lbs./in |

Typical Properties of ULTRASEAL SP Membrane:

| Property | Test Method | Typical Value |
| --- | --- | --- |
| Hydrostatic Head Resistance | ASTM D 5385 mod | 231 Ft. (70 m) |
| Permeability | ASTM D 5084 | <1 x 10-11cm/sec |
| Grab Tensile Strength | ASTM D 4632 | 300 lbs./in |
| Puncture Resistance | ASTM D 4833 | 130 lbs. |
| Low Temperature Flexibility | ASTM D 1970 | Unaffected at -25F (-32C) |
| Elongation | ASTM D 4632 | 75 % |
| Peel Strength to Concrete | ASTM D 903 MOD | 10 lbs./in |

071700-4

D.	ACCESSORY WATERPROOFING PRODUCTS: All accessory waterproofing materials shall be provided by the waterproofing manufacturer or shall have manufacturer’s written 	approval for substitution.

1. Bentoseal:  Trowel grade detailing mastic.

2. Hydrobar Tubes: 2” (50 mm) diameter x 2’ (60 cm) long, water soluble tube container filled with active granular material

3. Waterstoppage:  50 lbs. (22.7 kg) bag of active granular material.

4. Akwaswell: 10.5 oz (310 ml) tubes of hydrophilic rubber caulk

5. Termination Bar: Min. 1/8” thick x 1” (25 mm) wide stainless steel or aluminum bar with pre-punched holes on 6” (150 mm) centering for fastening.

6. Cementitious Board: ½” thick cementitious wall board for protection of waterproofing during the removal of metal soldier pile cap and top lagging boards.

7. CETCO Seamtape: sealant tape for applicable membrane laps

8. Cortex – A low permeable geotextile waterproofing material that utilizes Active Polymer Core (APC) technology.

9. CETSEAL – single-component polyether general sealant and adhesive

10. TB-Boots – pre-formed, single piece thermoplastic cover for tie-back heads and soil nails. Three sizes available: TB-6SN, TB-8, and TB-10.

11. GF-40SA –flashing membrane used for grade and thru-wall detailing.

E.	SHEET AND BASE DRAINAGE COMPOSITE

1. Aquadrain 15XP – 4-ft x 52-ft roll of three dimensional polypropylene drainage core with a geotextile adhered to one side to allow water passage while restricting soil particles. Composite includes a thin polyethylene sheet on the back of the drainage core. Compressive strength: 15,000 psf (718 kPa); Water Flow Rate, 20 gpm/ft (251 l/m/m); Thickness, 7/16” (11 mm).

2. Aquadrain 100BD – 1” thick x 12” high roll of three dimensional drainage core with a geotextile adhered to both sides to allow water passage while restricting soil particles. Compressive strength: 10,000 psf (457 kPa); Water Flow Rate, 97 gpm/ft (1,197 l/m/m); Thickness, 1” (25 mm).

PART 3 - EXECUTION

A.	Comply with manufacturer's product data, including product application and installation instructions, as well as, manufacturer's shipping and storage recommendations.

3.01 	SUBSTRATE INSPECTION AND CONDITIONS

- The installer, with the Owner’s Independent Inspector present, shall examine conditions of substrates and other conditions under which this section work is to be performed and notify the contractor, in writing, of circumstances detrimental to the proper completion of the work. Do not

proceed with work until unsatisfactory conditions are corrected and are acceptable for compliance with manufacturer's warranty requirements. General substrate conditions acceptable for the waterproofing installation are listed below. For conditions not covered in this Section, contact the waterproofing manufacturer for guidance.

B.	WORKING MUD SLAB: Working concrete mud slabs should have a float finish to provide a planar surface; without sharp angular depressions, voids or raised features.

C..	COMPACTED SOIL OR GRAVEL SUB-GRADE: Sub-grade shall be compacted to a minimum Modified Proctor compaction of 85% or greater as specified by civil/geotechnical engineer. The finished sub-grade surface shall be well-leveled, uniform, free of debris and standing water or ice. Aggregate sub-grades shall consist of ¾” (19 mm) stone or smaller and rolled flat, free from any protruding sharp edges. If substrate consists of large aggregate, place a high-strength geotextile layer over the aggregate and then provide several inches of compacted soil or sand for uniform support and containment of waterproofing sheets. Specific sub-grade preparation shall be approved by the project’s civil or geotechnical engineer.

071700-5

D.	WOOD TIMBER SHORING: Wood lagging shoring should extend to the lowest level of the waterproofing installation with any voids or cavities exterior of the lagging timbers filled with compacted soil or cementitious grout. Interior surface of lagging boards should be planar and tight together with gaps less than 1” (25 mm). Gaps in excess of 1” should be filled with cementitious grout, compacted soil, wood, extruded polystyrene (20 psi min.) or CETCO approved polyurethane spray foam. Do not use plywood or other surface treatment over large lagging gaps that leave the cavity void. In areas where lagging gaps are 2-1/2” (63 mm) or less, Aquadrain sheet drainage can be installed over lagging to provide uniform surface to mount the waterproofing without requirement of filling gaps. All lagging board nails and other mechanical projections shall be removed or pounded flush. Install a protection material over all soldier piles with raised lagging hanger bolts, form tie rods, or other irregular surface; protection material should extend a minimum 6” (150 mm) to both sides of the steel piling.

E.  	CUT ROCK FACE OR AUGER CAST CAISSON SHORING WALLS: Interior surface of cut rock and concrete auger pile retention walls should be planar without irregular surface conditions, voids, and sharp transitions that would leave a void space to the outside of the drainage and waterproofing installation. Irregular rock, void pockets, cracks, sharp concave transitions should be completely filled or smoothed with cementitious grout, shotcrete, or other approved solid material.

F.	MECHANICAL OR OTHER PENETRATIONS: Mechanical, structural, or architectural materials that will pass through the plane of the waterproofing membrane shall be properly installed and secured in their final position prior to the installation of the waterproofing system.

G.	CONCRETE:  Concrete to be waterproofed shall be properly placed and consolidated. Reinforced structural slabs should be a minimum of 6" (150 mm) thick when placed on a working mud slab. Reinforced concrete slab(s) on compacted grade shall be a minimum of 4” (100 mm) thick. When hydrostatic conditions exist, install Ultraseal SP under all footings, elevator pits and grade beams. Cast-in-place concrete to receive waterproofing shall be of sound structural grade with a smooth finish, free of debris, oil, grease, laitance, dirt, dust, or other foreign matter which will impair the performance of the waterproofing and drainage system and which do not comply with manufacturer's warranty requirements. Ultraseal BT can be installed on green structural concrete as soon as the forms are removed provided the contractor gains written approval from project structural engineer listing any site specific concrete curing time requirement. Do not apply Ultraseal waterproofing directly over lightweight insulating concrete, wood, or steel decking.

      - Remove dirt, debris, oil, grease, cement laitance, or other foreign matter which will impair or negatively affect the performance of the waterproofing and drainage system.

      - Protect adjacent work areas and finished surfaces from damage or contamination from waterproofing products during installation operations.

      - Form fins, ridges, ponding ridges and other protrusions should be level and smooth with concrete surface.

      - Honeycombing, aggregate pockets, tie-rod holes and other voids shall be completely filled with non-shrink cementitious grout and level with monolithic concrete surface.

5.	Concrete work shall use conventional cast-in-place forms that produce a smooth surface. Do not use stay-in place concrete forming; use removable forming products only.

6.	All heavily reinforced columns and pilasters integrated with or attached to the structural shotcrete foundation wall be formed and cast-in-place.

- 7.	Horizontal deck or roof concrete surfaces should be sloped for positive drainage to the deck drains or the perimeter edges. Deck drain positions should be designed with an appropriate sump depression surrounding the drain.

071700-6

- 8. 	Precast concrete deck units shall be installed and secured to structural supports in accordance with the concrete panel manufacturer’s requirements and industry practice. All joints between precast units shall be completely grouted and flush with deck. Any differential in elevation between precast units shall be feathered for a smooth transition.

- 9.	All expansion joints should receive applicable expansion joint sealant product manufactured by others prior to the installation of the Ultraseal Waterproofing System. Expansion joint material is the primary seal at the expansion joint and the expansion joint material manufacturer is responsible for water tightness of the joint.

NOTE: Related work to be completed under Division 3. Waterstop-RX shall be installed in all applicable vertical and horizontal concrete construction cold pour joints and around applicable penetrations, structural members, and tie-rod form holes that extend through the wall. Refer to Waterstop-RX Product Manual for further installation procedures and guidelines.

3.02 	SURFACE PREPARATION

A.	Remove dirt, debris, oil, grease, cement laitance, or other foreign matter which will impair or negatively affect the performance of the waterproofing and drainage system.

B.	Protect adjacent work areas and finish surfaces from damage or contamination from waterproofing products during installation operations.

3.03 	GENERAL INSTALLATION GUIDELINES

A. 	Underslab: Install Ultraseal SP Waterproofing System with the tan geotextile liner facing the concrete to be waterproofed in both horizontal and vertical applications. Concrete should be placed against tan geotextile side of membrane.

B.	Property Line Shoring Walls:  Install Ultraseal BT with minimum 6” (150 mm) sheet edge overlaps fastened with both washer-head fasteners placed maximum 24” (600 mm) on center and pneumatic staples placed 6” (150 mm) on center. Install pneumatic staples within 1” (25 mm) of sheet edge to tightly secure entire overlap assembly to the shoring wall.

C.	Secure center line of Ultraseal BT sheets to shoring wall with pneumatic staples or washer-head fasteners as required to hold membrane tight against shoring wall.

D.	Expansion Joints: Ultraseal waterproofing is not an expansion joint filler or sealant, but may be used as an expansion joint cover over properly installed expansion joint material placed during substrate preparation. To use Ultraseal as an expansion joint cover, trowel 1/8" (3 mm) thick, 6" (150 mm) wide layer of Bentoseal centered over expansion joint. Install a 24" (60 cm) wide strip of Ultraseal BT centered over the expansion joint. Then place the main course of Ultraseal BT.

3.04	AQUADRAIN DRAINAGE COMPOSITE

A.	At the base of the lagging wall, install Aquadrain 100BD base-drain horizontally oriented with the open core edge up and the 2” (50 mm) fabric flap side away from the lagging wall. Secure the bottom edge of 100BD to the lagging wall with washer-head fasteners every few feet. Use couplers and corner fittings, as required, to form a continuous 100BD installation. Install discharge outlet fittings to connect with discharge pipes as required for the project.

071700-7

B.	Install the bottom course of Aquadrain 15XP sheet drainage horizontally oriented (geotextile side against the lagging wall) with the 15XP bottom edge fabric flap tucked behind the top edge of the 100BD against the lagging to prevent the passage of soil into the core at the connection. Bottom edge of 15XP core should be in contact with open top core edge of 100BD. Place the 2” (50 mm) fabric flap of the 100BD over the back of the 15XP core and secure it with CETCO Seamtape. Secure the top edge of 100BD to the lagging wall with washer-head fasteners 24” (600 mm) on center.

C. 	Install subsequent rolls of Aquadrain 15XP sheet drainage to within 12” (300 mm) of finished grade or as shown on the project drawings. Tightly abut adjoining sheet drain core edges and tuck the extra fabric flaps behind the adjacent roll edge to keep soil from entering the sheet drain. Secure sheet drain to lagging wall with washer-head fasteners.

D.	Cementitious Board: Prior to installing Aquadrain to finished grade elevation, install ½" (12 mm) thick cementitious wall board centered over steel soldier pile from finished grade elevation to specified depth that the top of steel soldier pile and wood lagging will be removed. Cementitious wall board will protect waterproofing when top of soldier pile is excavated and removed. Remove cementitious wall board with removal of metal soldier pile head and lagging.

3.05	SLAB EDGE TO LAGGING WALL ULTRASEAL BT TRANSITION COURSE

A.	Install Ultraseal BT base corner transition sheet horizontally oriented (white poly side against the shoring wall; APC side facing installer) with the bottom edge extending out onto the horizontal substrate a minimum 12" (300 mm) and the top edge of the sheet extending a minimum 12" (300 mm) above the finished slab elevation. Secure Ultraseal BT sheet to lagging wall through Aquadrain sheet with washer-head fasteners maximum 24" (600 mm) on center. Overlap edges of adjacent Ultraseal BT sheets a minimum 6" (150 mm).

B.	If the slab thickness is greater than 24" (600 mm), install a second full sheet or cut strip of Ultraseal BT on the lagging wall to meet the 12" (300 mm) requirement above of the top slab elevation. Overlap top edge of previous sheet and edges of adjacent sheets a minimum 6" (150 mm).

3.06	ULTRASEAL BT COURSE ON LAGGING SHORING – NON-HYDROSTATIC CONDITION

A.	Starting at the base corner, install course of Ultraseal BT horizontally oriented (white gemembrane liner side against lagging; APC side facing installer) to lagging wall over the Ultraseal BT transition course previously installed in Section 3.05 Work. Secure sheet edges to shoring with both washer-head fasteners placed maximum 24" (600 mm) on center and pneumatic staples placed 6" (150 mm) on center within 1" (25 mm) of sheet edge.

B.	Secure center line of Ultraseal BT sheets to shoring wall with pneumatic staples or washer-head fasteners as required to secure membrane tight against shoring wall.

C.	After the bottom horizontal course, Ultraseal BT sheets can be installed either vertically or horizontally oriented. Continue Ultraseal BT installation up wall to finished grade elevation detail, staggering all sheet roll ends of adjacent courses a minimum 24" (600 mm). Do not allow horizontal Ultraseal BT overlap joints to run at same elevation as the shotcrete lift joints. Plan by chalk lining the location of shotcrete lift joint lines. Overlap adjacent Ultraseal BT sheet edges a minimum 6” (150 mm).

D.	Tie-Back Heads: For all tie-back heads and soil nails, install waterproofing system with applicable size TB-Boot in accordance with manufacturer’s detail for specific project condition(s). For irregular shoring wall conditions at tie-backs or oversize tie-back heads consult manufacturer for alternate detail for specific project condition(s).

071700-8

E.	Penetrations: For all mechanical, structural and other penetrations install waterproofing system per manufacturer’s detail for specific project condition(s).

F.	Rebar Anchorage: Install Bentoseal ¾" (18 mm) thick around all rebar anchorage penetrating Ultraseal BT. Then install a length of Waterstop-RX around the shaft of the rebar anchorage tight against the Bentoseal.

G.	Inspect finished Ultraseal BT installation and repair any damaged material prior to shotcrete placement. Assure Ultraseal BT overlap is not separated during shotcrete placement.

3.07	UNDER SLAB INSTALLATION

A.	Install Ultraseal SP under all footings, elevator pits and grade beams when hydrostatic conditions exists or are anticipated per the historical high ground water elevation reported in the project’s geotechnical documents.

B.	Install Ultraseal SP membrane under slab extending to base of shoring wall (tan geotextile side up facing installer), fully overlapping the 12” (300 mm) horizontal tail of the Ultraseal BT corner transition sheet installed per Section 3.04 Work. Secure corner edge of membrane with washer-head fasteners or pneumatic staples 12” (300 mm) on center.

C. 	Place Ultraseal SP directly on properly prepared substrate (tan geotextile side up facing installer) with adjoining edges overlapped a minimum of 4” (100 mm). Stagger sheet end seams a minimum of 24” (60 cm). Mechanically fasten or staple Ultraseal SP as required to prevent movement from construction operations or concrete placement. When the slab is poured in sections, extend Ultraseal SP a minimum 12" (300 mm) beyond the slab edge to enable proper overlapping.

D.	Install waterproofing system at all grade beams, pile caps, and other detail areas in accordance with manufacturer’s detail for specific project condition(s).

E. 	Slab Penetrations: For all pipe, rebar, structural or other penetrations install waterproofing system in accordance with manufacturer’s standard detail for specific project condition(s).

F. 	Inspect finished Ultraseal SP installation and repair any damaged material prior to concrete slab placement. Assure that Ultraseal SP is not displaced during concrete placement.

NOTE: Related work to be completed under Division 3. Waterstop-RX shall be installed in all slab joints, around applicable slab penetrations and structural members. Refer to Waterstop-RX Product Manual for further installation procedures and guidelines.

3.08	EXCAVATION, GRADE TERMINATION AND BACKFILL

A.	Coordinate with excavation and backfill operations conducted under Division 31 Work to remove the top few wood lagging timbers and top end of the metal soldier piles per local building code or project requirements. Identify and repair any waterproofing and drainage sheet damaged by excavation and removal of soldier pile heads and lagging. Where excavated, fasten all exposed Ultraseal BT overlap seams maximum 24” (600mm) on center and apply CETCO SeamTape centered along overlap seams.

B.	Terminate Ultraseal BT membrane 12” (300 mm) below finished grade elevation secured with washer-head fasteners maximum 12” (300 mm) on center to exterior surface of concrete wall. Per manufacturer’s detail for specific project condition(s), install GS-40SA grade flashing to primed concrete substrate with bottom edge overlapping top edge of Ultraseal BT membrane minimum 4” (100 mm). Overlap all roll ends a minimum 4” (100 mm) to form a continuous flashing. Height of flashing shall be per project details and specifications. Install a rigid termination bar along the top edge of GF-40SA; fastened maximum 12” (300 mm) on center. Complete grade termination detail with tooled bead of CETSEAL along the top edge, at all penetrations through the flashing, and all exposed overlap seams.

071700-9

C. 	Backfill shall be placed and compacted to minimum 85% Modified Proctor density promptly after waterproofing has been installed. Closely coordinate with contractor responsible for Backfill work by informing them each time a waterproofed area is ready for backfill. Backfill shall consist of compactable soil or angular aggregate (3/4” or less) free of debris, sharp objects, and stones larger than ¾” (18 mm). Care should be used during backfill operation to avoid damage to the waterproofing system. If damage occurs, cease backfilling and report damage. Damaged waterproofing must be repaired per manufacturer’s guidelines.

3.09	CLEAN UP

- Clean areas where adjacent finished surfaces are soiled by Work of this Section. Remove all tools, equipment and remaining product on-site. Dispose of section work debris and damaged product following all applicable regulations.

End of Section 071700