CCW-MIRAPLY-H

MATERIAL CERTIFICATION

This is to certify that CCW MiraPLY-H is a horizontal grade, self-adhering membrane that is comprised of a tough, durable and flexible TPO backing with a butyl alloy adhesive designed for blindside waterproofing in below-grade construction.  CCW MiraPLY is manufactured in the USA.

CCW manufactures CCW MiraPLY-H membrane to comply with the following ASTM typical property values and meets the specification requirements:

| CCW-MiraPLY-H-Property | Test Method | Unit | Typical Value* |
| --- | --- | --- | --- |
| TPO |  | mils (mm) | 45 (1.14) |
| Butyl Alloy |  | mils (mm) | 25 (.64) |
| Thickness | ASTM D 1970 | mils (mm) | 70 (1.78) |
| Water Vapor Transmission (Water Method) – With Seams | ASTM E 96 | perms | 0.090 |
| Tensile Strength | ASTM D 882 | psi | 1,500 |
| 300% Modulus | ASTM D 412 | psi | 1,000 |
| Lap Seam 90º T-Peel | ASTM D 1876 | pli. | 15.0 |
| Elongation @ Break @ 23ºC (Die C) | ASTM D 412 | % | 325 |
| Flexibility Temperature @ -29ºC (-20ºF) | ASTM D 1970 | Pass/Fail | No Cracking @ -29ºC (-20ºF) - Pass |
| Hydrostatic Pressure Resistance | ASTM D 5385 | ft. | >231ft. (100 psi) |
| Peel Strength Over Poured Concrete (tested w/2” strips) | ASTM D 903 | pli. | >5.0 |
| Puncture Resistance Load at Puncture | ASTM E 154 | lb. | 375 |
| Tear Strength | ASTM D 624 | psi | 1,000 |
| Soil Decay Testing – E 96 Permeance | ASTM E 154 | - | Pass |
| Soil Decay Testing – Weight Loss | ASTM D 154 |  | Pass |
| Lateral Water Migration Resistance | ASTM D 5385 modified |  | Pass at 100 psi (231 ft.) of hydrostatic pressure |

Rev. January 5, 2016