Spec Note: This specification includes materials and installation procedures for Air-Bloc 32MR, an elastomeric non permeable, mold resistive air barrier membrane meeting the requirements of the Massachusetts Energy Code for the building envelope.  Air-Bloc 32MR is used in cavity wall construction to provide an air/vapor and rain barrier membrane.  This specification should be adapted to suit the requirements of individual projects. It is prepared in CSI three part format and should be included as a separate section under Division 7 - Thermal and Moisture Protection.

PART 1 - GENERAL

1.01	GENERAL REQUIREMENTS

A.	General Conditions, Supplementary Conditions, Instructions to Bidders and Division One General Requirements shall be read in conjunction with and govern this section.

B.	This Specification shall be read as a whole by all parties concerned.  Each Section may contain more or less than the complete Work of any trade.  The Contractor is solely responsible to make clear to the Subcontractors the extent of their Work.

1.02	DESCRIPTION

A.	Supply labor, materials and equipment to complete the Work as shown on the Drawings and as specified herein to bridge and seal the following air leakage pathways and gaps:

1.	Connections of the walls to the roof air barrier.

2.	Connections of the walls to the foundations.

3.	Seismic and expansion joints.

4.	Openings and penetrations of window and door frames, store front, curtain wall.

5.	Piping, conduit, duct and similar penetrations.

6.	Masonry ties, screws, bolts and similar penetrations.

7.	All other air leakage pathways in the building envelope.

- Materials and installation methods of the primary air/vapor barrier membrane system and accessories.

- Materials and installation methods of through-wall flashing membranes.

1.03	RELATED SECTIONS

- Concrete	Section [03 XX XX]

- Masonry	Section [04 XX XX]

- Gypsum Sheathing	Section [06 XX XX]

- Plywood Sheathing	Section [06 XX XX]

- Insulation	Section [07 XX XX]

- Roofing	Section [07 XX XX]

- Wall Panels	Section [07 XX XX]

- Flashing	Section [07 XX XX]

- Sealants	Section [07 XX XX]

- Door Frames	Section [08 XX XX]

- Window Frames	Section [08 XX XX]

1.04	REFERENCES

A.	The following standards are applicable to this section:

- ASTM E 2178: Standard Test Method for Air Permeance of Building Materials.

- ASTM E 283: Standard Test Method for Determining the Rate of Air Leakage Through Exterior Windows, Curtain Walls, and Doors Under Specified Pressure Differences Across the Specimen.

- E 1677 Specification for Air Retarder (AR) Material or System for Low-Rise Framed Building Walls

- ASTM E 330: Standard Test Method for Structural Performance of Exterior Windows, Curtain Walls, and Doors by Uniform Static Air Pressure Difference.

- ASTM E 331: Standard Test Method for Water Penetration of Exterior Windows, Skylights, Doors, and Curtain Walls by Uniform Static Air Pressure Difference

5.	ASTM E 96: Water Vapor Transmission of Materials.

6.	CGSB 37-GP-56M: Membrane, Modified, Bituminous, Prefabricated, and Reinforced.

7.	AMMA 2400: Standard Practice for Installation of Windows with a Mounting Flange in Stud Frame Construction.

8.	ASTM E 2112:  Standard Practice for Installation of Exterior Windows, Doors and Skylights.

9.	ASTM D 5590: Standard Test Method for Determining the Resistance of Paint Films and Related Coatings to Fungal Defacement by Accelerated Four-Week Agar Plate Assay

1.05	SUBMITTALS

A.	Submit documentation from an approved independent testing laboratory certifying the air leakage and vapor permeance rates of the air barrier membranes, including primary membrane and transition sheets, exceed the requirements of the Massachusetts Energy Code and in accordance with ASTM E 2178.

1.	Test report submittals shall include test results on porous substrate and include sustained wind load and gust load air leakage results.

B.	Submit manufacturers’ current product data sheets for the air barrier membrane system.

1.06	QUALITY ASSURANCE

A.	Submit document stating the applicator of the primary air/vapor barrier membranes specified in this section is qualified by the manufacturer as suitable for the execution of the Work.

B.	Perform Work in accordance with manufacturer’s written instructions and this specification.

C.	Maintain one copy of manufacturer’s written instructions on site.

D.	Allow access to Work site by the air barrier membrane manufacturer’s representative.

E.	Components used shall be sourced from one manufacturer, including sheet membrane, air barrier sealants, primers, mastics, and adhesives.

- Single-Source Responsibility:

1.	Obtain air barrier materials from a single manufacturer regularly engaged in manufacturing the product.

2.	Provide products which comply with all federal, state and local regulations controlling use of volatile organic compounds (VOCs).

1.07	MOCK-UP

A.	Construct mock-up in accordance with Section 01 43 39 – Mock-ups.

B.	Provide mock-up of air/vapor barrier materials under provisions of Section 01 33 23 - Shop Drawings, Product Data and Samples.

C.	Where directed by [engineer] [architect] [consultant], construct typical exterior wall panel, 6 foot long by 6 foot wide, incorporating substrate, window frame, attachment of insulation and showing air barrier membrane application details.

D.	Allow 48 hours for inspection of mock-up by [engineer] [architect] [consultant] before proceeding with air barrier work. Mock-up may remain as part of the Work.

E.	Test mock-up for air and water infiltration to conform with Section 01400 - Quality Control, in accordance with ASTM E 783 and ASTM E1105.

1.08	PRE-INSTALLATION CONFERENCE

A.	Contractor shall convene [one] week prior to commencing Work of this section, under provisions of Section 01 31 19 – Project Meetings.

B.	Ensure all contractors responsible for creating a continuous plane of air tightness are present.

1.09	DELIVERY, STORAGE AND HANDLING

A.	Refer to current Product MSDS for proper storage and handling.

B.	Deliver materials to the job site in undamaged and original packaging indicating the name of the manufacturer and product.

C.	Store role materials on end in original packaging.  Protect rolls from direct sunlight until ready for use.

D.	Store air barrier membranes, adhesives and primers at temperatures of 40 degrees F and rising.

E.	Keep solvent away from open flame or excessive heat.

F.	Wasted Management and Disposal

- Separate and recycle waste materials in accordance with Section [01355 - Waste Management and Disposal], and with the Waste Reduction Work Plan

G.	Contractor to verify compliance for Volatile Organic Compounds (VOC) limitations of products to comply with all federal, state and local regulations controlling use of volatile organic compounds (VOCs).

1.10	COORDINATION

- Ensure continuity of the air seal throughout the scope of this section.

1.11	ALTERNATES

- Submit request for alternates in accordance with Section 01 25 00 – Substitution Procedures.

- Submit requests for alternates a minimum of ten (10) working days prior to bid date

- Alternate submission to include:

1.	Evidence that alternate materials meet or exceed performance characteristics of Product requirements as well as documentation from an approved independent testing laboratory certifying the air leakage rates and vapor permeance rates of the air barrier membranes, including primary membrane and transition sheets, exceed the requirements of the Massachusetts Energy Code and in accordance with ASTM E2357, and has 0 rating - no fungal growth as tested to ASTM D 5590.

2.	Copies of the manufacturer’s current ISO certification.

3.	Ten (10) references clearly indicating the membrane manufacturer has successfully completed projects of similar scope and nature for a minimum of ten (10) years.

4.	Manufacturer’s complete set of details for air barrier membrane system showing a continuous plane of air tightness throughout the building envelope.

- Acceptable alternates will be confirmed by addendum.  Substitute materials not approved in writing prior to bid date shall not be permitted for use on this project.

1.12	WARRANTY

A.	Provide manufacturer’s standard 10-year material warranty.

PART 2 – PRODUCTS

  - MATERIALS

- Air/vapor barrier membrane components and accessories must be obtained as a single-source from the membrane manufacturer to ensure total system compatibility and integrity.

      - Acceptable Manufacturer:	Henry Company

999 N Sepulveda Blvd, Suite 800

El Segundo, CA 90245

(800) 598-7663

www.Henry.com

2.       Acceptable Manufacturer:	Bowman Construction Supply

10801 E. 54th Avenue

Denver, CO 80239

Phone: (303) 696-8960

www.bowmanconstructionsupply.com

2.02	MEMBRANES (Basis-of-Design)

A.	Primary liquid air/vapor barrier membrane for temperatures above 40 degrees F shall be Air-Bloc 32MR manufactured by Henry; a one component elastomeric membrane, trowel or spray applied, compatibility with substrates, transition membranes and insulation.  Membrane shall have the following physical properties:

1.	Meets the air leakage requirements of the Massachusetts Commercial Energy Code (780 CMR, Ch. 13) Energy Conservation Requirements for the Building Envelope,

2.	Air permeability: 0.00012 CFM/ft2 @ 1.6 lbs/ft2 to ASTM E 2178 and ASTM E 283 and have no increased air leakage when subjected to a sustained wind load of 10.5 lbs/ft2 for 1 hour and gust wind load pressure of 62.8 lbs/ft2 for 10 seconds when tested at 1.6 lbs/ft2  to ASTM E 331,

3.	Rating 0 -No fungal growth as tested to ASTM D 5339,

4.	Water vapor permeance: 0.08 perms to ASTM E 96,

5.	VOC Content: No appreciable VOC (less then 100g/L),

6.	Elastic Recovery: 90% to CAN/CGSB 37.58M86,

7.	Meets CAN/CGSB-51-33 Type I Water Vapor Permeance requirements

B.	Self-adhering transition membrane shall be Blueskin SA, LT, or HT manufactured by Henry; an SBS modified bitumen, self-adhering sheet membrane complete with a blue engineered thermoplastic film.  Membrane shall have the following physical properties:

1.	Air leakage: <0.0001 CFM/ft² @1.6 lbs/ft2 to ASTM E2178,

2. 	Vapor permeance: 0.03 perms to ASTM E 96,

3.	Membrane Thickness: 0.0394 inches (40 mils),

4.	Low temperature flexibility: -22 degrees F to CGSB 37-GP-56M,

5.	Elongation: 200% to ASTM D412-modifed

Spec Note: Masonry Flashings are typically specified in Section 04 05 23.16.  Coordinate material selection and application with air barrier membrane systems.  Blueskin TWF is specifically designed for flashing details with a stronger film and resistance to flow.

C.	Alternate self-adhering membrane for all window and window sill flashings, door openings, inside and outside corners and other transitions shall be HE200 AM Metal Clad manufactured by Henry; a SBS modified bitumen, self-adhering sheet membrane complete with surface layer of metallic aluminum film that many sealants adhere well to.  Membrane shall have the following physical properties:

- Peel Adhesion to Primed Steel 15.0 to ASTM D 1000,

- Vapor Permeance: < 0.014 perms to ASTM E 96,

- Membrane Thickness: 0.0443 inches (45 mils),

- Low temperature flexibility: -15 degrees F to ASTM D146 min,

- Elongation: 40% to ASTM D412-modifed min

D	Liquid-applied flashing alternate to self-adhered flashing membranes for all window, door, MEP penetrations, inside/outside and dissimilar material connections shall be Air-Bloc LF manufactured by Henry; a moisture-curing single component STPe liquid-applied flashing compatible with a variety of substrates and all Henry liquid and self-adhered air barrier membranes.  Liquid-flashing shall have the following physical properties:

  - Elongation: minimum 250% minimum to ASTM D412

  - Tensile Strength: 132% psi minimum to ASTM D412

  - Nail Sealability: Pass to AAMA 711

  - VOC Content: 25 g/L max

  - Solids Content by Volume: 95%

  - Moisture Absorption: .1% to ASTM D570

E.	Through-wall flashing membrane (Self-Adhering) shall be Blueskin TWF manufactured by Henry; an SBS modified bitumen, self-adhering sheet membrane complete with a yellow engineered thermoplastic film.  Membrane shall have the following physical properties:

1.	Membrane Thickness: 0.0394 inches (40 mils),

2.	Film Thickness: 4.0 mils,

3.	Flow (ASTM D5147): Pass @ 212 degrees F,

4.	Puncture Resistance: 134 lbf to ASTM E 154,

5.	Tensile Strength (film): 5000 psi minimum ASTM D 882,

6.	Tear Resistance: 45lbs.-MD, 17lbs.-CD to ASTM D1004,

7.	Low temperature flexibility: -22 degrees F to CGSB 37-GP-56M

2.03	ADHESIVE AND PRIMERS

A.	Primer for self-adhering membranes at temperatures above 25 degrees F shall be Aquatac Primer manufactured by Henry; a polymer emulsion based adhesive, quick setting.  Primer shall have the following physical properties:

1.	Color: Aqua,

2.	Weight: 8.3 lbs/gal,

3.	Solids by weight: 53%,

4.	Water based, no solvent odors,

5.	Drying time (initial set): 30 minutes at 50% RH and 70 degrees F

B.	Adhesive for self-adhering membranes at all temperatures shall be Blueskin Adhesive manufactured by Henry, a synthetic rubber based adhesive, quick setting, having the following physical properties:

1.	Color: Blue,

2.	Weight: 6 lbs/gal,

3.	Solids by weight: 35%,

4.	Drying time (initial set): 30 minutes

C.	Adhesive with low VOC content for self-adhering membranes at all temperatures shall be Blueskin LVC Adhesive manufactured by Henry, a synthetic rubber based adhesive, quick setting, having the following physical properties:

1.	Color: Blue,

2.	VOC: <240 g/L,

3.	Solids by weight: 40%,

4.	Drying time (initial set): 30 minutes

2.04	JOINT TREATMENT, PENETRATION & TERMINATION SEALANT

A.	Joint Treatment, penetration and termination Sealant shall be HE925 BES Sealant manufactured by Henry; a moisture cure, medium modulus polymer modified sealing compound having the following physical properties:

        - Compatible with sheet air barrier, roofing and waterproofing membranes and substrate,

        - Complies with Fed. Spec. TT-S-00230C, Type II, Class A,

        - Complies with ASTM C 920, Type S, Grade NS, Class 25,

        - Elongation: 450 – 550%,

        - Remains flexible with aging,

        - Seals construction joints up to 1 inch wide

B.	Alternate joint treatment fabric: HE 183 yellow open weave glass fabric or approved equal.

Spec Note: THERMAL SHORT CIRCUITING To reduce heat loss and restrict air convection between the air barrier membrane and insulating materials, secure the insulation in place with an insulation adhesive applied in a serpentine pattern and butter the joints of panels.  Coordinate with the Cavity Wall Insulation Section.

2.05	INSULATION ADHESIVE

A.	Insulation adhesive shall be Air-Bloc 21 Insulation Adhesive manufactured by Henry; a synthetic, trowel applied, rubber based adhesive, having the following physical properties:

1.	Compatibility: With air barrier membrane, substrate and insulation,

2.	Air leakage:  0.0026 CFM/ft2 @ 1.6 lbs/ft2 to ASTM E283,

3.	Water vapor permeance: 0.03 perms to ASTM E96,

4.	Long term flexibility: CGSB 71-GP-24M

PART 3 EXECUTION

3.01	EXAMINATION

A.	Verify that surfaces and conditions are ready to accept the Work of this section.  Notify [engineer] [architect] [consultant] in writing of any discrepancies.  Commencement of the work or any parts thereof shall mean acceptance of the prepared substrates.

B.	All surfaces must be sound, dry, clean and free of oil, grease, dirt, excess mortar or other contaminants.  Fill spalled areas in substrate to provide an even plane.  Strike masonry joints flush.

C.	Where curing compounds are used they must be clear resin based without oil, wax or pigments.

D.	Do not proceed with application of air barrier membrane when rain is expected within 24 hours.

E.	Condition materials to room temperature prior to application to facilitate handling.

3.02	SURFACE PREPARATION

A.	Water Based Elastomeric Emulsion Air Barrier Membrane: liquid applied water based air barrier membrane may be applied to green concrete 16 hours after forms are removed.

B.	Ensure all preparatory Work is complete prior to applying primary air barrier membrane.

C.	Mechanical fasteners used to secure sheathing boards or penetrate sheathing boards shall be set flush with sheathing and fastened into solid backing.

3.03	INSTALLTION OF AIR VAPOR BARRIER SYSTEM

A.	JOINT TREATMENT

1.	Seal joints ¼ inch and less between panels of exterior grade gypsum sheathing, plywood, OSB or cementitious panels with joint treatment sealant.

a.	Fill joint between sheathing with approved joint treatment sealant ensuring contact with all edges of sheathing board.  Strike flush any excess sealant over joint layer to form a continuous layer over the joint.

2.	Seal gaps and voids or irregular joints greater than ¼ inch between panels of exterior grade gypsum, exterior grade gypsum sheathing, plywood, OSB or cementitious panels with a strip of self-adhering air/vapor barrier transition membrane lapped a minimum of 1-1/2 inches on both sides of the joint.

a.	Prime surfaces as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering air/vapor barrier transition membrane, remove protective film and press firmly into place.  Ensure minimum 2 inches overlap at all end and side laps of membrane.

c.	Roll all laps and membrane with a counter top roller to ensure seal.

3.	Alternately, joints not exceeding 1/8 inch can be sealed with yellow open weave glass fabric.

a.	Apply yellow open weave glass fabric centered over joint followed by a 1/8 inch (120mils) thick trowel application of air/vapor barrier membrane.

b.	Allow to dry prior to application of primary air/vapor barrier membrane.

B.	INSIDE AND OUTSIDE CORNERS

1.	Seal inside and outside corners of sheathing boards with a strip of self-adhering air/vapor barrier transition membrane extending a minimum of 3 inches on either side of the corner detail.

a.	Prime surfaces as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering transition membrane, remove protective film and press firmly into place.  Ensure minimum 2 inches overlap at all end and side laps of membrane.

c.	Roll all laps and membrane with a counter top roller to ensure seal.

C.	CRACK TREATMENT – MASONRY AND CONCRETE

1.	Seal cracks over 1/16 inches in masonry and concrete with a strip of self-adhering air/vapor barrier transition membrane lapped a minimum of 1 1/2 inches on both sides of the crack.

a.	Prime surfaces as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering air/vapor barrier transition membrane, remove protective film and press firmly into place.  Ensure minimum 2 inches overlap at all end and side laps of membrane.

c.	Roll all laps and membrane with a counter top roller to ensure seal.

2.	Alternately, static cracks 1/16 inch to 1/8 inch can be sealed with primary air/vapor barrier membrane.

a.	Fill crack with primary air barrier membrane.

b.	Allow to dry prior to application of primary air/vapor barrier membrane.

D.	Liquid-Applied Flashing Option

- Use for door and window openings, MEP penetrations and dissimilar material connections.

a.	Apply liquid flashing to all material joints and tool smooth.

b.	Apply liquid flashing in a serpentine fashion to the entire window opening and tool smooth to a minimum 25 mils wet film thickness.  Spread material to cover the inside of rough openings and extend 4 inches onto adjacent surfaces.  Create a slight positive slope towards the exterior of sill conditions by applying more material to the interior side of sills to create a taper towards the exterior while maintaining a minimum 25 mils wet film thickness.

c.	Apply liquid flashing to MEP penetrations with a maximum of ½ inch annular space.  Extend liquid flashing a minimum 4 inches onto penetrating item and surrounding surfaces to a minimum of 25 mils dry film thickness.

d.	Apply liquid flashing to inside/outside corners and dissimilar material connections.  Extend a minimum 4 inches onto adjacent surfaces a minimum of 4 inches and a minimum wet film thickness of 25 mils dry film thickness.

e.	Apply fluid-applied membrane air barrier onto liquid lashing a minimum of 2 inches.

E.	TRANSITON AREAS

1.	Tie-in to structural beams, columns, floor slabs and intermittent floors, parapet curbs, foundation walls, roofing systems and at the interface of dissimilar materials as indicated in drawings with self-adhering air/vapor barrier transition membrane.

a.	Prime surfaces as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering air/vapor barrier transition membrane, remove protective film and press firmly into place.  Provide minimum 3 inch lap to all substrates.

c.	Ensure minimum 2 inch overlap at all end and side laps of membrane.

d.	Roll all laps and membrane with a counter top roller to ensure seal.

Spec Note: Best construction practice requires window sill details to be waterproofed and flashed prior to the placement of the window assembly.  SBS modified self-adhering membranes provide the flexibility to wrap around the configurations of wall openings and provide the self-sealing properties to guard against leaks by mechanical fastener attachment.

Spec Note: Specific window manufacturer’s instructions over-ride Henry specifications for window openings.  The installer is responsible to resolve any conflicts in the specifications, sequencing, materials or techniques between window manufacturer’s instructions and Henry specifications BEFORE CONSTRUCTION.

F.	WINDOWS AND ROUGH OPENINGS

1.	Wrap rough openings with self-adhering membrane as detailed.

a.	Prime surfaces as per manufacturers’ instructions and allow to dry.

b.	Align and position self-adhering air/vapor barrier transition membrane, remove protective film and press firmly into place.  Ensure minimum 2 inch overlap at all end and side laps of membrane.

c.	Roll all laps and membrane with a counter top roller to ensure seal.

G.	THROUGH-WALL FLASHING MEMBRANE

1.	Apply through-wall flashing membrane along the base of masonry veneer walls and over shelf angles as detailed.

a.	Prime surfaces and allow to dry, press membrane firmly into place, over lap minimum 2 inches at all end and side laps.  Promptly roll all laps and membrane to ensure the seal.

b.	Applications shall form a continuous flashing membrane and shall extend up a minimum of 8 inches up the back-up wall.

c.	Seal the top edge of the membrane where it meets the substrate using termination sealant.  Trowel-apply a feathered edge to seal termination to shed water.

d.	Install through-wall flashing membrane and extend 1/2 inch from outside edge of veneer.  Provide “end dam” flashing as detailed.

H.	PRIMARY AIR/VAPOR BARRIER

1.	Apply by spray or flat trowel a complete and continuous unbroken film of liquid air/vapor and rain barrier membrane.

a.	For temperatures above 40 degrees F and rising, apply one component water based elastomeric emulsion air/vapor barrier membrane at a rate of 20 sq.ft/gallon to a uniform wet film thickness of 75 mils for smooth surfaces depending upon surface texture and porosity.  For rough surfaces, apply elastomeric emulsion air/vapor barrier membrane at a rate of 14 sq.ft/gallon to a uniform wet film thickness of 110 mils depending upon surface texture and porosity.

2.	Spray-apply or trowel around all projections and penetrations ensuring a complete and continuous air barrier membrane.  Lap liquid applied membrane 1 inch over self-adhering membranes to seal leading edge.

3.	Allow air barrier membrane to dry as per manufacturers recommendations prior to placement of insulating materials.

3.04	APPLICATION OF TERMINATION SEALANT

A.	Seal membrane terminations, heads of mechanical fasteners, masonry tie fasteners, around penetrations, duct work, electrical and other apparatus extending through the primary water resistive air barrier membrane and around the perimeter edge of membrane terminations at window and door frames with specified termination sealant.

3.05	FIELD QUALITY CONTROL

A.	Make notification when sections of Work are complete to allow review prior to covering air barrier system.

3.06	INSTALLATION OF INSULATION

A.	Coordinate with Cavity Wall Insulation Section [XXXXX] for insulating materials.

B.	Apply insulation adhesive in a serpentine pattern over the air barrier membrane.

1.	Dab Method: Apply walnut-sized dabs of insulation adhesive spaced 6 inches on center to substrate.  Apply insulation using sufficient hand pressure to compress dabs up to 2 inches in diameter.

2.	Bead Method: Apply ¼ inch beads 6 inches on center in a serpentine pattern.

C.	Immediately embed insulation into the adhesive and press firmly into place to ensure full contact.  Apply additional adhesive if allowed to skin over.

Spec Note:  Insulation ends and edges are recommended to be buttered with insulation adhesive to prevent thermal bridging and air and moisture circulation behind insulation boards.

3.07	PROTECTION

A.	Damp substrates must not be inhibited from drying out.  Do not expose the backside of the substrate to moisture or rain.

B.	Cap and protect exposed back-up walls against wet weather conditions during and after application of membrane.  Drying time varies depending on temperature and relative humidity. Protect air barrier Work against wet weather conditions for a minimum of 24 hours.

C.	Air barrier membranes are not designed for permanent exposure.  Good practice calls for covering as soon as possible.  Special consideration must be given to the exposed un-insulated membrane during winter months of construction so as to avoid the risk of condensation.

END OF SECTION