CCW-MIRAPLY-V

MATERIAL CERTIFICATION

This is to certify that CCW MiraPLY-V is a vertical grade, self-adhering membrane that is comprised of a tough, durable and flexible reinforced TPO backing with a butyl alloy adhesive designed for blindside waterproofing in below-grade construction.  CCW MiraPLY is manufactured in the USA.

CCW manufactures CCW MiraPLY-V Membrane to comply with the following ASTM typical property values and meets the specification requirements:

| CCW-MiraPLY-V-Property | Test Method | Unit | Typical Value* |
| --- | --- | --- | --- |
| TPO |  | mils (mm) | 45 (1.14) |
| Butyl Alloy |  | mils (mm) | 25 (.64) |
| Thickness | ASTM D 1970 | mils (mm) | 70 (1.78) |
| Water Vapor Transmission | ASTM E 96 B | perms | 0.090 |
| Tensile Strength | ASTM D 882 | psi | 1,500 |
| 300% Modulus | ASTM D 412 | psi | 1,000 |
| 900 T-Peel | ASTM D 1876 | lb. | 15.0 |
| Elongation @ Break @ 230C (Die C) | ASTM D 412 | % | 325 |
| Flexibility Temperature @ -290C (-200F) | ASTM D 1970 | Pass/Fail | No Cracking - Pass |
| Hydrostatic Pressure Resistance | ASTM D 5385 | ft. | >231 (100 psi) |
| Peel Strength Over Poured Concrete (tested w/2” strips) | ASTM D 903 | lb. | 5.6 |
| Puncture Resistance Load at Puncture | ASTM E 154 | lb. | 375 |
| Tear Strength | ASTM D 624 | psi | 1,000 |
| Soil Decay Testing – E 96 Permeance | ASTM E 154 | - | pass |
| Soil Decay Testing – Weight Loss | ASTM D 154 |  | Pass |
| Lateral Water Migration Resistance | ASTM D5385 modified | psi | Pass at 100 psi (231 ft) of hydrostatic pressure |

Rev. January 18, 2016